## Slide 1: AIDAINNOVA WP10
Samuel Unterhofer
R&D engineer

## Slide 2: Csem at a glance
115.4
M TURNOVER
in 2024
1984
FOUNDED
> 50
VENTURES
since 1984
630
SPECIALISTS
We are a public-private, non-profit Swiss technology innovation center
We enable competitiveness by developing and transferring world-class technologies to the industrial sector
We fuel the innovation of more than 200 industrial partners every year.
177
PATENT
FAMILIES
Tissot T-Touch Connect Sport

## Slide 3: We focus on three research priorities

## Slide 4: OUR MAIN RESEARCH TOPICS
HIGH-PRECISION AM
INTEGRATED FUNCTIONS
ENABLING MATERIALS & PREDICTIVE QUALITY

## Slide 5: OUR CORE COMPETENCIES IN AM
LITHOGRAPHY BASED AM
AEROSOL JET PRINTING
LASER POWDER BED FUSION
DESIGN FOR AM
MATERIAL CHARACTERIZATION

## Slide 6: Additive Manufacturing Infrastructure
EOS-M290 FDR (40 µm laser spot)
Build volume: (250 x 250 x 300 mm3)
Materials: Al, Ti alloys, Inconel, Tungsten, Copper
LASER POWDER BED FUSION
Trumpf TruPrint 1000 (30 µm laser spot)
Build volume: (Ø100 x 100 mm3)
Materials: Al, Ti alloys, NiTi, Composites, Multimaterials, High entropy alloys, etc.
LITHOGRAPHY BASED AM (polymer, metal, ceramic)
BMF MicroArch S240 (10 µm pixel)
Build volume: (100 x 100 x 75 mm3)
Materials: Acrylates, Alumina, Zirconia
Incus Hammer Lab35 (35 µm pixel)
Build volume: (56 x 90 x 120 mm3)
Materials: 316L, Ti6Al4V, Copper
Solflex 635UHD (35 µm pixel)
Build volume: (130 x 110 x 130 mm3)
Materials: Acrylates
AEROSOL JET PRINTING
Optomec AJ300 (10 - 2000 µm line)
Build area: (300 x 300 mm2)
Materials: Ag, Au, Pt, Cu, Carbon black, Epotek, Polyimide

## Slide 7: CSEM aim for AIDAinnova WP10
Define the optimal geometrical features attainable for 3D printed ultra-thin cold plates in metal alloys

## Slide 8: CSEM objectives for AIDAinnova WP10
Test samples
  Thermal conductivity
  Long cavity test
  Pipe roughness
  Flatness (multi-microchannel)
Minimal wall thickness
  Minimum leak-tight wall thickness
Powder removal
  Minimum ratio (D/L) for single straight pipes
  Design feature for 180° bent pipes
  Minimum ratio (D/L) for multi-microchannel
Smart pipe
  Printing parameters
  Aluminium: Al-12-Si
Two disk dimensions
With and without heat treatment (350°C, air, 1h)
Result: 130-160 W/mK

## Slide 9: CSEM objectives for AIDAinnova WP10
Test samples
  Thermal conductivity
  Long cavity test
  Pipe roughness
  Flatness (multi-microchannel)
Minimal wall thickness
  Minimum leak-tight wall thickness
Powder removal
  Minimum ratio (D/L) for single straight pipes
  Design feature for 180° bent pipes
  Minimum ratio (D/L) for multi-microchannel
Smart pipe
  Printing parameters
  Aluminium: Al-12-Si
Prototype with one evaporative channel
Glass cover
Metal plate
O-ring
Result: no leached particles observed

## Slide 10: CSEM objectives for AIDAinnova WP10
Test samples
  Thermal conductivity
  Long cavity test
  Pipe roughness
  Flatness (multi-microchannel)
Minimal wall thickness
  Minimum leak-tight wall thickness
Powder removal
  Minimum ratio (D/L) for single straight pipes
  Design feature for 180° bent pipes
  Minimum ratio (D/L) for multi-microchannel
Smart pipe
  Printing parameters
  Aluminium: Al-12-Si

## Slide 11: CSEM objectives for AIDAinnova WP10
Test samples
  Thermal conductivity
  Long cavity test
  Pipe roughness
  Flatness (multi-microchannel)
Minimal wall thickness
  Minimum leak-tight wall thickness
Powder removal
  Minimum ratio (D/L) for single straight pipes
  Design feature for 180° bent pipes
  Minimum ratio (D/L) for multi-microchannel
Smart pipe
  Printing parameters
  Aluminium: Al-12-Si
Method tested:
He leaking rate + Water burst up to 80 bars

## Slide 12: CSEM objectives for AIDAinnova WP10
Test samples
  Thermal conductivity
  Long cavity test
  Pipe roughness
  Flatness (multi-microchannel)
Minimal wall thickness
  Minimum leak-tight wall thickness
Powder removal
  Minimum ratio (D/L) for single straight pipes
  Design feature for 180° bent pipes
  Minimum ratio (D/L) for multi-microchannel
Smart pipe
  Printing parameters
  Aluminium: Al-12-Si

## Slide 13: CSEM objectives for AIDAinnova WP10
Test samples
  Thermal conductivity
  Long cavity test
  Pipe roughness
  Flatness (multi-microchannel)
Minimal wall thickness
  Minimum leak-tight wall thickness
Powder removal
  Minimum ratio (D/L) for single straight pipes
  Design feature for 180° bent pipes
  Minimum ratio (D/L) for multi-microchannel
Smart pipe
  Printing parameters
  Aluminium: Al-12-Si

## Slide 14: CSEM objectives for AIDAinnova WP10
Test samples
  Thermal conductivity
  Long cavity test
  Pipe roughness
  Flatness (multi-microchannel)
Minimal wall thickness
  Minimum leak-tight wall thickness
Powder removal
  Minimum ratio (D/L) for single straight pipes
  Design feature for 180° bent pipes
  Minimum ratio (D/L) for multi-microchannel
Smart pipe
  Printing parameters
  Aluminium: Al-12-Si

## Slide 15: CSEM objectives for AIDAinnova WP10
Phase 1
  Benchmarking for AM grade powder
  Development of process parameters
Phase 2
  Same investigation as Al-12-Si but on a limited number of samples
  KOVAR: Fe-29-Ni-17-Co

## Slide 16: CSEM objectives for AIDAinnova WP10
Phase 1
  Benchmarking for AM grade powder
  Development of process parameters
Phase 2
  Same investigation as Al-12-Si but on a limited number of samples
  KOVAR: Fe-29-Ni-17-Co

## Slide 17: CSEM objectives for AIDAinnova WP10
Phase 1
  Benchmarking for AM grade powder
  Development of process parameters
Phase 2
  Same investigation as Al-12-Si but on a limited number of samples
  Joint feasibility between aluminium and kovar
  µCT scan + Thermal cycling
  KOVAR: Fe-29-Ni-17-Co

## Slide 18: Multimaterial printing to join kovar & alu
EDX Mapping
SEM
Printing direction

## Slide 19: Multimaterial printing to join kovar-alu
Printing direction
CTE increasing
Al
Kovar (Fe)
250 µm

## Slide 20: Conclusion
Al-12-Si
  Material properties has been characterized
  Minimum leak-tight wall thickness has been discovered
  Minimum ratio (D/L) for powder removal on straight pipes & 180 degree-bent pipes has been discovered
Kovar
  Benchmarking for AM grade powder has been done
  Process parameters has been developped
  Joint feasibility between aluminium and kovar has been demonstrated
  Joint reliability under investigation