## Slide 1: Description of the Leak Tests Performed on EWBs at CERN
L. Hermida Pena (SY-STI-TCD)
14/07/25

## Slide 2: Outline
Introduction
Leak tests performed at CERN
Status of the Tests & Results
Conclusions

## Slide 3: Outline
Introduction
Leak tests performed at CERN
Status of the Tests & Results
Conclusions

## Slide 4: Introduction
  The Edge Welded Bellows are critical components of the collimators. They allow for the displacement of the shaft and create an interface between Vacuum and the atmospheric pressure.
Mobile table
Shaft
Jaw
Cooling pipe
Courtesy of: C. Piccinni

## Slide 5: New Production 2025
  A new production was launched in January 2025 due to poor cycling behaviour with the following configuration:
  As of 14/07/2025:
  LHCTCTP_0054: Fully delivered on the 05/06/2025
  LHCTCLPX__0160: Fully delivered
Bellow type | Final Configuration | Series Quantity | Test bellows
LHCTCTP_0054 Index AG | 70 convolutions (vs prod. 2024: 58) | 101 | 8
LHCTCLPX__0160 Index AC | 82 convolutions (vs prod. 2024: 61) | 67 | 8

## Slide 6: SAT
  As stated in DO-33714/SY/HL-LHC, the received bellows are undergoing the following Site Acceptance Tests:
  Leak Test
  Cycling test
  Metrology

## Slide 7: Outline
Introduction
Leak tests performed at CERN
Status of the Tests & Results
Conclusions

## Slide 8: Leak Tests Performed at CERN
  LHCTCLPX_T0132
  Double-Beam
  LHCTCSPMT0068
  Single-Beam

## Slide 9: Leak Tests Performed at CERN
  LHCTCLPX_T0132
  Seals
  Shaft
  Cover
  Support

## Slide 10: Leak Tests Performed at CERN in July 2025
  Visual Inspection
  Installation on the Tooling
  Gas evacuation
  Helium mass spectroscopy
  Every bellow is inspected visually to check for unconformities.

## Slide 11: Leak Tests Performed at CERN in July 2025
  Visual Inspection
  Installation on the Tooling
  Gas evacuation
  Helium mass spectroscopy
  The bellows are installed in the tooling.

## Slide 12: Leak Tests Performed at CERN in July 2025
  Visual Inspection
  Installation on the Tooling
  Gas evacuation
  Helium mass spectroscopy
  The bellows are pumped down. The helium leak test sensitivity achieved is 2.00E-10 mbar.l/s.

## Slide 13: Leak Tests Performed at CERN in July 2025
  Visual Inspection
  Installation on the Tooling
  Gas evacuation
  Helium mass spectroscopy
  Helium is sprayed on the outside of the bellow, and a mass spectrometer inside the vacuum system detects if helium gets in.

## Slide 14: Outline
Introduction
Leak tests performed at CERN
Status of the Tests & Results
Conclusions

## Slide 15: Status of the SAT & Results
  2 leaky bellows have been detected
Bellow Reference | Date of arrival at CERN | Date of He leak test | Leak Rate
HCTCP_054-VT000015 | 05/06/2025 | 4/07/2025 | 3.5E-5 mbar.L.s-1
HCTCLPX_160-VT000002 | 25/06/2025 | 7/07/2025 | 3.1E-6 mbar.L.s-1

## Slide 16: HCTCLPX_160-VT00015
  Pictures taken on the weld number 35 from the big flange.

## Slide 17: HCTCLPX_160-VT00015
  Pictures taken on the weld number 35 from the big flange.

## Slide 18: HCTCLPX_160-VT00015
  Pictures taken on the weld number 35 from the big flange.

## Slide 19: HCTCLPX_160-VT00015
  Pictures taken on the weld number 35 from the big flange.

## Slide 20: HCTCTP_054-VT000015

## Slide 21
HCTCTP_054-VT000015 Tomography

## Slide 22: HCTCLPX_160-VT00002 Tomography

## Slide 23: Status of the SAT & Results
Test | # bellows | Outcome
Leak tightness | 80/101 | OK
Metrology | 12 CMM + 2 Tomography | OK
UHV cleanliness | To be performed as last SAT step | N/A
Destructive cycling | 8 | See tables below
LHCTCTP_0054: full series received on CW 23
Cycling outcomes (@ stroke ± 20 mm; 7 s/Cy):
Bellow S/N | # cycles
HCTCTP_0054vAG-VT100012 | 190 736
HCTCTP_0054vAG-VT100013 | 190 736
HCTCTP_0054vAG-VT100090 | 190 736
HCTCTP_0054vAG-VT100108 | 190 736
Bellow S/N | # cycles
HCTCTP_0054vAG-VT100010 | 45 880
HCTCTP_0054vAG-VT100008 | 45 880
HCTCTP_0054vAG-VT100003 | 45 880
HCTCTP_0054vAG-VT100001 | 45 880
Cycling interrupted before leak appearance
As of 30/06 morning, 9.30 am; no leak. Cycling still ongoing.
Courtesy of: C. Piccinni

## Slide 24: Status of the SAT & Results
Test | # bellows | Outcome
Leak tightness | 19/75 | OK
Metrology | 12 CMM + 2 Tomography | TBD CMM, Tomo OK
UHV cleanliness | To be performed as last SAT step | N/A
Destructive cycling | 4 | See tables below
LHCTCLPX_0160: full series received on CW 23
Cycling outcomes (@ stroke ± 20 mm; 7 s/Cy):
Bellow S/N | # cycles
HCTCLPX_160-VT000039 | Ongoing
HCTCLPX_160-VT000014 | Ongoing
HCTCLPX_160-VT000016 | Ongoing
HCTCLPX_160-VT000017 | Ongoing
Courtesy of: C. Piccinni

## Slide 25: Outline
Introduction
Leak tests performed at CERN
Status of the Tests & Results
Conclusions

## Slide 26: Conclusions
2 bellows have leaked:
  HCTCP_054-VT000015
  HCTCLPX_160-VT000002
This is a critical problem, as all bellows have to be leak tight, and this should have been detected before delivery.
CERN will continue to perform the leak tests on the whole production.
The rest of the SAT so far are ok.

## Slide 27: Thank you for your attention