## Slide 1: Optical Fibre Sensing CRAB Cryomodule
Michael GUINCHARD on behalf of EN-MME-EDM
STFC Visit

## Slide 2: Introduction
  here

## Slide 3: Introduction
Mechanical measurements are done on several types of components : superconducting magnets, dumps, RF cavity, detectors in different conditions as electro-magnetic field, vacuum, radiation, cryogenic, water, etc…

## Slide 4: Introduction
STRAIN MEASUREMENTS IS A KEY TECHNIQUE !
Strong interest in optical strain measurement systems for harsh environmental conditions ;
Beginning of the study in 2011 with FBG technology;
Main requirements:
    Optical strain measurements
    1.9 K up to 400 K
    DAQ integrated system
As a measurement lab, we must perform a metrology qualification of new systems before field implementation.

## Slide 5: Strain Sensing Techniques at CERN
Robust well proven technology
Bulky cabling
Electrical Strain Gauge (ESG)
Fiber Bragg Grating (FBG)
Rayleigh Backscattering (RBS)
Discrete
Distributed
80’s
2011
2021
Single optical fiber
Challenging bonding process for
cryogenic temperatures
Single optical fiber
Sub mm spatial resolution
Challenging bonding process for cryogenic temperatures

## Slide 6: Principles of Optical Fibre Sensing (OFS)
Intrinsic sensors
When the OF itself is the sensing element The physical measurand modulates one of the light properties.
Extrinsic sensors
When the OF is only used to transmit the light The physical measurand modulates the light emission in an object external to the fibre.
Optical Fibres Sensing refers to the use of optical fibres to measure various physical parameters: temperature, strain, pressure, chemical composition, vibrations, radiation, rotation, shape, EM field, etc.
The information is encoded in at least one property of the light travelling in the optical fibre: intensity, phase, polarization, wavelength

## Slide 7: Working principle of the FBG
Through the coating inscription technique;
Fabricated with ultra short femtosecond laser pulses [7].
FBG interrogator
Optical fiber
Temperature sensing
Fiber Bragg grating
Strain sensing
Through-coating FBG inscription process [4].
[8]
Reflection spectra of an FBG presenting the effect of tensile and compressive strains on the Bragg wavelength.

## Slide 8: Working principle of the RBS
Optical Frequency Domain Reflectometry (OFDR) technology in a single-mode optical fiber was reported in 1981 for the first time (Eickhoff and Ulrich, 1981) as a method to measure the spatial distribution of the Rayleigh scattering and optical losses along the optical fiber (0.5 m spatial resolution achieved) [6];
However, it has recently been investigated and commercialized for numerous monitoring applications (0.1 mm spatial resolution achieved) [11].
Rayleigh backscattering is caused by the random fluctuations in the index profile along the optical fiber.
Rayleigh scattering [9].
Rayleigh scattering from air molecules [9].
Diagram of the operating principle behind c-OFDR.
Distributed sensing in optical fiber [10].

## Slide 9: Advantages of the optical fiber strain sensors
Works in harshest environments
Flexibility
Very small;
From 125 μm down to 40 μm cladding diameter;
Less invasive than ESG;
Lightweight.
FBG technique
Real-time sensing up to 40 sensors per single optical fiber (depending on the optical interrogator performance);
Static and dynamic measurements up to 2000 Hz;
Better time resolution.
RBS technique
Ultra-high spatial resolution down to 0.65 mm;
Static and dynamic measurements up to 250 Hz;
Better spatial resolution.
Immune to electromagnetic interference;
Chemically inert;
Different optical fiber types can be used depending on the need (radiation-hard; high-temperature, water-resistant, etc.).
Source: CERN
Applications at CERN

## Slide 10: Strain sensing at cryogenic temperatures
A perhaps surprising property of optical fibers is that they remain flexible at cryogenic temperatures [12];
Zirconia ferrule has a very low thermal expansion coefficient, which reduces material stresses caused by temperature gradients; and is also very close to that of the fiber.
Hydrogen liquid is seen as one of the energy vectors of the future;
must be cooled to 20.28 K to be in liquid state;
Future emerging research with strain sensing at cryogenic temperatures.
Production and utilization of hydrogen from renewable energy [13].

## Slide 11: Technical Challenges
Adhesion technique is a crucial parameter as the deformations of the studied material need to be perfectly transferred to the sensor and need to be repeatable  Specific procedure
Adhesion technique developed internally at CERN for strain sensing experience in harsh environments such as cryogenic temperatures.
Courtesy of CERN EN-MME-MM

## Slide 12: Technical Challenges
Main temperature effects on the optical fibers :
  Strong attenuation of the optical power due to the thermal contraction (- 15 dB) which can disturb the peak tracking (optical budget issue);
  High insertion losses observed at cryogenic temperatures on the optical fiber feedthroughs / connectors.

## Slide 13: Validation Process
Optical strain gauges validation campaign down to cryogenic temperatures :
  Evaluating the repeatability and reproducibility down to 77 K;
  Evaluating the trueness of the three measuring systems down to 4.2 K according to ISO 5725.
 |  | ESG (1) | FBG (2) | RBS (3)
Apparent strain at 77 K | Mean Value (µm/m) (SS304L) | -3377 | -3924 | -3954
 | Repeatability (µm/m) | 9 | 63 | 120
 | Reproducibility (µm/m) | 32 | 78 | 122
 | Precision (%) | 1.2 % | 2.5 % | 4.3 %
Trueness at 4.2 K (%) |  | 4.3% | 3.5 % | 1.2 %
Accuracy at 4.2 K (%) |  | 4.4 % | 4.3 % | 4.5 %
LC11-3/350 – HBK®
High-reflectivity (>50%) femtosecond FBG in Polyimide coating – FBGS Technologies GmbH
Polyimide coating SM OF – Polytec GmbH

## Slide 14: Validation Process
Optical and strain gauges validation campaign down to cryogenic temperatures

## Slide 15: Applications
HL-LHC superconducting quadrupole magnets (MQXF) :
  7m length coils instrumented with OFS (FBG / discrete measurements) to assess the stress state (key parameter in the magnet performance);
  Stress monitoring performed during the loading, thermal cycles and powering processes.

## Slide 16: Applications
HL-LHC superconducting quadrupole magnets (MQXF) :
  Aluminum outer shell instrumented with OFS (RBS / distributed measurements) to assess the stress state during loading operation;
Optical fiber glued around the perimeter
Start point
End point
Azimuthal Strain (um/m) @ 200 bar
Alignment pin
(optical fiber not glued)

## Slide 17: Applications
HL-LHC superconducting quadrupole magnets (MQXF) :
  Real time data acquisition + Cloud data streaming  Grafana Dashboards

## Slide 18: Applications
Embedded OFS in carbon fiber structure (EP-DT Collaboration)
Courtesy of CERN EN-MME-MM

## Slide 19: Developments
Optical feedthrough development in the EN-MME (Design, FEA, Workshop) :
  Some issues to extract optical fiber signal from 1.9 K bath with commercial connectors ;
  Internal development to produce a brazed solution without connectors to improve the optical losses at cold.
Brazing methodology :
Single-mode pure-silica core optical fiber with 35 μm ± 5 % Cu-alloy thickness;
OFE copper inserts also brazed into the center of the AISI 316LN flange
Lab Cryocooler + LUNA OFDR
Courtesy of CERN EN-MME-FW

## Slide 20: Developments
Optical feedthrough development in the EN-MME group :
Performance after 10 thermal cycles :
- Leak tight at 10-12 mbar.l/s;
- No optical losses visible at 77 K ;
- Next tests will be performed at 1.9 K.

## Slide 21: Crab Cavity instrumentation Design
Michael GUINCHARD on behalf of EN-MME-EDM
STFC Visit

## Slide 22: Fiber Bragg grating based strain sensor
lhcacfis0037

## Slide 23: Optical fiber bonding
Optical fiber bonding on the blades.

## Slide 24: Fiber Bragg grating based strain sensor

## Slide 25: Optical fiber bonding
Optical fiber bonding on the FPC tubes.

## Slide 26: Optical fiber flange configuration
Flange
Receptacle R03 optical connector
Plug P01
optical connector
Insulating vacuum
Outside environment
Atmospheric pressure
Crab cavity design
Evaluation of the strain along the blades and FPC:
Bending strain;
Traction stress.

## Slide 27: Optical fiber flange configuration
Evaluation of the strain along the blades and FPC:
Bending strain;
Traction stress.

## Slide 28: Crab Cavity instrumentation Results
Michael GUINCHARD on behalf of EN-MME-EDM
STFC Visit

## Slide 29: Transport results – Optical measurement system
Chart: Temperature = f(Times)
Stop Measurement during the night
Full transport data
Transport effects
Low frequency effects are related to temperature

## Slide 30: Transport results – Optical measurement system
Typical response of the blade instrumentation during transport event
Strain (m/m)

## Slide 31: Transport results – Optical measurement system
Chart: Temperature = f(Times)
Stop Measurement during the night
Full transport data

## Slide 32: Transport results – Optical measurement system
 | 18th August 2023 | 17th October 2023 | 23th October 2023 | variation due to transport
 | Strain (µm/m) | Strain (µm/m) | Strain (µm/m) | Strain (µm/m)
CAV1_FPC_Secondary_Line | 29.12 | -13.4 | -23.8 | -10.4
CAV1_FPC_Short_Side | -29.91 | -43.41 | -59.47 | -16.06
CAV1_FPC_Long_Side | 17.97 | -76.33 | -99.1 | -22.77
CAV1_FPC_Cavity_Line | 104.7 | -24.16 | -46.58 | -22.42
CAV1_RightBlade_Cavity_Long Side | 299.1 | 281.62 | 262.4 | -19.22
CAV1_RightBlade_Secondary_Long Side | 22.24 | -43.96 | -52.49 | -8.53
CAV1_RightBlade_Secondary_Short Side | -268.3 | -418.47 | -447.9 | -29.43
CAV1_RightBlade_Cavity_Short Side | -388.7 | -489.43 | -519.1 | -29.67
CAV1_LeftBlade_Secondary_Long Side | 90.7 | 59.36 | 26.7 | -32.66
CAV1_LeftBlade_Cavity_Long Side | 6.579 | -47.39 | -41.57 | 5.82
CAV1_LeftBlade_Cavity_Short Side | -147.3 | -242.3 | -267.74 | -25.44
CAV1_LeftBlade_Secondary_Short Side | -103.3 | -146.14 | -161.43 | -15.29
CAV2_FPC_Secondary_Line | -73.02 | -129.23 | -141.69 | -12.46
CAV2_FPC_Short_Side | 41.06 | -19.99 | -29.3 | -9.31
CAV2_FPC_Long_Side | 168.6 | 64.92 | 53.54 | -11.38
CAV2_FPC_Cavity_Line | 48.74 | -44.96 | -58.38 | -13.42
CAV2_LeftBlade_Secondary_Long Side | -182.9 | -139.04 | -170.8 | -31.76
CAV2_LeftBlade_Cavity_Long Side | -34.94 | -153.79 | -169.67 | -15.88
CAV2_LeftBlade_Cavity_Short Side | -360.1 | -411.13 | -387.81 | 23.32
CAV2_LefttBlade_Secondary_Short Side | 48.44 | -23.51 | -42.46 | -18.95
CAV2_RightBlade_Cavity_Short Side | -44.86 | -97.98 | -118.8 | -20.82
CAV2_RightBlade_Secondary_Short Side | -184.1 | -321.01 | -354.98 | -33.97
CAV2_RigthBlade_Secondary_Long Side | 150.6 | 98.07 | 64.25 | -33.82
CAV2_RightBlade_Cavity_Long Side | 26.02 | -5.79 | -31.13 | -25.34

## Slide 33: Transport Results – Worst case event
Chart: Max Peak = f (Times)
Sample rate = 4096 Hz
Sample rate = 1024 Hz
Sample rate = 1024 Hz
Sample rate = 1024 Hz
Blue frame
Sample rate = 1000 Hz
18/10/23 11h30 19/10/23_10h00 20/10/23 8h30

## Slide 34: Transport Results – Worst case event
Chart: Max Peak = f (Times)
Sample rate = 4096 Hz
Blue frame
Sample rate = 1000 Hz
18/10/23 11h30 19/10/23_10h00 20/10/23 8h30
0.2 g @ 2 Hz

## Slide 35: Repair of Cavity #1 FPC (Straightening)

## Slide 36: Repair of Cavity #1 FPC (Straightening)

## Slide 37: Crab Cavity instrumentation What’s next ?
Michael GUINCHARD on behalf of EN-MME-EDM
STFC Visit

## Slide 38: Expected instrumentation
Bladdes instrumentation will be done at CERN before shipping
FPC instrumentation will be done at STFC by CERN
Optical fiber lines will be installed at STFC by CERN

## Slide 39: What do we expect from STFC team ?
Local experts must be identified and/or trained to support our activities remotely.
Internal instrumentation based on optical fibers is useful also during assembly operations  Optical instrumentation must be connected most of the time !

## Slide 40: Discussions and Lab Visit