## Slide 1
Graphene-optimized Silicon Carbide Detector (GSCD) Plan
WG6 subproject with RG 6.4
Notes: Now let me show our proposal.

## Slide 2
Prototype —GSCD1 Prototype —GSCD2
Graphene is used as an electrode
Used as an electrode
Reduces the contact barrier
Graphene
Passivation layer
Motivation and Goals
PIN/LGAD epitaxial structure
Goals:
Reduce the contact barrier and improve the P-ohmic contact performance—— GSCD2
Reduces the rising time and improves the time sensitivity of the device.——GSCD1/GSCD2
Graphene
electrode
electrode
Notes: The motive and Goals of this proposal are using graphene to improve charge collection rate and time resolution.
There are two schemes /skiːm/:
1、Using graphene as an electrode to make GSCD one structure detector to remove the metal.
2、The GSCD two structure detector to reduce the contact barrier and improve the P-ohmic
/ˈəʊmɪk/ contact performance.

## Slide 3
Research Progress——GSCD1(G/RE PIN)
Graphene
electrode
electrode
PIN epitaxial structure
Prototype —GSCD1(G/RE PIN)
Surface Electrode PIN: SE PIN
Graphene/Ring Electrode PIN: G/RE PIN
Ring Electrode PIN: RE PIN
Rise time（ ＞ 120V）: RE PIN＞ G/RE PIN ≈ SE PIN
A small signal rise time of a device means that the device is more sensitive to time response. The graphene optimizes the RE PIN signal response time and can replace metal for particle detector electrode materials.
Surface Electrode
Ring Electrode
Pad
Ring Electrode

## Slide 4
Scientific problems to be solved
How to effectively improve charge collection rate and time resolution?
  Using graphene to reduce the contact barrier and improve the P-ohmic contact performance
  Graphene is used as an electrode
How to reduce graphene defects?
  Transfer graphene to direct growth graphene on SiC
Readout electrical board and readout ASICs?
  Improve signal-to-noise ratio
  impedance mismatch
Effect of irradiation on the performance
  Effects of different irradiation types on 4H-SiC devices
  Understanding of temperature dependence
Notes: We mainly solve the above scientific /ˌsaɪənˈtɪfɪk/ problems:
  Firstly How to effectively improve charge collection rate and time resolution?
  We can use graphene as an electrode or use it to reduce the contact barrier and improve the P-ohmic contact performance
Secondly, How to reduce graphene defects?
Transfer graphene to direct growth graphene on SiC
  Thirdly, Readout electrical board and readout ASICs need to improve signal-to-noise ratio /ˈreɪʃiəʊ/ and impedance mismatch /ɪmˈpiːdns ˌmɪsˈmætʃ/.
  Fourthly, Effect of irradiation /ɪˌreɪdiˈeɪʃ(ə)n/ on the performance: Effects of different irradiation types on graphene and SiC; Understanding of temperature dependence

## Slide 5
Deliverables & time scales & contributing institutions
No. | Title | Description | Start date | End date | Institutions
Di.1 | Fabrication of Graphene/SiC PIN | Fabrication of Graphene/SiC PIN | 1/2025 | 8/2025 | IHEP
Di.2 | Fabrication of Graphene/SiC LGAD | Fabrication of Graphene/SiC LGAD | 8/2025 | 12/2025 | IHEP
Di.3 | Electronics Readout | Development of the readout single board and ASICs | 6/2025 | 12/2025 | IHEP, IAT
Di.4 | Characterization | IV, CV, Charge collection, time resolution test | 1/2026 | 12/2026 | IHEP, JLU, IAT
Di.5 | Irradiation | Irradiation Graphene/SiC devices | 1/2027 | 6/2027 | IHEP
Di.6 | Study of Irradiation Defects | Analysis of device defects caused by different types of irradiation | 1/2027 | 6/2027 | IHEP, IAT
JLU: Jilin University
IAT: Shandong Institute of Advanced Technology
Notes: This is Deliverables & time scales & contributing institutions /ˌɪnstɪˈtjuːʃənz/. Our contributing institutions include IHEP, JLU, IAT.

## Slide 6
Collaborative work
WG2, 3, 5: characterization of irradiated and non-irradiated devices
WG4: modelling of radiation damage
WG8: dissemination and outreach
Converge on a WG6 subproject with RG 6.4 Two-dimensional material detector
Welcome to join us!
Contact Person
wangcc@ihep.ac.cn
Notes: Our proposal will work with WG2, 3, 4,5 and 8. Converge on a WG six subproject with RG six point four two-dimensional material detector. Welcome to join us! Please contact me if you are interested.