## Slide 1
Developing a 3 GHz HTS rf pulse compressor: Background

## Slide 2
High accelerating gradient

## Slide 3
Normal Conducting High Gradient
Peak surface electric fields about x 2.5 higher
https://doi.org/10.1103/PhysRevAccelBeams.21.061001,
https://doi.org/10.1103/PhysRevAccelBeams.20.052001 etc.

## Slide 4
Here in Valencia!

## Slide 5
Even higher-gradient through cooling to cryogenic temperatures

## Slide 6
Cryogenic copper - RF
https://doi.org/10.1103/PhysRevAccelBeams.21.102002
https://doi.org/10.1103/PhysRevLett.90.224801

## Slide 7
Cryogenic copper – Pulsed dc
https://doi.org/10.1103/PhysRevApplied.14.061002

## Slide 8
https://doi.org/10.1103/PhysRevSTAB.15.071002
Breakdown rate – Vacancy model

## Slide 9
Describing mobile dislocation population evolution:
Breakdown rate – Dislocation dynamics model
https://doi.org/10.1103/PhysRevLett.120.124801

## Slide 10
C3 – Cool Copper Collider
Person view:
Advantage – Lower peak power requirement, fewer power sources.
Disadvantage – Lower efficiency. Limited increase in copper conductivity compared to Carnot cooling cost.
Challenge – Micron-level alignment in LN2 environment.

## Slide 11
RF pulse compressors
RF pulse compressors are high Q cavities that can store and quickly discharge RF energy, giving a power gain. High Q0 is crucial for this application, usually around 200,000.

## Slide 12: Accelerator Outlook: Pulse Compressor
Pulse compressor tests (11.4 GHz) with HTS tape at SLAC coming soon
G.Le Sage
Photo by Ankur Dhar

## Slide 13
Axion haloscope cavities and high quality factor from HTS
Low temperature first

## Slide 14: Motivation and Cavity preparation
3) Soldering
Ag
Substrate
Buffer layers
Ag
REBCO
Cu
Solder
Solder
Cu
Ag
REBCO
Substrate
Buffer layers
Ag
Cu
Surface to coat
Cu
Solder
Cu
Ag
REBCO
Cu
Surface to coat
Cu
Substrate
Buffer layers
Ag
Cu
4) Substrate extraction
Motivation:
Axion haloscope
Increase Q
copper coating  superconducting coating
Requirement: High quality factor in a high external DC magnetic field
Tape attached at ICMAB by G. Telles, N. Lamas, X. Granados, T. Puig, J. Gutierrez

## Slide 15: Achievements
Factor of 20 improvement from room temperature Cu to 4 K HTS
Factor of 6 improvement from 4 K Cu to 4 K HTS

## Slide 16: Achievements from other Experiments
CAPP Experiment: Q0 of 1.3 E7 achieved @ 5.4 GHz and at 8 T
Differences to RADES:
Geometric factor
Almost no bending of tape
Low frequency and f2 scaling of Q

## Slide 17: Outlook: HTS direct coating for axion detectors
Coated by THEVA and Ceraco by
EB- PVD
Layer architecture
ISD deposition
    - buffer layer is required , which provides a biaxially textured surface
    - Deposition of MgO layer on an inclined substrate
Cavity made of flat pieces would have been more advantageous for this coating
Notes: EB- PVD
For growth on polycristalline substrates a buffer layer is required which provides a biaxially textured surface
A hysteresis can be seen between ramp-up and ramp-down. Surprising was the fact that the quality factor during ramp-down was always larger than during ramp-down at the same field and reaches a maximum at 0.5 T. The effect comes probably due to the shielding currents that flow within the superconductor to and concentrate the magnetic field lines. When ramping down the magnetic field from 5 T some of the currents flowing may continue flowing and reduce the magnetic field in the superconductor

## Slide 18
Now moving from low-power and low-temperature to high-temperature and high-power

## Slide 19: HTS high power characterisation test stand
Test stand
at SLAC:
High-Q X-band hemispheric cavity with a TE032-like mode at 11.4 GHz.
Zero E-field and maximum H-field on the sample
Sample accounts for ⅓ of total cavity loss
Can achieve Hpeak of about 360 mT using 50 MW XL-4 Klystron.

## Slide 20: HTS low power characterisation of flat samples
Improvement compared to | (a) HTS tape | (b) HTS coating
Cu disc @ 4 K | 10 | 16
Cu disc @ 80 K | 4 | 5
Experiment at SLAC,
plots by:
E. Nanni
M. Schneider
A. Dhar
Coating on Cu+MgO

## Slide 21: Summary and Conclusion
cavities have different geometries
High power RF use of HTS looks extremely promising
So far no hints of performance limit in RF current up to the maximum power available in the test
The next step is to go from TWT to a Klystron to see where the limits are
Fig 1: Summary of low-power HTS characterisation results

## Slide 22
We have all the key scientific and technological elements to build a 3 GHz HTS pulse compressor!