## Slide 1
Hengpei Liao
Email： hengpeiliao@outlook.com
Phone: +44 07752572734
Research Associate, University of Strathclyde
Superconducting magnets & Superconducting machines

## Slide 2
Development of trapped field magnets using 2G HTS coated conductors
13 March 2025

## Slide 3
Contents
What are the trapped field magnets and their applications
2. Trapped field magnets using 2G HTS coated conductors
3. Magnetization of the HTS-stacked ring magnet
4. Mechanical analysis of the hybrid HTS-stacked ring magnet
5. Magnetization of the HTS double-pancake coil with joints
6. Introduction of Applied Superconductivity Lab at Strathclyde

## Slide 4
What are the trapped field magnets and their applications

## Slide 5: What are the trapped field magnets
Two GdBCO bulk trapped 17.6 T at the centre at 25 K
17.89 T trapped by HTS stacks at 6.5 K
Field cooling magnetization and trapped field magnets
Top seeded melting growth
Typical HTS tape structure
Type-II superconductors

## Slide 6: Applications of trapped field magnets
Portable high field medical devices
Bearings for energy storage flying wheels
High power density HTS machines
Maintain strong magnetic field without external power supply
High speed transportation
HTS undulator with bulk superconductors

## Slide 7: The challenges of current HTS trapped field magnets
Size:
There are inherent limitations due to the unique growth fabrication method. As the size increases, there can be significant microstructural changes which negatively affect the superconducting and mechanical properties.
Limited solutions: Multi-seed TSMG can be used for growing larger bulks with inferior performance.
Mechanical strength:
For typical ReBCO bulks, the axial tensile strength ranges between 5–10 MPa, while the strength perpendicular to the axis lies between 20–30 Mpa. As the bulk grows larger, the strength decreases further.
Limited solutions: Impregnation with resin, metal ring pre-tightening, structure optimization.
HTS bulk materials
Size:
Thanks to the progress in manufacturing HTS coated conductors (tapes), HTS stacks fabricated by stacking HTS tapes have demonstrated the potential in achieving high trapped field as HTS bulk materials.
The thickness of the HTS stacks is not limited.
Since the width of available HTS tapes is limited (12 mm), to further expand HTS stacks with homogeneous properties can not be achieved.
HTS stacks
Traditional HTS trapped field magnets

## Slide 8
2. Trapped field magnets using 2G HTS coated conductors

## Slide 9: 2. Trapped field magnets using 2G HTS coated conductors
HTS-Stacked ring magnet
Advantages of HTS-stacked ring magnets :
Flexible geometry
Quality controlled by standard coated conductor manufacture
Higher reliability by stacking independent HTS tapes
Closed-loop HTS coils
Advantages of Closed-loop HTS coils:
Regulated shapes
Quality controlled by standard coated conductor manufacture
Slow current decay due to joint resistance

## Slide 10
3. Magnetization of the HTS-stacked ring magnet

## Slide 11: 3. Magnetization of the HTS-stacked ring magnet
An HTS-stacked ring magnet with reinforcement was developed with 160 12-mm Fujikura HTS tapes
It was measured with field cooling magnetization and achieved a trapped field of 3.7 T at 25 K.
During magnetization process, it was noticed that the central field showed an ascent phenomenon, which was not observed in traditional HTS material magnetization
Hengpei Liao, et al. Journal of Applied Physics 134, 083902 (2023)
Sample before impregnation

## Slide 12: 3. Magnetization of the HTS-stacked ring magnet
During magnetization process, it was noticed that the central field showed an ascent phenomenon, which was not observed in traditional HTS material magnetization

## Slide 13: 3. Magnetization of the HTS-stacked ring magnet
Numerical analysis was employed to investigate the reason of the ascent phenomenon
Penetration sequence of HTS-stacked ring magnets is different from that of traditional HTS bulks
The inner layers and outer layers are penetrated (magnetized) simultaneously
Induced current in each domains
Induced current density distribution

## Slide 14: 3. Magnetization of the HTS-stacked ring magnet
Induced current in each domains
Induced current density distribution
Considering an HTS bulk material with the same geometry of the HTS-stacked ring magnet
The outer layers are firstly penetrated and the induced current in outer layers is much higher than the inner layers.
The central field doesn’t show ascent during magnetization
The unique stacking method and penetration sequence lead to the central field ascent of the HTS-stacked ring magnet

## Slide 15: 3. Magnetization of the HTS-stacked ring magnet
Based on previous analysis, a model with the number of tapes doubled was investigated
In this configuration, the final central field (4.95T) is higher than the initial applied field (4.5T)
Potential of achieving higher trapped field than applied field

## Slide 16: 3. Magnetization of the HTS-stacked ring magnet
Hengpei Liao, Journal of Applied Physics 133, 023902 (2023)
Hengpei Liao, Journal of Applied Physics 134, 083902 (2023)
HTS-stacked rings
HTS bulks
HTS stacks
7.35 T
6.6 T
HTS bulks and HTS stacks are used as the inserts for HTS rings to increase the trapped field (25 K):
HTS bulk inserts: 3.35 T 7.35 T
HTS stack inserts: 3.79 T 6.6 T

## Slide 17: 3. Magnetization of the HTS-stacked ring magnet
2-stage magnetization of hybrid HTS-stacked ring magnet
Step A, both the HTS-stacked rings and HTS bulks start penetration. However, some parts inside these magnets still remain untouched, meaning no current is flowing there yet.
The transition from the first to the second phase occurs at time step B, where the HTS-stacked rings achieve full penetration
This full penetration in the HTS-stacked rings remains consistent through rest time steps
Post time step B, even as the HTS-stacked rings' magnetization pace decelerates, induced current continues to increase due to increased Ic.

## Slide 18
4. Mechanical analysis of the hybrid HTS-stacked ring magnet

## Slide 19: 4. Mechanical analysis of the hybrid HTS-stacked ring magnet
Only the ends of the HTS tapes are fixed
The open sides are pushed towards the middle
Significant stress concentration is observed at the end of splits

## Slide 20: 4. Mechanical analysis of the hybrid HTS-stacked ring magnet
After impregnation and mechanical press
The stress concentration is reduced significantly, especially at the end of splits
Assuming the magnet’s boundaries are all fixed, the stress concentration disappears
Hengpei Liao, Weijia Yuan and Min Zhang. Mechanical Analysis of Trapped Field HTS-stacked Ring Magnets with and without HTS Stack Inserts, Acta Mech. Sin. 40, 723281 (2024)

## Slide 21: 4. Mechanical analysis of the hybrid HTS-stacked ring magnet
Y-axis Lorentz force load distribution in the z-y cross-section of HTS stacks
Lorentz force experienced during the magnetization of the HTS stacks
Asymmetric magnetic flux (-By, +By) generated by HTS-stacked rings affecting the HTS stack inserts
Stress distribution in the cross-sections of HTS stacks

## Slide 22
5. Magnetization of the HTS double-pancake coil with joints

## Slide 23: 5. Magnetization of the HTS double-pancake coil with joints
The total resistance at 77 K of the two joints: 12 nΩ ±1 nΩ
A bridge-type joint was chosen for ensuring the resistance between superconducting layers is minimized and proper mechanical strength
After soldering, the resistance of the joints were measured with the coil kept outside the LN2

## Slide 24: 5. Magnetization of the HTS double-pancake coil with joints
Central field is 4.58 T after 4.5 T field cooling magnetization
Both magnetizations see a higher trapped field than the applied one
Field decayed to 4.54 T (-0.87%) after 30 minutes
Our 4K magnetization experiment was supported by LNCMI-CNRS, a member of the European Magnetic Field Laboratory (EMFL)
The HTS coil was then impregnated with wax and aluminum nitride powder
Hengpei Liao, Xavier Chuad, Jung-Bin Song, Weijia Yuan and Min Zhang. A novel trapped field magnet enabled by a quasi-operational HTS coil. iEnergy. Vol 3. 261–267 (2024)

## Slide 25: 5. Magnetization of the HTS double-pancake coil with joints
Current of each turn is constrained as the same
No current constraints for each HTS domain
There are both negative and positive current density in the outer turn of the HTS DP coil
There are only positive components
The cause of the negative current density can be considered as the reversed magnetization which coincides with the rising trapped field.
Field distributions of the DP coil model and the bulk model along the central line

## Slide 26: Comparison
 | HTS ring with/without insert | HTS coil with joints | HTS bulk
Charging method | FC magnetization | FC magnetization Thermal switch charging | FC/pulsed magnetization
Field distribution | Asymmetrical | Symmetrical | Subject to fabrication quality and grain boundary
Current decay | Subject to flux flow | Subject to joint resistivity/flux flow | Subject to flux flow
Quality control | Medium | Easy | Hard
Size flexibility | Good | Good | Limited
Mechanical strength | High | Medium | Low

## Slide 27
6. Introduction of Applied Superconductivity Lab at Strathclyde

## Slide 28
Glasgow, UK
University of Strathclyde
Core strengths in engineering, science, and business
Home to 22,000 students
Electronic and Electrical Engineering
  500 academic/research plus support staff and PhD students
  1,000 undergraduate and MSc students
  Largest power systems research institute in Europe

## Slide 29
Applied Superconductivity Laboratory
Research focus:
fundamental research of high temperature superconductors;
Cryogenic aviation propulsion, future grid and fusion generation.
Research Team:
2 Professors, 10 PhDs, 4 Post-docs
Related projects:
ERC: superconducting machines for zero emission aviation
ATI Zero Emission Sustainable Transportation ZEST 1
H2020: Investigation and Maturation of Technologies for Hybrid Electric Propulsion
Industrial projects:
Spirits Aerospace: LH2 tank testing
Collins Aerospace: cryogenic converters
GKN: HTS busbars

## Slide 30
25 K cryostat for experiments
Experiment results with N2
We plan to test neon liquid/gas circulation
Boiling point of Neon: 27.1K
Aviation propulsion
HTS fusion
HTS for power applications

## Slide 31
* Cryogenic drive in presentation

## Slide 32
Thank you