## Slide 1
Overview WP2
Quantum materials 0, 1 & 2D
Focus on nanoscintillators
Christophe Dujardin
Institut Lumière Matière
University Lyon 1 & CNRS
Anna Paola Caricato
University of Salento

## Slide 2
A complex energy relaxation scheme.
Requires solid state description (excitons, phonons… not taken into account in GEANT4)
At the end of the process, the deposited energy is shared among : Light- Heat & Storage
The timing: first stage in the ps regime and ligth can be emitted days afterwards.
For calorimetry, scintillator are generally bulk (crystals) to ensure stopping power.
Important properties are: density (stopping power), Scintillation yield (Ph/MeV), timing (depends on the targetted application.
Introduction: What is scintillation?

## Slide 3
Most of the characteristic distances are larger than 10nm
Scintillation at the nanoscale: what are the differences?

## Slide 4
Scintillation at the nanoscale: what are the differences?
Even in the keV regime, penetration depth of electrons is larger than the NP size.

## Slide 5
Scintillation at the nanoscale: what are the differences?
GEANT4 on a 10 nm NP, with 10keV electron… in the range of 1% of effective energy deposition
Bulin, nanoscale, 2015

## Slide 6
Scintillation at the nanoscale: what are the differences?
Escape occurs even during the heat generation stage
Kirkin, IEEE TNS 2012
Dujardin, Adv. Opt. Matter. 2025

## Slide 7
Material preparation:
The synthesis routes allow to prepare original shapes with preserved properties
(plastics, flexible, thin films, porous…)
Original emission properties (accelerated)
In quantum dots, accelerated emission may occur
Collective phenomena may accelerate the emission
Shapping the environment may lead to Purcell effect (acceleration)
Potential advantages of nanotechnologies

## Slide 8
PDMS loaded with efficient emitters
Material preparation: Plastics, flexible screens
Lian JPCL 2021
Zhou ACS Energ. Lett 2022
Meng, Adv. Func. Matter. 2024
Flexible & X-ray screens
Flexible X-ray screen

## Slide 9
Material preparation: Ultra fast screens
Toci, J.Lum. 2019

## Slide 10
Ultra-porous scintillators
Material preparation: aerogels
Silica
YAG:Ce
for gaz detector purpose
Marie-Luce, Nat. Photon. 2024
Assembly of NP
Silica aerogels are used for beam monitoring -> adding scintillation?

## Slide 11
It includes targets (Cd) for neutrino
Material preparation: Liquid Scintillator (LS)
Other class of Liquid Scintillator
Ultra dense Liquid
HfO2 loading d=(2.5)
Courtesy F.Chaput
Baravaglio, Nanoscale 2024
Winslow, JINST 2012
Rather unexplored area, Nanoscintillators in liquid for Calorimetry

## Slide 12
Multicolor emissions
Quantum effects in 0D materials
Quantum effects (90’s): Exciton confinement (emission rate, wavelength…)
core shell structure (effect of the shell on the electron & hole wavefunctions)
Size effect
Shell effect
Kholocheva, ACS Photonics 2024

## Slide 13
Accelerated emissions: multiexcitons
In nanosystems, ultra fast emissions may occur: multiexciton generation (MEG)
tX0, tXX= tX0 /4, tXX = tX0 /9…
Here Spherical QuantumWells
Meng, Nanoscale 2021

## Slide 14
Accelerated emissions: multiexcitons
The same effect in 1D materials (Nanoplatelets)
Meng, Mat. Adv. 2022

## Slide 15
Fast emission also in 2D materiels
2D perovskites: combine bulky crystals and benefit of 2D confined systems
Xie et. al. Chem. Mat. 2020

## Slide 16
Combination with dense matrix
But nanoscintillators cannot be used alone (problem of stopping power): metamaterials

## Slide 17
Combination with dense matrix
Example of assembly of bulk combined with Nanoplatelets: energy sharing demonstration
Turtos et. al. NPJ-2D 2019

## Slide 18
Combination with dense matrix
But it cannot be used alone (problem of stopping power): metamaterials
BGO crystal
2D perovskites
shared events (g-rays)
extra fast photons (under x-rays)
Rogers et. al. APL 2022

## Slide 19
Many combinations are possible
But it is very time consuming to test every parameter
A nice monte carlo simulation paper (oriented TOF-PET)
Krause, Adv Theory and Simulations 2024

## Slide 20
Some numbers…
CTR a sqrt (tD/N)
Lets start with LSO (20ph/keV, 40ns)
Assume 90% of the energy in LSO, and 10% in a « ultra fast nano* » (1ns for the ex.)
460 keV in LSO
51keV in nano*
(tD/N)LSO=(tD/N)nano* if Nnano=500 (for 51keV)
To obtain a signicative CTR improvement, the effective scintillation yield of the nano* should largely exceed 10 ph/keV….

## Slide 21
Purcell effect: nanostructure silica
Roques-Carmes, Science 2022

## Slide 22
Purcell effect: modification of the radiation pattern
Kurman, Science advance 2024

## Slide 23
Purcell/Plasmonic effect: Accelerated time response
Ye, Adv. Matter 2024
But 100nm thick…

## Slide 24
Purcell at « large » scale
Makowsky, Arxiv 2024

## Slide 25
Superfluorescent scintillation: collective effect for fast emission
Katznelson, arxiv 2025

## Slide 26
Targetting calorimetry

## Slide 27
Targetting calorimetry: Radiation hardness

## Slide 28
The use of nanocrystals appears a bit contradictory: tiny objects to detect high energy particles
Effective media approach cannot be use to describe the systems
Nanoparticles are always embeded in media, which is never passive
Original developments at the lab scale
Concluding remarks about 0D,1D and 2D scintillators

## Slide 29
About the papers
Nanoscintillators
(almost doped insulators)
Quantum dot + Scintillat*
(CdSe + a bit of perovskite)
perovskite + Scintillat*
(CsPbBr3 the champion)

## Slide 30
And the SCINT conference
A lot!

## Slide 31
GEANT 4, but it does not account for solid state physics
Microtheory (Vasil’ev, Engineering of Scintillation Materials and Radiation Technologies 2017)
Most recent (Roques-Carmes, Science 2022) (dedicated to Purcell effect)
Modeling

## Slide 32
Potential role of DRD5-WP2 in this landscape?
WP2-a: Application specific tailoring
Because of the publication "race," everyone claims to have the best sample.
However, most researchers do not come from the scintillation or end-user community. This situation requires a rationalization of the measurement protocol. Even "simple single crystals" may exhibit measurement fluctuations.
The dream scenario would be to define a standard geometry and establish a few "centers of measurement" for the community. These centers would facilitate cross-measurement for cross-calibration, focusing on transmission, scintillation spectra, scintillation yield, and time response.
One key aspect is radiation hardness, which involves defining an irradiation protocol and conducting remeasurements.
Additionally, the open data aspect is crucial.

## Slide 33
Potential role of DRD5-WP2 in this landscape?
WP2-a: Application specific tailoring
And then an open database specific to nanoscintillators
Here the 30’s year old Berkeley database for bulk materials

## Slide 34
Building a community
WP2-b: Extended functionalities
Requirement to define a target in terms of application
Universal scintillator will never exist!
WP2-c: modeling
Goal? Being predictive or descriptive

## Slide 35
Building a community
Setting a small working group?
In Crystal Clear Collaboration and SCINT conference community?