## Slide 1: Tentative selection of IT cryomagnets to keep as spare magnets
Selection done considering
  Known non-conformities on main magnets and corrector magnets
  LS2 powering performance test
  Maximum local dose taken during Run 1, Run 2 and objective of Run 3
    On main magnets
    On corrector magnets

## Slide 2
correctors:
MCBX: larger aperture
MQSX: coils off mid planes
MC S/T X & MC O/OS/SS X
Polarity : FDF = configuration Run1, Run2 and beginning of Run 3
Without considering the change of Atlas magnet polarity
Insulation degradation may appear (to be confirmed)
Above 30 MGy for main magnets
Above 7 MGy for corrector magnets

## Slide 3: Q2 IR1 : Nom – V up to 2023; RP- V up to 2024 ;  Nom – H
IR1: Nom-V
V
IR1: RP-V
V
IR1: Nom-H
V
H
260 fb-1 < L < 380
0 < L < 260 fb-1
380 fb-1 < L < 530?
Cham2024
87%
40%
50%
= top
= bottom
Q2a (update 12.2024)
100 fb-1
100 fb-1
IR1: Nom-V
IR1: RP-V
IR1: Nom-H
5MGy/100fb-1

## Slide 4: Q2 IR5 : Nom – H up to 2024 ;  RP - V
IR5: Nom-H
H
IR5: RP-V
H
V
0 < L < 380 fb-1
380 fb-1 < L < 530?
127%
50%
IR5: Nom-H
IR5: RP-V
2MGy/100fb-1

## Slide 5: For Q1 in IR1 and IR5
300 fb-1
IR1: Nom-V
V
IR1: RP-V
V
IR1: Nom-H
V
H
260 fb-1 < L < 380
0 < L < 260 fb-1
380 fb-1 < L < 530?
IR5: Nom-H
H
IR5: RP-V
H
V
0 < L < 380 fb-1
380 fb-1 < L < 530?
87%
40%
50%
127%
50%
Q1~ 15*530/300=26.5MGy
Idem pour IR5
Mail de F. Cerutti:
Pour les quatre Q1 (P1 et P5), dans l'hypothèse 580 fb-1 (c'est-à-dire200 fb-1 sur 2025+2026) on va arriver sur les 25 MGy.

## Slide 6: For Q3 in IR1 and IR5
IR1: Nom-V
V
IR1: RP-V
V
IR1: Nom-H
V
H
260 fb-1 < L < 380
0 < L < 260 fb-1
380 fb-1 < L < 530?
IR5: Nom-H
H
IR5: RP-V
H
V
0 < L < 380 fb-1
380 fb-1 < L < 530?
87%
40%
50%
127%
50%
Mail de F. Cerutti:
Niveau main quadrupoles, les aimants moins impactés sont les deux Q3 d'ATLAS (Point 1) qui selon les calculs toucheront 15 MGy après 580 fb-1
Puis il y a les deux Q3 de CMS (P5), qui passeront à peine les 20 MGy après les mêmes 580 fb-1.
9
+4
+4
18
+3

## Slide 7: Weakness on MCBX combined magnets : https://edms.cern.ch/document/1395638 (see LMC#183)
QH issue on Q1.R1 : 1017174 One of the two quench heater circuits (YT1121) breaks down above 1000V Power supply of the QHC reduced to 800V
Known non-conformity on IT magnets

## Slide 8: Training quenches in RCBXx.x1 in Post LS2 (combined+individual)
***, ***, ***
*, **, *
Ranking 1,2,3

## Slide 9: Training quenches in RCBXx.x5 in Post LS2 (combined+individual)
*, *, **
**, ***, **
Ranking 1,2,3

## Slide 10: Wrap up
 | Q1 | Q2 | Q3 | MCBX | MCBX1,2,3 Powering test | 
IR1 | 25MGy @580 fb-1 | 27MGy @530 fb-1 30MGy @580 fb-1 | 15MGy @580 fb-1 | 100% powering test (95% for 2L1) | ***, ***, *** for L1 * , ** , * for R1 | HQ issue on Q1.R1
IR5 | 25MGy @580 fb-1 | 27MGy @530 fb-1 28MGy @580 fb-1 Both on Q2a and Q2b | 20MGy @580 fb-1 | 100% powering test (85% for 2R5, 90% for 1L5) | * , * , ** for L5 ** , ***, ** for R5 | 
 | First : Q1L1 Second: Q1R5 | First : Q2L1 Second: Q2R5 | First : Q3L1 Second: Q3L5 Third : Q3R5 |  |  | 
My first choice @ 530 fb-1 : Q1, Q2, Q3L1  major constraint for dismantling
If L (2025+2026)> 530 fb-1: Q1L1 , Q2R5, Q3L1 (and Q3L5)
Note: during YETS test, RCBX circuits IR1 & IR5 are tested only individually up to 300A
The baseline is also to keep the present spare triplet cryo-magnets (Q1, Q2 and Q3) , plus the above selection.
Q1 magnet was tested at cold in 2018 at SM18, but the tests are still pending for Q2 and Q3!