## Slide 1: Nb3Sn/Cu - Status and perspectives
Valentin Giglia
TE-VSC-SCC
TE-VSC Seminar – 18th March 2024

## Slide 2
Outline
Introduction: Why Nb3Sn
Nb3Sn on small sample for development
QPR for fine tuning
Towards first cavity depositions
Conclusion

## Slide 3
Introduction
Superconducting Radio Frequency (SRF) Cavities
  Accelerate charged particles
    Electromagnetic standing wave
    Force applied to charged particle
  Bulk Nb
  Nb/Cu (LHC, ISOLDE):
    Cu = high thermal conductivity
    Lower load on cooling system

## Slide 4
Introduction
SRF Cavity Performance
    Quality factor Q =
    Dissipated power proportional to Rs
    Rs ↘ with ↗  Good indicator !
1.3GHz, 4.2K
400 MHz, 4.2K

## Slide 5
Introduction
How Nb3Sn compares to Nb ?
Q0 at 4.5 K ~ bulk Nb at 2 K
Better overall performances
 | Nb | Nb3Sn
Tc (K) | 9.2 | 18.3
RBCS (nW) | 45 | 0.4
Hsh (mT) @4.2K and 500MHz | 220 | 425
Max th. Eacc (MV/m) | 50 | 100
How this is interesting for accelerators ?
For FCC: bulk Nb cavities for booster operations
Could operate at 4.5K instead of 2K + Use of Cu substrate
Energy and cost savings for future colliders

## Slide 6
Introduction
Nb3Sn
Theoretical Max Tc @ -1.5 GPa
Some challenges for Nb3Sn dev:
  Very narrowed region in phase diagram
  Requires high temperature process
  Composition is crucial to ensure high perf.
    Optimal Sn content 25 At.%
  Perf. are hindered by mechanical stress
[3] A. Godeke. Supercond. Sci. Technol. 19 (2006)
[1]
[2]
[1] J. Charlesworth, I. MacPhail, and P. Madsen, J. Mater. Sci. 5, 580 (1970)
[2] G. De Marzi et al. J. Phys.: Condens. Matter 25 (2013)
[3]

## Slide 7
Outline
Introduction: Why Nb3Sn
Nb3Sn on small sample for development
QPR for fine tuning
Towards first cavity depositions
Conclusion

## Slide 8
Development on small Cu samples
Ta
Nb3Sn
Surface preparation:
  SUBU (chemical polishing)
  EP (Electro polishing)
  PEP (Plasma electro polishing)
Coating process Bi-Polar HiPIMS:
  Samples mounted on T-regulated, rotative support
  Two steps coating
    1St dep: Ta barrier*
    2nd dep: Nb3Sn layer
50 μm
*Prevents from copper diffusion [1] 
[1] E A Ilyina et al. Supercond. Sci. Technol. 32. (2019)

## Slide 9
Development on small Cu samples
High Power Impulse Magnetron sputtering:
  High power density during short pulses
  Advantages for thin films:
    Higher plasma ionisation
    Higher film density
  Bi-Polar for Nb3Sn devs:
    Both negative and positive pulses
    PP pushes charged species towards the sample
    Even higher film density
b)
C.P.A Carlos et al. FCC week 2022

## Slide 10
Development on small Cu samples
Nb3Sn | Range explored | Best results
Gaz | Kr | Kr
Temperature (◦C) | [500,750] | 750
Pressure (mBar) | [, ] | [, ]
Positive Pulse (V) | [35,130] | 50
Annealing (hrs) | [0,72] | 24
Nb3Sn | Range explored | Best results
Gaz | Kr | Kr
Temperature (◦C) | [500,750] | 750
Pressure (mBar) |  | 
Positive Pulse (V) | [35,130] | 50
Annealing (hrs) | [0,72] | 24
High Power Impulse Magnetron sputtering:
  High power density during short pulses
  Advantages for thin films:
    Higher plasma ionisation
    Higher film density
  Bi-Polar for Nb3Sn devs:
    Both negative and positive pulses
    PP pushes charged species towards the sample
    Even higher film density
Extensive ongoing study (started by S. Leith):

## Slide 11
Development on small Cu samples
Best results on small samples:
  Tc is capped at 16K
  First order impact of mechanical stress
  (Different CTE between Cu and Nb3Sn)
Demonstration:
  Same coating recipe on different substrates
  Tc ↗ when CTE becomes closer to Nb3Sn
  Total improvement = 2K
A promising solution:
  Changing Cu substrate for CuW
  First coating in characterization now
S. Leith

## Slide 12
Outline
Introduction: Why Nb3Sn
Nb3Sn on small sample for development
QPR for fine tuning
Towards first cavity depositions
Conclusion

## Slide 13
Recipe fine tuning with QPRs
QPR = Quadrupole resonator:
  Flat object as close as possible to a cavity
  For thin films RF characterization
  Allows to quantify Rs
Before Dep
During Dep
After Dep

## Slide 14
Recipe fine tuning with QPRs
Comparison with Nb/Cu layers:

## Slide 15
Recipe fine tuning with QPRs
Comparison with Nb/Cu layers:

## Slide 16
Recipe fine tuning with QPRs
Comparison with Nb/Cu layers:

## Slide 17
14nW
Recipe fine tuning with QPRs
41nW
Comparison with Nb/Cu layers:
  Significant improvements these past 2 years
  Rs 2-3 times lower for Nb3Sn vs Nb !!!!
Notes: Cohérence

## Slide 18
Recipe fine tuning with QPRs
Comparison with Nb/Cu layers:
  Significant improvements these past 2 years
  Rs 2-3 times lower for Nb3Sn vs Nb !!!!
Extrapolation to cavity:
  Better performance than Nb/Cu cavities
  On the right way towards FCC requirements
Constant dev to even higher perfs:
  Substrate material and preparation
  Coating adjustments
First validation for cavity application
FCC ee
1cell
Notes: Estimation FCC ajustée aux facteurs LHC

## Slide 19
Outline
Introduction: Why Nb3Sn
Nb3Sn on small sample for development
QPR for fine tuning
Towards first cavity depositions
Conclusion

## Slide 20
Towards cavity coating: Requirements
Dia. 500mm
High temperature deposition (750C):
  Requires large furnace
  Cu cavities must be upgraded:
    Increased cavity thickness
    Rigid support structure inside the furnace ?
    Alternative materials?

## Slide 21
Towards cavity coating: Requirements
Dia. 500mm
High temperature deposition (750C):
  Requires large furnace
  Cu cavities must be upgraded:
    Increased cavity thickness
    Rigid support structure inside the furnace ?
    Alternative materials?
Nb3Sn target ideal geometry:
  Hollow and cylindrical (like Nb or Ta targets)
  Advantages:
    Use our long-term experience
    Allows for vertical coating
    Avoid cavity rotation required by flat target

## Slide 22
Towards cavity coating: Limitation
Dia. 500mm
Nb3Sn target specifications:
  Alloyed target
  Limitation to 2 targets:
    One for diffusion barrier layer
    One for Nb3Sn
Nb3Sn target undesired properties:
  Fragile and prompt to cracking
  Dust creation
  Not compatible with cylindrical shapes
Root cause identification:
  Thermal cycles, power ramp rate, max power
  The cracking is unavoidable
1 Coating
10 Coatings

## Slide 23
Towards cavity coating: Solution
Dia. 500mm
Most promising solution:
  Bonding on backing plate
  BP made of CuW (same CTE as Nb3Sn)
First tests on small target:
  Positive on Ø 20mm target
  Ongoing for Ø 50mm target (then 150mm)
New magnetron design:
  Grounded magnet and dark space shields
  Cooling liquid bath for:
    Magnet
    Target through BP
V. Sibue and M. Crouvizier (EN-MME)
G. Girod (EN-MME)
80mm

## Slide 24
Conclusions
Big improvements have been made with the Nb3Sn/Cu technology :
  Confirmation of Nb3Sn coating repeatability
  RF performances higher than Nb/cu cavities
  Very promising for FCC
First cavity coating system designs:
  Nb3Sn bonding on CuW is very promising to mitigate target breaking
  Allows for polyedric target  deposition system as close as possible to well known settings
Future developments:
  Complete target survival tests with larger targets
  Studies on QPR :
    Coating improvements
    Flux trap, thermal gradient effect
  Nb3Sn coating on CuW

## Slide 25
Thank you for your attention