## Slide 1: Evaluation of LGAD Performance Degradation due to TID Aging Under 10 keV X-ray Irradiation
3rd DRD3 week, WG2
Jun 4, 2025
Thalia A. Silva1 , Alexis C. Vilas-Bôas1 , Marcelo A. Pavanello1, Renato C. Giacomini1, Nilberto H. Medina2, Marco A. Leite2 , F. Rogelio Palomo3 and Marcilei A. Guazzelli1
1Centro Universitário FEI, Brazil
2Instituto de Física da USP, Brazil
3Universidad de Sevilla, Spain

## Slide 2: Outline
Motivation
  Introduction
  Sirius Synchrotron (Brazil) in Comparison to ESRF (EU)
  Importance of LGAD to Brazil
Methodology
  Device under test (DUT)
  X-ray Facility
  Electrical characterization setup
Results
  Foward current vs Voltage (If x V)
  Reverse current vs Voltage (Ir x V)
  Capacitance ( 1/C2 x V)
Conclusions and Future steps
2
Thalia A. Silva – 3rd DRD3 week

## Slide 3: 1
Motivation
Thalia A. Silva – 3rd DRD3 Week
3

## Slide 4: Motivation
Introduction
Thalia A. Silva - 3rd DRD3 week
4
Dr. Rogelio. Palomo
Dra. Marcilei Guazzelli
Thalia Alves da Silva

## Slide 5: Motivation
SIRIUS Synchrotron (BRAZIL)
ESRF Synchrotron (EU)
5
Category | Sirius (Brazil) | ESRF (EU)
Facility Type | 4th-gen. synchrotron | 4th-gen. synchrotron
Location | São Paulo, Brazil | Grenoble, France
Beam Energy | 3 GeV | 6 GeV
Beam Current | Up to 350 mA | ~200 mA
Natural Emittance | 0.28 nm·rad | 0.15 nm·rad
RF Frequency | 500 MHz | 352 MHz
Circumference | ~518 meters | ~844 meters
Radiation & Optics | Sirius | ESRF
Spectral Brightness | > 10²¹ photons/s/mm²/mrad²/0.1%BW | > 10²² photons/s/mm²/mrad²/0.1%BW
Photon Energy Range | Infrared to ~40 keV | Soft to hard X-rays (~0.1 keV to 100 keV)
Spectral Range | IR to hard X-rays | EUV to hard X-rays
Beam Focus | Nanofocus capability (e.g., Carnaúba beamline) | Ultra-nanofocus (e.g., ID16B beamline)
Operating Modes | Multi-bunch (future single-bunch capability) | Multi-bunch, hybrid, and single-bunch modes
Projeto Sirius – a Nova fonte sincrotron do Brasil

## Slide 6: Motivation
Importance of Low Gain Avalanche Detector (LGAD)to Synchrotrons
Thalia A. Silva – 3rd DRD3 week
6
The ideal detector for beamline experiments requires reach of fs. A good candidate to high temporal and spatial efficiency currently is the LGAD with ps.
Technological relevance for advanced facilities: LGADs offer high-performance detection solutions suitable Sirius Synchrotron .
Potential for innovation and strategic use: The possible integration of LGADs into Sirius beamlines has the potential to enhance the quality of experiments and promote the use of next-generation detection technologies in national strategic infrastructures like CNPEM.
Notes: LGADs are important in Brazil because they offer advanced solutions to meet some of the technological demands of facilities like Sirius. Just like the ESRF in France, Sirius operates with ultra-high brightness X-ray beams, which are essential for cutting-edge research in areas such as nanotechnology, biosciences, and applied physics. These experiments require detectors capable of withstanding extreme environments without performance loss — precisely the kind of performance LGADs provide. Therefore, developing and applying this technology in Brazil strengthens national scientific autonomy and drives innovation in strategic centers like CNPEM.

## Slide 7: 2
Methodology
Thalia A. Silva - 3rd DRD3 week
7

## Slide 8: Methodology
LGAD HPK 3.2 Single Pad
  Active area: 1.3 × 1.3 mm
  Active depth: 50 µm
  Gain layer: 2.2 µm
  Internal gain: 20
  Electric field: ~300 kV/cm
Thalia A. Silva - 3rd DRD3 week
8
This study investigated TID effects on LGADs through 10 keV X-ray exposure, with a focus on I–V and C–V curves measured before, during and after irradiation at varying radiation doses.
A. Moreno

## Slide 9: Methodology
Thalia A. Silva - 3rd DRD3 week
9
X-RAY facility
DUT distance = 15 cm
10 keV X-ray
LERI

## Slide 10: Methodology
Electrical characterization setup
Thalia A. Silva – 3rd DRD3 week
10
Keithley 4200 SCS
For If x V measurements were voltages ranging from -1 to 1 V, with 200 mA current compliance, and 1000 points.
For Irev x V measurements were voltages ranging from 0 to -200 V, with 100 mA current compliance, and 4000 points
CxV : Vpp = 30 mV/RMS and VD = 0.4 to -30 V and two distinct frequencies: 1 MHz and 3 MHz..

## Slide 11: 3
Results
Thalia A. Silva - 3rd DRD3 week
11

## Slide 12: Results
Forward current vs Voltage (If x V)
Thalia A. Silva – 3rd DRD3 week
12
It is known that the LGAD was not designed to operate under forward bias, as its functionality relies on carrier multiplication through impact ionization. This physical effect occurs under reverse current and for applied high electric fields. However, to understand the physical mechanisms that affect the functionality of this device under the TID effects, it is interesting to analyze its behavior under forward bias conditions.

## Slide 13: Results
Reverse current vs Voltage (Ir x V) and Breakdown Voltage (VB)
Thalia A. Silva – 3rd DRD3 week
13
Breakdown voltage degradation is due to TID-induced damage in the passivation oxides, especially in the oxides located over the Junction Terminal Extensions (JTEs).

## Slide 14: Results
Reverse current vs Voltage (Ir x V) and Breakdown Voltage (VB)
13
Breakdown voltage degradation is due to TID-induced damage in the passivation oxides, especially in the oxides located over the Junction Terminal Extensions (JTEs).
Thalia A. Silva – 3rd DRD3 week

## Slide 15: Results
Capacitance vs Voltage (C x V) and 1/C2 vs Voltage
Thalia A. Silva – 3rd DRD3 week
14
For the measurements is possible to acquire the Gain layer depletion (VGL), through the second derivative.
The behavior observed in the capacitance curve measured at 3 MHz can be attributed to the release of radiation-induced charge carriers previously trapped in defect states. This process alters the effective charge density at the device junction, directly impacting the capacitance value.
VGL = -28.8 V
VGL
Initial High Capacitance
Full depletion
Gain layer depletion
Voltage (V)
Capcitance (nF)
A. Moreno

## Slide 16: 4
Conclusions
Thalia A. Silva - 3rd DRD3 week
15

## Slide 17: Conclusions
If x V
Thalia A. Silva – 3rd DRD3 week
16
Ir x V
1 MHz 1/C2 x V
Numeric overview of the results
3 MHz 1/C2 x V
 | Pre-rad | 2 krad(Si) | 91 krad(Si) | 451 krad(Si) | Post-R.T.A.
VD (V) |  | 0.611 | 0.638 | 0.606 | 0.626
VB (V) | -166 | -159 | -195 | -143±50 | Undefinable
VGL (V) | -28.80 | -28.80 | -28.80 | -28.80 | -28.80
VGL (V) | -28.85 | -28.85 | -28.80 | -28.85 | -28.85
0.611

## Slide 18: Conclusions
There was a significant variation observed in device electrical characteristics during irradiation, particularly evident in I x V curves with decreased conduction voltage and degradation in avalanche region.
There was not a total recovery of electrical properties observed within a week of Room Temperature Annealing between irradiation steps.
Compromise of its original function in high-energy particle detection due to observed changes.
The degradation is due to TID-induced damage in the passivation oxides, especially in the oxides located over the Junction Terminal Extensions (JTEs).
Thalia A. Silva – 3rd DRD3 week
17

## Slide 19: 5
Future Steps
Thalia A. Silva - 3rd DRD3 week
18

## Slide 20: Future Steps
Collaboration with
Thalia A. Silva – 3rd DRD3 week
19
LGAD CNM
nLGAD CNM
Anode
Cathode
Thermopar
Future steps aim to study surface damage caused by Total Ionizing Dose (TID) using LGAD, nLGAD, and PIN diodes from IMB-CNM.
These initial tests helped setup a more efficient methodology for this type of device
This study will also consider temperature variations, monitored using a thermopar, the extraction of the gain, to enable a comparative analysis of the three types of diodes.
Guard Ring

## Slide 21
E-mail : thalisilva@fei.edu.br
Orcid: 0009-0002-0508-7937
20
Thank you!