## Slide 1
From Van der Pauw Test Structures to Compensated LGADs: A Simulation–Measurement Synergy to Quantify Donor Removal
A. Fondacci, A. R. Altamura, R. Arcidiacono, M. Boscardin, N. Cartiglia, T. Croci, M. Centis Vignali, M. Ferrero, A. Morozzi, F. Moscatelli, D. Passeri, G. Paternoster, B. Regnery, V. Sola, R. S. White
3rd DRD3 week on Solid State Detectors R&D

## Slide 2
Defining the Challenge, Designing the Approach
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D
Acceptor removal has been studied in detail for many years and is at the core of the LGADs' radiation hardness.
Donor removal is now becoming very interesting as it plays a crucial role in the functioning of resistive LGADs and compensated LGADs.
CBL / CBH (0.6 - 1)
CHBL / CHBH (0.8 - 1)
CHBL / CHBH (0.4, 2, 3, 5)
NO Carbon

## Slide 3
Defining the Challenge, Designing the Approach
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D
Acceptor removal has been studied in detail for many years and is at the core of the LGADs' radiation hardness.
Donor removal is now becoming very interesting as it plays a crucial role in the functioning of resistive LGADs and compensated LGADs.
Resistive LGADs
n++
p+
p++
p
-
+
-
+
-
+
-
+
p+
Compensated LGADs
CBL / CBH (0.6 - 1)
CHBL / CHBH (0.8 - 1)
CHBL / CHBH (0.4, 2, 3, 5)
NO Carbon

## Slide 4
Defining the Challenge, Designing the Approach
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D
Donor removal is now becoming very interesting as it plays a crucial role in the functioning of resistive LGADs and compensated LGADs.
A Simulation–Measurement Synergy to Quantify Donor Removal at high initial concentrations (ND > 1015 atoms/cm3)
Van der Pauw test structures
  Clean environment (a dedicated test structure for each implant under study) to investigate donor removal by examining the change in sheet resistance with irradiation.
  RSD2 batch NPLUS test structures (TS) irradiated and analysed; DC-RSD1 batch NPLUS TS are under irradiation; NLGAD batch NGAIN TS will be analysed once FBK realises the batch.
Compensated LGADs
  EXFLU1 batch samples offer an opportunity to study donor removal to further initial donor concentrations than those of the previously mentioned samples by reproducing in simulation the capacitance variation with irradiation.
  These samples will also enable us to begin examining the interplay between donor removal and acceptor removal (Do acceptor and donor removals behave similarly together or alone?).
Resistive LGADs
n++
p+
p++
p
-
+
-
+
-
+
-
+
p+
Compensated LGADs

## Slide 5
Van der Pauw test structure
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D

## Slide 6
RSD2 batch — NPLUS
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D

## Slide 7
NPLUS profiles before irradiation
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D

## Slide 8
New University of Perugia radiation damage model
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D
Donor removal
Acceptor creation
Donor removal
Acceptor creation
Doping analytical parameterisation
Traps in the bandgap
Surface damage (+Qox)
Bulk damage
https://www.etp.kit.edu/english/1669.php

## Slide 9
RSD2 NPLUS W3 — Neutron Proton
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D
Donor removal with
Acceptor creation with
Acceptor creation with
Donor removal with

## Slide 10
RSD2 batch — NPLUS — TCAD Measurements
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D

## Slide 11
EXFLU1 batch - PGAIN
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D
Acceptor creation
Acceptor removal
Acceptor removal
Acceptor removal

## Slide 12
EXFLU1 batch — PGAIN — TCAD Measurements
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D

## Slide 13
Acceptor removal
EXFLU1 batch – Compensated LGADs
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D
Single pad Compensated LGAD
Donor removal - Change cD until experimental C-Vs are reproduced!

## Slide 14
EXFLU1 batch – Compensated LGADs
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D
By exploiting the experimental acceptor removal coefficient cA = 2.50⋅10-16 cm², agreement with C-V measurements is achieved using a donor removal coefficient cD = 6.50⋅10-16 cm².
Assuming the same dependence on the initial doping density and considering the different concentrations of implanted boron and phosphorus atoms, it results that cD ~ 2⋅cA.
By exploiting the extracted cD (6.50⋅10-16 cm²) and the experimental cA = 8.26 · 10-17 cm² for the carbonated gain implant, a good agreement between measurements and simulations was achieved.
The latter cA, being one third of the former, confirms that carbon slows acceptor removal in the same way as in standard LGADs, even in the presence of phosphorus in the gain implant region.

## Slide 15
Preliminary cD at high initial donor concentrations
A. Fondacci et al.
3rd DRD3 week on Solid State Detectors R&D
CBL / CBH (0.6 - 1)
CHBL / CHBH (0.8 - 1)
CHBL / CHBH (0.4, 2, 3, 5)
NO Carbon
RSD2
EXFLU1
Squares = Donor removal
Diamonds = Acceptor removal

## Slide 16
Conclusion
Doping removal can be estimated via changes in sheet resistance under irradiation:
For surface implants of opposite conductivity to the substrate: van der Pauw measurements alone are sufficient;
For deep and/or same conductivity type implants: simulation is required to interpret van der Pauw measurements.
Preliminary analyses indicate:
Correlation between C-V and van der Pauw extracted removal coefficients;
A more pronounced donor removal than acceptor removal.
New analyses (EXFLU1, RSD2, DC-RSD1, NLGAD) aim to strengthen and validate these results.
Thank you for your attention!
A. Fondacci (alessandro.fondacci@pg.infn.it), A. R. Altamura, R. Arcidiacono, M. Boscardin, N. Cartiglia, T. Croci, M. Centis Vignali, M. Ferrero, A. Morozzi, F. Moscatelli, D. Passeri, G. Paternoster, B. Regnery, V. Sola, R. S. White