## Slide 1
CERN Summer Student Lecture - 2025
Accelerator Technology Challenges: Superconducting magnets (2/2)
Susana Izquierdo Bermudez
(susana.Izquierdo.Bermudez@cern.ch)
European Organization for Nuclear Research (CERN)

## Slide 2: Outline
Part I
  Particle accelerators, magnets and the need of superconductors
  Magnetic design and coil fabrication
Part II
  Mechanical design and assembly
  Quench, training and protection
  Outlook, what brings the future

## Slide 3: Mechanical design
In the presence of a magnetic field B, an electric charged particle q in motion with a velocity v is acted on by a force FL called electro-magnetic (Lorentz) force [N]:
A conductor element carrying current density J (A/mm2) is subjected to a force density fL [N/m3]
Some examples (values per aperture):
Nb-Ti LHC MB (8.3 T)
  Fx = 340 t per meter
  Fz = 27 t
Nb3Sn DS dipole (11T)
  Fx = 620 t per meter
  Fz = 47 t

## Slide 4: Electro-magnetic force
The e.m forces in a dipole/quadrupole magnet tend to push the coil
  Towards the mid-plane in the azimuthal direction
  Outwards on the radial direction.

## Slide 5: Electro-magnetic force
In the coil ends, the electromagnetic forces tend to push the coil outwards in the longitudinal direction (Fz > 0)
Fz
Fz
Fz
Fz
11 T dipole for HL-LHC
MQXF quadrupole for HL-LHC

## Slide 6: Electro-magnetic force
The x/y e.m. force on a dipole coil varies
  with the square of the bore field
  Linearly with the bore radius (a)
The axial e.m. force on a dipole coil varies
  with the square of the bore field
  with the square of the bore radius
Approximation of thin shell dipole, see how to derive the equations in [2]
See how to derive the equation in [2]

## Slide 7: Stress and strain - definitions
A stress  or  [Pa] is an internal distribution of force [N] per unit area [m2].
  When the forces are perpendicular to the plane the stress is called normal stress () ; when the forces are parallel to the plane the stress is called shear stress ().
  Stresses can be seen as way of a body to resist the action (compression, tension, sliding) of an external force.
A strain  (l/l0) is a forced change dimension l of a body whose initial dimension is l0.
  A stretch or a shortening are respectively a tensile or compressive strain; an angular distortion is a shear strain.

## Slide 8: Stress and strain - definitions
The Elastic modulus (or Young modulus, or modulus of elasticity) E [Pa] is a parameter that defines the stiffness of a given material. It can be expressed as the rate of change in stress with respect to strain (Hook’s law):
The Poisson’s ratio  is the ratio between “axial” to “transversal” strain. When a body is compressed in one direction, it tends to elongate in the other direction. Vice versa, when a body is elongated in one direction, it tends to get thinner in the other direction.
 = -trans/ axial
A cube with a Poisson's ratio of 0.5, courtesy of Wikipedia
E =  / 

## Slide 9: Pre-stress
The prestress paradigm is that coil should never be in tension but always precompressed (as reinforced concrete)
The initial reasons for this paradigm were field quality concerns: change of b3 (A. Tollestrup, Ann. Rev. Sci. 1984, father of Tevatron magnets and collared structure)
Later, it was believed that the detachment provokes training – and this is what many of us think still today
The paradigm is always used in design and not always followed in reality
  Typically, for the first models and prototypes one speaks of “conservative” loading, meaning that the preload is lower than what required to avoid pole unloading in operational conditions
  The fear is to break something of degrade the conductor

## Slide 10: Superconducting dipoles (NbTi)
HERA
1991-2007
Bore: 75 mm
Field: 5.0 T
Fx = 0.6 MN/m
Fz = 87 kN
Tevatron
1983-2011
Bore: 76 mm
Field: 4.3 T
Fx = 0.5 MN/m
Fz = 78 kN
RHIC
2000-running
Bore: 80 mm
Field: 3.5 T
Fx = 0.3 MN/m
Fz = 48 kN
LHC
2008-running
Bore: 56 mm
Field: 8.3 T
Fx = 1.7 MN/m
Fz = 265 kN
Fx per quadrant/Fz per aperture

## Slide 11: The HL-LHC Nb3Sn magnets
MQXF
4 pairs of shorter and more powerful dipole bending magnets to free up space for the new collimators (2x5.5 m length 11 T dipoles to replace 14.3-m-long LHC MB dipole)
Initially planned for 2020, now delayed
30 large aperture and more powerful quadrupoles around ATLAS and CMS to decrease the beam size and increase the integrated luminosity by a factor 10
Construction of pre-series and series magnets on-going, joint effort between CERN and US-AUP
E. Todesco
F. Savary
HL-LHC MBH 11 T

## Slide 12: The 12 T challenge – e. m. force
LHC MB
NbTi, Bp = 8.6 T
Fx = 3.4 MN/m
σθ,em = 50-60 MPa
Fz = 265 kN
HL-LHC MBH 11 T
Nb3Sn, Bp = 11.7 T
Fx = 7.2 MN/m
σθ,em = 100-110 MPa
Fz = 450 kN
HL-LHC MQXF
Nb3Sn, Bp = 11.3 T
Fx = 6.8 MN/m
σθ,em = 100-110 MPa
Fz = 1200 kN
Fx per half magnet; Fz per aperture
≈ 2 times more force/stress than in the LHC-MB dipoles, in a brittle conductor

## Slide 13: Deformation and stress
Effect of e.m forces
  change in coil shape  effect on field quality
  a displacement of the conductor  potential release of frictional energy
  Nb-Ti magnets: possible damage of insulation at~150-200 MPa.
  Nb3Sn magnets: possible conductor degradation at about 150-200 MPa.
All the components must be below stress limits.
Displacement scaling = 50
LHC dipole at 0 T
LHC dipole at 9 T
By P. Ferracin

## Slide 14: Overview of the coil stress
Collaring: By clamping the coils, the collars provide
  coil pre-stressing;
  rigid support against e.m. forces
  precise cavity
Yoking: Ferromagnetic yoke around the collared coil provide
  Magnetic function
  Mechanical function (increase the rigidity of the coil support structure and limit radial displacement)
  Alignment, assembly features…
Shell welding: two half shells welded around the coil to provide
  Helium container
  Additional rigidity
  If necessary, the welding press can impose the desired curvature on the cold mass
By P. Ferracin

## Slide 15: Overview of coil stress
4. Cool-down
  Components shrink differently
    Again, coil positioning within 20-50 μm
  Significant variations of coil stress
5. Excitation
  The pole region of the coil unloads
    Depending on the pre-stress, at nominal field the coil may unload completely
All these contributions taken into account in the mechanical design:
  Minimize coil motion (pre-stress)
  Minimize cost and dimension of the structure
  Maintain the maximum stress of the component below the plasticity limits
  …and for (especially) Nb3Sn coils, limit coil stress (150-200 MPa).

## Slide 16: Al shell: MQXF in HL-LHC
Aluminum shell, bladder and key technology, prima for accelerators
During cool-down increase in coil/shell stress
  Predictable stress variation  Capability to control final coil and shell stress
MQXFS4
MQXFS6

## Slide 17: Pre-stress: HL-LHC Nb3Sn magnets
This is the example of the MQXF and 11 T, the Nb3Sn magnets for the HiLumi upgrade.
  Strain gauges placed in the pole in MQXF, in the collar nose in 11 T. They allow seeing the pole unload
  Estimated stress proportional to square of current (forces)
  The end of the linear region implies a pole unloading, i.e. that the coil at the pole is not compressed any more
Reference pre-stress target for series magnets
Reference pre-stress target for series magnets

## Slide 18: Pre-stress – MQXF example
MQXFS6b reached the MQXF record of 19.1 kA, 93% of short sample at 1.9 K
Reassembled with much lower preload
Nominal without training, ultimate reached after retraining, and kept after thermal cycle
Very good indication of wide preload window, reproducibility of performance after reassembly and thermal cycle
Apparent plateau above ultimate may indicate that larger preload is beneficial to reach 90% of short sample
Unloading during powering
of MQXFS6b&6c
Training of MQXFS6b&6c

## Slide 19: Axial support
‘Two schools’ in terms of longitudinal support, with no consensus on the magnet community:
  Limit the coil displacements due to electromagnetic forces by having a rigid structure in the longitudinal direction (LHC Dipole, MBH-11 T concept, end-plate welded to the shell)
  Limit the coil displacements due to electromagnetic forces by having a rigid structure in the longitudinal direction and pre-load coil ends to compensate the axial forces and keep coil end turns under compression (MQXF, FRESCA2, concept, )

## Slide 20: Axial support: force or not force?
Two type of axial displacements:
  Relative movement of the coil with respect to the structure. It depends on the overall stiffness of the structure, i.e., independent of the level of pre-load in the ends.
  Relative movement of the coil ends with respect to the pole. It depends on the level of pre-load.
This was extensively studied in LBNL, developing the rods - plate axial pre-load system we are currently using for MQXF
S. Caspi, P. Ferracin., “Towards integrated design and modeling of high field accelerator magnets,” IEEE Trans. Appl. Supercond., vol. 16, no. 2, pp. 1298–1303, June 2006.
20
Axial displacements of inner layer’s (0.2 friction factor assumed).
Limited axial support (top) and full axial support (bottom).

## Slide 21: Axial support: welded end plate
We take as example the 11 T dipole for the HL-LHC
Slight pre-load at room temperature, to guarantee that there is still contact coil to end plate at 1.9 K.
Goal: limit the coil displacements providing a rigid lateral support
1in1 models:
  43 mm thick end-plate, 12 mm stainless steel shell.
2in1 models:
  75 mm thick end-plate, 15 mm stainless steel shell.

## Slide 22: Axial support: rods and end-plate
We take as example the MQXF quadrupole for the HL-LHC
Direct connection between the motion of the rod and the one of the coil ends
Goal: keep the pole turn under compression during powering.
Short models (1.2 m):
  Aluminum rods, 36 mm diameter
  Nitronic 50 end plate, 75 mm thick
MQXFA (4.2 m):
  Stainless steel rods, 32 mm diameter
  Nitronic 50 end plate, 75 mm thick
MQXFB (7.15 m):
  Stainless steel rods, 35 mm diameter
  Nitronic 50 end plate, 75 mm thick
 | Rod Strain [µɛ] | Rod Stress [MPa] | Force [MN] | % of Fem at Inom | Rod elongation [mm]
MQXFS | 75 | 6 | 0.02 | 2 | 0.12
MQXFA | 80 | 13 | 0.05 | 4 | 0.37
MQXFB | 80 | 16 | 0.06 | 5 | 0.60
Measured delta in the rods during powering from 0 to Inom

## Slide 23: Summary
We presented the force profiles in superconducting magnets. In dipole and quadrupole magnets, the forces are directed towards the mid-plane and outwardly.
    They tend to separate the coil from the pole and compress the mid-plane region
    Axially they tend to stretch the windings
The importance of the coil pre-stress has been pointed out, as a technique to minimize the conductor motion during excitation.
There are several ways of designing a support structure
  The solution for a given magnet is not unique
Structures based on collars are the workhorse of Nb-Ti magnets
  Guarantees adequate support to avoid deformation and allows giving azimuthal prestress
Aluminum shell structure guarantees that the peak pre-stress is reached in operational conditions
  Introduced in LNBL, used in several Nb3Sn. It has been scaled from 1-m-long to 3.4 m long magnets with LARP, and to 7.2 m long magnet in HL LHC MQXFB at CERN

## Slide 24: References
[1] MJB Plus, Inc. “Superconducting Accelerator Magnets”, an interactive tutorial.
[2] Paolo Ferracin, USPAS - Superconducting Magnets for Particle Accelerators, Unit 10, 13 and 14 (available in https://indico.cern.ch/event/440690/ )
[3] Y. Iwasa, “Case studies in superconducting magnets”, New York, Plenum Press, 1994.
[4] M. Wilson, “Superconducting magnets”, Oxford UK: Clarendon Press, 1983.
[5] A.V. Tollestrup, “Superconducting magnet technology for accelerators”, Ann. Reo. Nucl. Part. Sci. 1984. 34, 247-84

## Slide 25: Outline
Part I
  Particle accelerators, magnets and the need of superconductors
  Magnetic design and coil fabrication
Part II
  Mechanical design and assembly
  Quench, training and protection
  Outlook, what brings the future

## Slide 26: Quench definition
Quench = irreversible transition to normal state
  Heat generation > cooling
  Mechanical events
    Frictional motion
    Epoxy cracking
  Electromagnetic events
    Flux-jumps ,AC loss
  thermal energy (redistribute the energy in the whole coil volume, joule heating)
  Conversion magnetic energy
  Thermal events
    Degraded cooling
  Nuclear events
    Particle showers
Why do magnets quench?
Thermal energy released by
What do we do when a magnet quenches?

## Slide 27: Training
Superconducting magnets typically quench before reaching their nominal performance, the so-called training
Training is characterized by two phenomena:
  The occurrence of premature quenches
  The progressive increase of the quench current
    Irreversible change in the coil’s mechanical status
    Somehow the magnet is ‘improving’ or getting better quench after quench
  Mechanical induced quenches are considered the main causes of training in a superconducting magnet (frictional motion & epoxy failure)
Main features relevant for operation
  The ability to reach the target current with adequate margin (virgin training)
  The retraining expected during operation (i.e., memory after thermal cycle)

## Slide 28: Training in the LHC
The LHC dipoles were assembled by three manufactures
All magnets tested at 1.9 K in SM18 before installation in the tunnel
  All powered above nominal (11850 A, 7 TeV)
  About 50 % powered to ultimate (8 % more than nominal, 12850 A)
  Less than 10 % went through thermal cycle (biased sample)
    Magnet not reaching 12850 A with 9 quenches were tested after thermal cycle
  Bonus strategy: magnets reaching ‘rapidly’ ultimate were given a bonus
Training of LHC sectors to 6.5 TeV
Memory after cycle is important to avoid training in the accelerator (time consuming, i.e., $$$$).
  In the LHC we have 1232 magnets, connected in series in 8 circuits (i.e., 154 magnets per circuit)
  If every magnet needs to quench once to reach nominal  154 quenches per sector, and we can do only 2-3 quenches per day  training in the machine is very expensive and that is why memory after thermal cycle is VERY important!
In general, memory is better in Nb3Sn than in NbTi

## Slide 29: Quench: why it can be a problem ?
Quench is the result of the resistive transition, leading to appearance of voltage, temperature increase, thermal and electro-magnetic forces, and cryogen expulsion
If the process does not happen uniformly: as little as 1 % of the magnet mass may absorb the total energy – large damage potential !
Result of the chain of events triggered by a quench in an LHC bus-bar
Result of degradation due to local heating in a NbTi coil
Result of electrical short circuit quench heater to coil in a Nb3Sn coil

## Slide 30: Protection strategies
Two limiting cases in terms of magnet protection strategy:
  External-dump: The magnet is dumped externally on a large resistance (Rdump >> Rquench) as soon as the quench is detected (e.g. ITER)
  Self-dump: The circuit is on a short circuit and is dumped on its internal resistance (Rdump = 0) (e.g. LHC). Actually, external dump is not an option for a chain of accelerator magnets.
    Typical JCu ≈ 1000…1250 (A/mm2)
      Meaning dT/dt ≈ 1000…2000 (K/s)
      We need to dump quickly! τ(300 K) ≈ 0.15…0.3 (s)
    Iop ≈ 15 (kA)
    E/l ≈ 1000 (kJ/m)

## Slide 31: The quench event: summary
Chart: time
Temperature rise in the conductor
Quench starts
Thermal energy released by a precursor
Quench front propagates
Quench detected
Quench validated
(power supply off, protection system fired)
Heaters effective
Distributed quench in the coil
Validation delay
Heater delay
Current decay due to the resistance growth in the coil
Typical time scale:
From quench start to quench detected ~ 5 ms
Validation delay ~ 10 ms
Heater delay ~ 20 ms
Current decay ~ 100-200 ms
Maximum acceptable temperature: 350K

## Slide 32: Protection strategy – External dump
The magnetic energy is extracted from the magnet and dissipated in an external resistor:
L
normal operation
S1
L
Rquench
quench
S1
Rdump
Rdump
R = 0

## Slide 33: Protection strategy – Self dump
In the case of the LHC, the magnetic energy is completely dissipated in the internal resistance, which depends on the temperature and volume of the normal zone
  (when increasing the temperature, the material becomes resistive resistance increase current decrease (fix voltage))
L
R = 0
D
normal operation
S1
L
Rquench
D
quench
S1

## Slide 34: Protecting a magnet string
Magnet strings (e.g. accelerator magnets, fusion magnetic systems) have exceedingly large stored energy (10’s of GJ):
    energy dump takes very long time (10…100 s)
    the magnet string is subdivided and each magnet is by-passed by a diode (or thyristor)
    the diode acts as a shunt during the discharge
M1
M2
M3
MN

## Slide 35: Adiabatic heat balance
The simplest (and conservative) approximation for the evolution of the maximum temperature during a quench is to assume adiabatic behavior at the location of the hot-spot:
Electrical resistivity of the stabilizer (Cu):
:
  The circuit is a RL circuit
    with the magnet inductance L
    and a highly variable resistance R(t), growing with time
    the higher the resistance, the faster the current dump, the lower hotspot

## Slide 36: Hot spot temperature
Adiabatic conditions at the hot spot:
Load due to the current decay, that should be made as fast as possible and is an observable: Quench tax
Can be integrated
Ability of the cable of « taking » the current (combination of enthalpy and resistivity): Quench capital (Γ)

## Slide 37: Protection limit
Ideal case: all magnet is quenched at the quench start
HERA
LHC-MB
HD2, 11T,
FRESCA2, RMM
Ultimate protection limit?
Reality: we need time to detect, validate and quench the magnet.
Enthalpy of the strand volume (neglecting the insulation)
Assuming adiabatic conditions
Magnet stored energy per unit volume.
Volumetric heat capacity of the cable
i = copper, superconductor and insulation.

## Slide 38: Detection and validation
The time needed to detect and validate a quench is very expensive in terms of temperature rise. And here is where current density become critical!
The detection threshold are defined through two parameters:
  A voltage level (above the noise level) – typically 100 mV  3-5 ms at nominal
  A validation time (to reject spurious spikes in voltages) – typically 10 ms
Voltages staying above voltage level for a time longer than validation time are interpreted as a magnet quench, and activate the protection system
  Therefore on the time needed to detect the voltage, one has to add the validation time  15 ms
All coil quenched after 35 ms from quench start
Nominal

## Slide 39: Quench initiation: quench heaters
Principle: temperature rise in the conductor through the heating of metal strips attached to the coil.
They are typically installed in the outer surface of the coil
Time required to induce a quench at nominal ∿ 10 ms
IL
Stainless Steel
Copper
MQXF Heater Lay-Out (heater in the inner and outer layers)
11 T Heater Lay-Out (only outer layer heaters)
OL - HF
OL - LF
OL - HF
OL - LF
Stainless Steel
Copper
Outer layer heater design
Outer layer heater design
Inner layer heater design

## Slide 40: Quench initiation: CLIQ
CLIQ (Coupling Losses Induced Quench)
  This system is based on injecting in the magnet coils two opposite impulses of current via a capacitor
  The mechanism is the heating due to interfilament coupling losses induced by the variation of the field
    It has been developed at CERN and patented in 2014 (EP13174323.9)
Electrical scheme of CLIQ implementation in a dipole
G. Kirby, V. Datskov, E. Ravaioli et al. IEEE TAS 24 (2014) 0500905

## Slide 41: The case of MQXF
The baseline protection scheme of the HL-LHC MQXF quadrupole relays on CLIQ + QH, a prima for accelerator magnets.
CLIQ + QH, provides a redundant protection system. In the case of MQXF, it reduces the quench load by 20 % at high current, decreasing the hot spot temperature by 100 K (350 K QH only, 250 K QH+CLIQ).
Comparison of quench load in MQXF magnets when protected only with QH and QH+CLIQ
Current decay in MQXF for CLIQ + QH or QH only protection

## Slide 42: Summary
Magnet protection concerns two different phenomena: increase of temperature (joule heating) and increase of voltage (transition to resistive state).
The two key parameters for the protection of a magnet are:
  Current density in the copper (heating rate)
  Energy density in the coil (needs to be dissipated in the coil enthalpy)
A resistor in series with the magnet allows to dump part of the energy, but it is not effective for long magnets or magnets in a string due to the voltage limitation.
For long and high current density, the protection relies on the induction of a rapid transition to resistive state in the full coil.
  In the LHC-MB NbTi magnets, the time margin is ≈ 100 ms.
  In the HL-LHC Nb3Sn magnets, the time margin is ≈ 40 ms.
Two systems to induce a resistive transition in the full coil:
  Quench heaters: temperature rise in the conductor through the heating of metal strips attached to the coil.
  CLIQ: temperature rise in the conductor through the inter-filament coupling losses induced by the variation of the field.

## Slide 43: References
General principles and equations:
  M.K. Wilson, Superconducting Magnets, Oxford, Clarendon Press, 1983.
More on quench propagation and scaling :
  A. Devred, General Formulas for the adiabatic propagation velocity of the normal zone, IEEE Trans on Magnetics, Vol. 25, No. 2, March 1989
  E. Todesco, “Quench limits in the next generation of magnets” CERN Yellow Report 2013-006 10-16
  S. Izquierdo Bermudez, et al., Analytical method for the prediction of quench initiation and development in accelerator magnets, Cryogenics, Volume 95, October 2018, Pages 102-109
U.S. Particle Accelerator School, lectures from Ezio Todesco, http://etodesco.web.cern.ch/etodesco/
Wide literature on specific results on magnets and outlook for future magnets, for instance
  H. Felice, et al., “Instrumentation and quench protection for LARP Nb3Sn magnets” IEEE Trans. Appl. Supercond. 19 (2009) 2458-2462
  S. Izquierdo Bermudez, et al., "Overview of the quench heater performance for MQXF, the Nb3Sn low-beta quadrupole for the high-luminosity LHC" IEEE Trans. Appl. Supercond. 28 (2018) 4008406
  T. Salmi, et al., “Quench protection analysis integrated in the design of dipoles for the Future Circular Collider” Phys. Rev. STAB 20 (2017)

## Slide 44: Outline
Part I
  Particle accelerators, magnets and the need of superconductors
  Magnetic design and coil fabrication
Part II
  Mechanical design and assembly
  Quench, training and protection
  Future outlook

## Slide 45: HL-LHC
The IR LHC today:
The HL-LHC IR:

## Slide 46: HL-LHC
A large variety of (fun) magnets
Challenge associated with the production of the first Nb3Sn accelerator-ready magnets
The project is now in series production phase, with the first chain of magnet being assembled in the IT-String in SM18!

## Slide 47: What is next?
From a magnet perspective,
  explore the limits of Nb3Sn and industrialize the technology.
  develop high temperature superconductors (HTS)
High Field Magnet (HFM) program coordinates these efforts in Europe https://arxiv.org/pdf/2504.16885
  Collaboration agreements between CERN and EU institutes to build demonstrators
  CERN also working on small scale demonstrators to explore the limits
US Magnet Development Program (MDP), pushing magnets beyond the present state of the art (https://usmdp.lbl.gov/)
Magnets under development in the High Field Magnet Program
https://home.cern/science/cern/fcc-study-media-kit

## Slide 48: What is next?
Other machines that also offer a great variety of challenges for magnet builders are also being explored, such as the muon collider
  a) production solenoid;
  b) 6D muon cooling solenoids:
  c) final muon cooling system;
  d) fust-cycling muon acceleration magnet;
  e) collider ring magnets;
  f) IR magnets.
See https://muoncollider.web.cern.ch/

## Slide 49: Beyond LTS: the broad world of HTS
The broad world of HTS, opens the door to fields > 16 T
So far, most of the developments focused on HTS inside outsert coils made of Nb3Sn or NbTi
EUCARD REBCO HST insert
CEA + CRNS Grenoble, J.M. Rey, F. Borgnolutti, M. Durante, CEA-Saclay
FEATHER2 REBCO HST insert
CERN, Gijs the Rijk, Glyn Kirby
Bi-2212 racetracks
MDP, US
Bi-2212 CCT
MDP, US

## Slide 50: In conclusion
Magnet technology is a complex, but very exciting, business: are you convinced?
There is no magic technology, some are more mature than others.
There are remaining challenges to go to high field in a robust and reproducible manner.
The High Field Magnets Program is being launched to tackle these issues.
The magnet community will need to be creative and pragmatic.
We need bright minds!

## Slide 51: Thank you
For questions, don’t hesitate!
susana.izquierdo.bermudez@cern.ch