## Slide 1
Electromechanical properties of ReBCO tapes, stack cables and coils
A. Kario, T. Nes, D. Velthuis, S. Wessel, J. Rietberg, A. Nijhuis, S. Otten, W. Huijskes, L. Rietkerk, C. Topaloglu, T. Hanhart, R. van Ingen, M. Goodwin, M. Dhalle, and H.H.J. ten Kate

## Slide 2
Single ReBCO tapes mechanical examinations
Transverse load
Axial tensile
ReBCO sub-stack cables
ReBCO demonstrator coils
Outline

## Slide 3
Cylinder press
Ball joint
Pushing block
Ti-plate
Terminal
Ball joint
Pushing block
Transverse load setup - ReBCO tapes at 77 K
Hydraulic press-based set-up, design and build for MuCOL related examinations.
Ball-joint alignment, titanium support, variable width, thickness, possible.

## Slide 4
Tape | 𝜎irr [MPa]
S-Innovation | > 900
Fujikura, 22-0012-09 | 400
SSCT, ST2903-105 | 750
Critical current as function of transverse load @77 K
Transverse load vary from 400 MPa to above 900 MPa for different manufacturers.
N-value follows the critical current degradation.
Transverse load limit is defined by substrate plastic deformation limit.

## Slide 5
Misalignment of mechanical load = earlier degradation
Focus Ion Beam cut, SEM images, examples of cracks.
ReBCO layer
Hastelloy substrate
Hastelloy substrate
ReBCO layer
Critical current decrease in the primary stage of loading.
Post-mortem analysis shows irregular positioning of the cracks in the ReBCO structure.

## Slide 6
substrate
buffer layers
platinum layer
ReBCO layer
crack
crack
cracks
Tape longitude section after transverse load up to 700 MPa
FIB cut shows damage by crack formation in ReBCO layer

## Slide 7
Axial tensile strain setup at 77 K
Stress-strain properties, Ic & irreversibility limit for tensile axial strain.
Tape | tSubstrate [𝜇m] | tCopper [𝜇m] | Ic [A]
SSTC | 52 | 22 | 186
Fujikura | 49 | 25 | 204
Faraday | 39 | 13 | 162
Substrate : Hastelloy, width = 4 mm
5 MPa
7

## Slide 8
Tape | E [GPa] | 𝜎ys [MPa]
SSTC | 125 | 600
Fujikura | 135 | 621
Faraday | 150 | 875
Tape | 𝜖irr[%] | 𝜎irr [MPa]
SSTC | 0.48 | 709
Fujikura | 0.43 | 626
Faraday | 0.58 | 900
Axial tensile Stress-Strain curves & Ic(𝜖)
8

## Slide 9
The 5-tape stack showed limited degradation (2-5%) for the bending radii of 250 mm and 150 mm.
The 10-tape stack had severe critical current degradation (20-25%) for the radii of 250 mm and 150 mm.
Bending at 50 mm caused detachment at the soldered interface and buckling to both cables.
Critical current and n-value for 5- tape stack depended on bending radius
Voltage tap
Current lead
Voltage tap
Bending of the soldered 5- and 10-tapes stack cables
9

## Slide 10
ReBCO stack cable critical current versus geometry
10
Two tapes stack
VIPER
Twisted Stack-Tape Slotted-Core
SuperOx YBCO 2G HTS data at 20 K from Robinson Inst. data base.
Tapes are assumed to be infinitesimally thick.
Length of the tapes can be neglected.
B-field (T)
Example of the geometry with magnetic field map.

## Slide 11
ReBCO stack cable critical current versus geometry
11
Tape width variation
Cable radius 12 mm
Tape separation 0.6 mm
2 tapes per stack
Cable radius variation
Cable radius 12 mm
Tape width 6 mm
2 tapes per stack
Separation between tapes
Cable radius 12 mm
Tape width 6 mm
6 tapes per stack

## Slide 12
12
Twente cryogenic press for loading stack (sub)cables
Pressing Force
ReBCO stack
Copper
stabilizer
20mm
ReBCO stack cables for transverse load
Pressing fin
Upgrade Twente cryogenic press: design and manufacturing of 4.5 kA current leads for stack test in LN2

## Slide 13
Transverse load test of dry-stack sub-cable at 77 K
V1 V2
V1 V2
V9
V9
Press bore was limiting cable length resulting in current shearing and lack of superconducting transition.
Press force distribution needs to be improved to perform measurements of transverse load in weak direction.

## Slide 14
Section 2 most degraded
Misalignment during loading of the stack.
Tapes extracted from stack after loading to 275 MPa

## Slide 15
Summary: mechanical properties of tapes and stacks
Transverse load varies from 400 to above 900 MPa for different manufacturers and is caused by plastic deformation of the substrate followed by cracks in the ReBCO layer.
Axial stress-strain also varies among different producers.
Bending of the soldered sub-stack at 50 mm radius caused detachment at the soldered interfaces and buckling in both 5 and 10 tapes cables.
Transverse load: existing bore is limiting the cable sample length causing current shearing and not seeing the superconducting transition.
Press force distribution needs to be improved to measure the transverse load effect in the weak direction.

## Slide 16
Outline:
Coil tests at 77K in self-field
Double tape dry-wound coil test at 4.2 K in background field.
Electro-magnetic and microstructural examination of extracted tape.
Time and temperature influence on tape critical current.
Double tape soldered coil test at 4.2 K in background field.
I
I
102 mm
52 mm
Copper terminal plate
Attachment current leads
G10 insulation
Clamping bolts
Current
in
Current out
146 mm
NI Coil-pack
Non-insulated ReBCO coils: geometry & construction
NI dry-wound
NI soldered
Dry-wound and soldered coils with single and double tape
T. H. Nes et al. 10.1109/TASC.2022.3148968
16
Notes: Coil description & outline

## Slide 17
Non-insulated ReBCO coils: critical current at 77 K in self-field
17
Coil critical current = 95 A, quench current = 116 A
Coil critical current = 38 A, quench current > 400 A
Coil critical current = 180 A, quench current =194 A
Coil critical current = 163 A, quench current > 240 A
Double tape coils
Two voltage criteria for both coils were used: 1 μV/m for soldered one and 10 μV/m for dry wound coil.
Single tape coils
Notes: -Ic (77K, s-f), as function of turn number, scheme of the coil, we see, single and double tape, where soldered-measured in all sectors and dry-inner only, quench current did not allow to measure all sectors (margin)

## Slide 18
18
Non-insulated ReBCO coils: magnetic field in the coil center at 77 K in self-field
Single tape coils
Ic=95 A
Ic=38 A
Magnetic field measurements in the center show saturation and current sharing especially in the case of soldered coils.
Double tape coils
Ic=180 A
Ic=163 A
Hall probe
Notes: -magnetic field was measured as well, in coil center, and in deviation from linearity we can nicely see the current sharing. Soldered: bigger saturation region, dry-only in single tape, the dry-wound double tape coil and soldered was chosen based on those measurements for Lhe test!

## Slide 19
19
Dry wound double-tape coil: critical current at 4.2 K in background field
Critical current of the coil as a function of cycling in self-field and in background magnetic field of up to 7 T.
Calculated critical current at 4.2 K and self-field: 2.4 kA
VI curves after cycling:
Ic reduced further to 530 A
Coil performance degraded by 30%.
Magnetic field B [T]
Solenoid background magnet
Dry-wound 2-tape pancake coil
Notes: Calculations of the Ic if the coil in external field show 2.4 kA of current for thise coil, coil was mounted in background magnet, instrumented, measured. Degradation in self-field, further degradation in background field, 30%

## Slide 20
Dry wound double-tape coil: degradation of the coil
T.H. Nes. PhD. Thesis, 2023
Magnetic field measurements in center of coil show degradation of the coil.
Coil measurements at 77 K in LN2 and in self-field after LHe show severe critical current reduction.
20
Notes: In terms of magnetic field-degradation is noticeable also, by lower values of the field, saturation of the field is not observed, no signs of current sharing. The coil was measured in LN2, to look at the possible reversible effects and we see permanent degradation to few amps in the central windings, tape was unwound for further examinations and measured using reel-to-reel technique

## Slide 21
21
Reel-to-reel measurement of the ReBCO tape from an unwound pancake coil shows permanent degradation of the critical current of the tape.
Dry wound double-tape coil: degraded at 4.2K in LHe, postmortem analysis Ic@77K, self-field
Red dots: measured critical current
Orange arrows: lower bound of Ic
Original tape: Ic = 380A.
end, 30 meter
beginning, 0 meter
Notes: Ic(tape position), cricles Ic and triangles lower bonund of Ic, here only half-length of the tape measurement is shown, no correlation, a lot of defects limiting Ic to few or 10th of Amps, different type of defects were observed visually and examined microstructurally

## Slide 22
22
Dry-wound double-tape coil: postmortem analysis, microstructure, blister type
22
Blisters
Cu ~ 20 microns
Ag ~ 2 microns
SEM, top layers
SEM, FIB cut
Irreversible degradation of the tape; local defect of blister type; internal delamination of the tape structure, on Ag-ReBCO interface and in the ReBCO layer itself.
melting
End of crack
SEM, FIB cut
Al2O3 ~ 80 nm
Y2O3 ~ 20 nm
MgO ~ 5 nm
LaMnO3 ~ 20 nm
CeO2 ~ 200 nm
SEM, FIB, buffer layers
delamination
400 nm
500 nm
10 μm
Notes: Blister, cut in the center, delamination, cuts further away, melting of the ReBCO

## Slide 23
Dry-wound double-tape coil: postmortem analysis, microstructure, meander type
23
23
Barium, Oxygen reaches layers on the surface
SEM
EDX: O map
EDX: Ba map
Confocal microscope, topology
Optical microscope, tape surface
Meander shape black spots
Irreversible degradation of the tape; local defect of the meander shape; out-diffusion of the barium to the surface of the tape.
Notes: Meander shapes, visible on the tape structure, surface, analyzed by confocal microscopy, layer out-diffusion of barium

## Slide 24
1h winding with 176°C Solder
V1
V2
V3
V5
Soldered ReBCO pancake coils: degradation due to soldering time and temperature excluded
Shanghai tape is like other fabricants tape, concerning heat treatment temperature and time.
Normalized Ic for 10 μV/cm vs heat treatment for 60 min.
24
Notes: Beside ni-dry-wound coil, we analyzed the soldered doble tape coil as well. Since we noticed lower Ic of the tape in inner sectors side examination of the SST tape as function of temperature and time was done, and degradation due to that was excluded.

## Slide 25
25
25
Non-insulated ReBCO coils: time constant
Coil | τ [s] | Reduction factor
Single tape | 7.4 ± 0.1 | 1.2 ± 0.4
Double tape | 6.1 ± 0.1 | 
Coil | τ [s] | Reduction factor
Single tape | 740 ± 12 | 3.3 ± 0.8
Double tape | 222 ± 2 | 
Magnetic field [T]
Time constant τ [s]
Short time constant of 25 s in dry-wound coil at 4.2 K and 5 T background field was measured.
While long-time constants of 10 min in soldered coil at 4.2 K and 5T background field are present.
Dry wound coils
Soldered coils
Notes: Time constants, when we look at those coils, 77K and self-field, reduction of factor 4 expected, due to 1-2 tapes and coil inductance, dry wound non, soldered below. In a case LHe measurements….

## Slide 26
26
Summary: ReBCO pancake coils experience
Dry-wound coils:
Small “self-protection” margin (~20 A at LN2) and short time-constants (25 s at 4.2 K and 5 T background field).
Severe degradation of entire tape length after test at 4.2 K in LHe, caused by different visible defects reducing the tape Ic.
Soldered coils:
Relatively big “self-protection” margin (>200 A at 77 K, LN2) but long-time constants (10 min at 4.2 K in LHe and 5 T background field).
Degradation of Ic due to temperature and time of soldering excluded.
Test at 77 K in self-field after LHe measurement should be done. No indication of degradation of the coil at 4.2 K in LHe was observed.
R.I.P.
NI-coils need to be studied using combination of multi-simulation tools (electromagnetic and mechanical) and extended experimental effort.

## Slide 27
At University of Twente, torture LAB, we contribute to the development of accelerator type magnets, by investigating various tapes, - cables; and non-insulated and insulated small coils, mostly looking at electromagnetic and mechanical properties.
Summary
Few references:
Nienke Buskens (2023), bachelor thesis, The Effect of Bending on the Critical Current of ReBCO Based Stack Cables : High Magnetic Fields for Muon Collider, https://essay.utwente.nl/96263/.
Ward Maxim Huijskes (2024), master thesis, Preparations of transverse stress experiment of soldered TSTC for high-field magnets.
Lennard Rietkerk (2024), master thesis, Transverse stress tolerance of ReBCO superconducting dry-wound stack cables.
Jurgen Rietberg (2024), master thesis, Critical Current testing of ReBCO tapes under applied axial tensile stress and strain with new TARSIS setup.