## Slide 1: Jc Scaling and Data Fitting for Nb3Sn Wires
Simon C. Hopkins
HFM-MDP Forum, 20 February 2025

## Slide 2: Scaling Laws for Nb3Sn
Nb3Sn shows a consistent scaling behaviour of flux pinning force Fp or critical current Ic with field, temperature and strain
There are many alternative parameterisations, but many can be reduced to the separable form:
  with
In this presentation, I omit the strain scaling for simplicity

## Slide 3: Field Dependence, f(b)
The pinning force density Fp scales with temperature, but has a fixed shape f(b) vs. reduced field (for a certain wire)
The classic pinning theories give:
  where p and q depend on the pinning mechanism
  For conventional Nb3Sn wires we expect p = 0.5 and q = 2 for grain boundary pinning  Fp,max at b = 0.2
  For point pinning, we expect p = 1 and q = 2 pinning  Fp,max at b = 0.33

## Slide 4: Temperature Dependence, h(t)
For the temperature scaling term:
  several parameterisations have been proposed, e.g.
  ‘Hybrid2’, ‘HFM’…
  Godeke, Bottura…
ν = 1.52 arises from an approximation to Maki-DeGennes; Ekin et al. found 1.50 ± 0.04
For fits to a variety of data, Ekin et al. found η to be 2–2.4, not necessarily completely independent of wire type

## Slide 5: Fitting Methodologies
Ekin distinguishes ‘raw scaling data’ from ‘global-fit-model’ values
  Raw scaling:
    separately scale f(b) at each T (and ε)  Bc2* and Fpmax
      note: relatively insensitive to the shape of f(b)
    analyse their T and ε scaling  bc2(t), h(t) etc. (a few parameters at a time)
    globally fit only the remaining parameters (e.g. the overall constant C) to the full Ic data set
  Global fit:
    assume a scaling model and simultaneously fit all parameters to the Ic data set
  The two can yield significantly different estimates of bc2(t) etc., and the former is expected to be better suited to extrapolation
Methods and minimum data sets extensively explored for ‘Extrapolative Scaling Expression (ESE)’ expression:
  Topical reviews by Ekin et al.: Supercond. Sci. Technol. 23 083001, 29 123002, 30 033005
  Combinations with magnetisation data by Pong et al.: Supercond. Sci. Technol. 35 095006

## Slide 6: Fitting Considerations: Fp, Ic, Jc
Ekin’s formulation was expressed as a scaling of pinning force Fp (per length)
  When fitting Ic data, a modest reduction in error has been reported by converting to Fp for fitting
This can be equivalently formulated for a volumetric pinning force density Fp and Jc
  Straightforward conversion, but it must be clear which Jc – e.g. non-Cu or layer Jc – is meant
  For large data sets, there may be a small distinction between fitting Jc calculated per sample (from its measured Cu/non-Cu) and fitting Ic with a subsequent conversion

## Slide 7: Fitting of Transport Ic
At CERN, transport Ic measurements are performed systematically for wire and cable acceptance
Some challenges for the available parameter ranges:
  Limited maximum current and field: at CERN, currently 15 T, ~2000 A
  Limited temperature range: at CERN, currently only ~1.9 K and ~4.2 K
  Routine testing covers a limited field range (depending on wire type, typically 12–15 T)
  At ‘low’ fields, limitations from magnetothermal stability as well as the current limit
The sample/test configuration and any subsequent data processing have a significant effect, and should be reported with the fit:
  Fits ‘work’ with or without self-field correction, but don’t yield the same result for f(b)
    When implemented in Roxie, a self-field flag must be set accordingly
  The strain state also depends on the sample configuration, and should be reported and/or (approximately) corrected to a zero (or defined) state
    Transport measurements at CERN are on Ti-Al-V barrels

## Slide 8: Fitting of Magnetisation Data
Magnetisation measurements typically allow measurements over a broad range of temperature
  VTI from 1.9 K to >> Tc for the VSM at CERN
Some very high field facilities exist, but field range is typically more limited:
  10.5 T at CERN; 5–7 T is common
  Often little overlap with transport data
At low field, flux jumps complicate the interpretation
Again, the sample/test configuration can be influential – in addition:
  Dependence on sample length – preferable to favour ‘long’ samples:
    Relative to the twist pitch, and
    More representative average, lower noise, reduced error contribution from end preparation etc.
  At CERN, constrained to ~6 mm diameter sample space: small ‘coils’ tested whenever possible

## Slide 9: Determination of Bc2*(T)
Determining Bc2* over the full temperature range is not straightforward from a single method:
  Transport data are often available only at low temperature, for which Bc2* is larger than the maximum test field
  Magnetisation data allow Bc2* to be found directly (only) at high temperature
There have been reports of significant errors in extrapolation to high field both for transport and magnetisation data
  Transport
  Segal et al., J. Phys. Conf. Ser. 1559 12062
  Magnetisation
  Tarantini et al., Supercond. Sci. Technol. 32 124003

## Slide 10: Determination of Bc2*(T)
A divergence between values determined from transport and magnetisation data has also been found at low temperature
Inhomogeneity is one possible contributor:
  A radial dependence of both composition (Sn at%) and microstructure is often found in Nb3Sn filaments/sub-elements
  This corresponds to a radial profile of Tc and Ic, with a form depending on the conductor type/design and its heat treatment.
Procedural approaches to address limited data, e.g. Pong et al.:
  Bc2*(T) from magnetisation reasonably reliable at high temperature (~10 K); Tc* fit may benefit from allowing fitting of ν
  Ekin et al., Supercond. Sci. Technol. 29 123002

## Slide 11: Sampling and Scope
The sampling and heat treatment cycle should also be reported with the fitting parameters:
  Generally Bc2 etc. depend on the heat treatment cycle, not just Fpmax
  Must be clear whether the fit represents a particular spool/cable/coil, the procurement specification, or some statistic of the performance distribution achieved in production
    All are useful: witness reports to evaluate coil performance, magnet design, etc.
    Important to note that small-scale orders for R&D activities may not accurately reflect the performance distribution obtained in large-scale procurement
Care is needed to avoid biasing the fit, e.g.:
  More tests at 4.2 K than 1.9 K – consider including only samples for which both are available
  If fitting by minimising errors, the error contributions could be weighted to correct various biases:
    Different numbers of data points vs. T and B
    Proportionally larger errors at low currents; larger absolute contributions at high current

## Slide 12: Non-Cu Jc(B,T) for Current Wires
For reference fits to current wire in HFM, I have used this form:
  Implemented in Roxie as ‘11. CERN High Field Nb3Sn’
  Consistent in form with witness reports
  Matches Hybrid2 presented earlier
    …but with ν adjustable, and terminology aligned
  Bp implies peak field on conductor: fits made with self-field correction
For initial fits, I have fixed several parameters
  α and ν at typical and nominal values – could be fitted later if sufficient data to justify differences
  p and q as expected for grain boundary pinning – not suitable for APCs/internal oxidation
α | 1
ν | 1.52
p | 0.5
q | 2

## Slide 13: Data for Fitting
Extensive transport Ic data are available from wire verification and cable qualification
  Only round wire (not rolled/cabled) considered
  Each fit for a single heat treatment cycle
  However, most data for a limited field range, with much lower sampling at 1.9 K than 4.2 K
    Wire from R&D procurement not initially characterised at 1.9 K
Very limited magnetisation data currently available:
  Tc0 has been obtained from Bc2(T) magnetisation data for the MQXF wire
  The same Tc0 value is temporarily assumed for other RRP wires, with Bc20 fitted from transport data
  Further tests are planned in the coming weeks

## Slide 14: Wire Types
 | DEM-0.7 | ERMC-0.7 | MQXF | ERMC-1 | DEM-1.1
d (mm) | 0.7 |  | 0.85 | 1.0 | 1.1
Layout | 60/91 | 78/91 | 108/127 | 162/169 | 
ds (µm) | 54 |  |  | 58 | 64
Cu/non-Cu | 1.8 (≥ 1.6) | 1.2 ± 0.2 | 1.2 ± 0.1 | 0.9 ± 0.2 | 
Nb:Sn | 3.6 (reduced Sn) |  |  | 3.4 (standard Sn) | 
Heat treatment | 665 °C 50 h |  |  | 650 °C 50 h | 665 °C 50 h
HL-LHC ref.
HFM high field coils (or ungraded)
HFM low field coils

## Slide 15: Heat Treatments
In the previous slide, heat treatment cycles are the manufacturer’s recommendations
  Established baseline for MQXF
Other cycles are in current use:
  To improve magnetothermal stability of ERMC-1 and DEM-1.1: 650 °C with 30 h or 50 h duration
  For graded designs with simultaneous reaction of conductors for which suggested HT cycles may differ (R2D2)

## Slide 16: MQXF and DEM-1.1
Fitting parameters for MQXF and DEM-1.1 wire are shown below for the HTs in current use
  Using 665 °C 50 h for DEM-1.1 increase Bc20 by ~0.5 T
 | MQXF | DEM-1.1 | 
Heat treatment | 665 °C 50 h 3_665_B | 650 °C 50 h 3_650_A | 650 °C 30 h 3_650_I
Scope | Mean | Typical1 | Low2
Bc20 (T) | 29.56 | 29.66 | 28.77
C0 (T·A/mm2) | 220303 | 240652 | 239814
Tc0 (K) | 16.25 |  | 
1 Sampling representative of one cable qualification
2 Spool at the low end of the Ic distribution

## Slide 17: MQXF and DEM-1.1
Non-Cu Jc(B) at 4.2 K and 1.9 K
4.2 K
1.9 K

## Slide 18: Next Steps
Currently compiling more complete data sets for each wire layout
  Transport Ic measurements and stability tests continuing for improved statistics as cables are qualified
  Comparison of alternative heat treatment cycles
  Magnetisation measurements resuming shortly for more robust temperature-dependent and low-field data
Propose to create an EDMS document for each wire design and reference fit, which can be updated (version controlled) as new data become available