## Slide 1
Experimental tests for winding technology of Final Cooling Solenoid
M. Abdel Hafiz
& Final Cooling Solenoid working group

## Slide 2
Final Cooling Solenoid
40 T , 50 mm bore diameter
Each pancake is in a solder matrix to redistribute stress
B. Bordini & al., 2024
Proposal for widing a pancake :
How does that effect the tape properties ?

## Slide 3
Final Cooling Solenoid
Outline
Effect of Temperature on tape
Description of the winding
Effect of the winding proposal on pancake properties
Chemical etching to control transverse resistance
Effect of the etching on pancake properties
All results presented from this study have been performed on a Theva TPL4421

## Slide 4: Temperature influence on IC Literature
IC degrades with time and temperature
2 mechanisms of degradation :
  Oxygen-out diffusion from grain boundaries of ReBCO layer
  T > 250°C  Oxygen-out diffusion from grains of ReBCO layer
Heat treatment cycle does not affect
Stabilizer thickness is a parameter of degradation
Depends on the manufacturing process
Vacuum could have an effect
G. Bradford & al. MT26 (2019)
20 minutes plateau
M. Bonura & al. (2022)
I. Falorio (2020)
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 5: Temperature influence on IC Preparing samples
Sample Holder
Sample holder :
G10 insulating plate (~ 1 mm)
Both sides :
  Cu coating (~75 )
  SnPb coating
Preparing and coating samples do not visibly affect IC on measured length
IC Degradation of Theva TPL tape < 3% after 2h @200°C in SnPb bath
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid
Sample cycled :
Coating tape and soldered to the sample holder
IC measurement @ 77K
Heated in solder bath @200 °C
Cycling process

## Slide 6: Hot winding Winding tool prototype
Tape spool
Flux bath
Rotating wheel
Wound spool
(Opened) Oven
Heater slot
Solder bath
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 7: Hot winding Winding protocol
Winding spool
Flux bath
Solder bath (Sn63Pb37)
Tape spool
Precoating tape
  Heat up to 200°C to melt SnPb (~15 min)
  Tape passes through flux and solder (~ 10 s)
  Gravity seems to be enough to remove some excess of solder
  Precoating tapes allows to :
    Control coating of tapes
    Remove flux bath during winding process
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 8: Hot winding Winding protocol
Precoating tape
  Heat up to 200°C to melt SnPb (~20 min)
  Tape passes through flux and solder (~ 10 s)
  Gravity seems to be enough to remove some excess of solder
  Precoating tapes allows to :
    Control coating of tapes
    Remove flux bath during winding process
Starting winding
  Heat up the oven to 200°C to melt SnPb (~45 min)
  Remove the door & install the mandrel
    Invar mandrel has been chosen for these tests
      Invar shrinkage from 473K to 77K is lower than HTS and limiting radial tensile stresses in the pancake during cooling down
      Invar bounds well and easily to SnPb
    Tape is pre-installed on the mandrel
      Hooked in a groove
      Spot welded to the mandrel
  Close the door and reheat to 200°C (~20 min)
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 9: Hot winding Winding protocol
Precoating tape
  Heat up to 200°C to melt SnPb (~20 min)
  Tape passes through flux and solder (~ 10 s)
  Gravity seems to be enough to remove some excess of solder
  Precoating tapes allows to :
    Control coating of tapes
    Remove flux bath during winding process
Starting winding
  Heat up the oven to 200°C to melt SnPb (~45 min)
  Remove the door & install the mandrel
    Invar mandrel has been chosen for these tests
      Invar shrinkage from 473K to 77K is lower than HTS and limiting radial tensile stresses in the pancake during cooling down
      Invar bounds well and easily to SnPb
    Tape is pre-installed on the mandrel
      Hooked in a groove
      Spot welded to the mandrel
  Close the door and reheat to 200°C (~20 min)
Winding pancake
  No controlled tension is applied nor measured
  Winding duration for 15m of tape took 20 to 40 minutes
Cooling down
  To room temperature (~ 1h)
2h of heating for the tape
4 Pancakes successfully prepared
Tin drop
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 10: Pancake Properties Preparation for experiment
Current leads
Outer ring
Inner ring
Voltage taps slots
Pancake
Installing current leads
  Ensure electrical contact from rings to pancake without melting the pancake (183°C)
    Low temperature solder (Bi58Sn42 138°C)
Tests performed @77K
  Measure critical current IC of the pancake
    Steady state study with low ramp rate
  Measure time constant
    Steps current
  Hall Probe located in the center of the pancake to measure central field
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 11: Pancake Properties Experiment Scheme
RS
Pancake
Hall probe
RT
RL
UL
US
UB
 |  |  | Power supply current
 |  |  | Shunt current
 |  |  | Pancake current
 |  |  | Transverse (radial) current
 |  |  | Lenghtwise (azimuthal) current
 |  |  | Shunt voltage
 |  |  | Pancake voltage
 |  |  | Hall Probe Voltage
 |  |  | Power supply current
 |  |  | Shunt current
 |  |  | Pancake current
 |  |  | Transverse (radial) current
 |  |  | Lenghtwise (azimuthal) current
 |  |  | Shunt voltage
 |  |  | Pancake voltage
 |  |  | Hall Probe Voltage
Pancake
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 12: Pancake Properties
 | Pancake 1 | Pancake 2 | Pancake 3 | Pancake 4
Inner radius |  |  |  | 
Outer radius |  |  |  | 
Nb of turns |  |  |  | 
Mean thickness per tape |  |  |  | 
Inductance |  |  |  | 
 | Pancake 1 | Pancake 2 | Pancake 3 | Pancake 4
Inner radius |  |  |  | 
Outer radius |  |  |  | 
Nb of turns |  |  |  | 
Mean thickness per tape |  |  |  | 
Inductance |  |  |  | 
Tape IC map
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 13: Pancake Properties
Steady state study : ramp of 0.05A/s
Transient study: Steps at different current
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid
 | Pancake 1 | Pancake 2 | Pancake 3 | Pancake 4
Inner radius |  |  |  | 
Outer radius |  |  |  | 
Nb of turns |  |  |  | 
Mean thickness per tape |  |  |  | 
Inductance |  |  |  | 
 | Pancake 1 | Pancake 2 | Pancake 3 | Pancake 4
Inner radius |  |  |  | 
Outer radius |  |  |  | 
Nb of turns |  |  |  | 
Mean thickness per tape |  |  |  | 
Inductance |  |  |  | 

## Slide 14: Pancake Properties Transient Study
 | Charge | Discharge
5 A | 4.87 | 4.92
10 A | 4.70 | 5.05
20 A | 4.78 | 5.02
50 A | 4.60 | 4.83
 | Charge | Discharge
5 A | 4.87 | 4.92
10 A | 4.70 | 5.05
20 A | 4.78 | 5.02
50 A | 4.60 | 4.83
with
Pancake 1 | 5.2 | 10.1
Pancake 2 | 4.8 | 11.5
Pancake 3 | 1.6 | 43.5
Pancake 4 | 3.1 | 22.5
Pancake 1 | 5.2 | 10.1
Pancake 2 | 4.8 | 11.5
Pancake 3 | 1.6 | 43.5
Pancake 4 | 3.1 | 22.5
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 15: Pancake Properties Steady State Study
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 16: Pancake Properties Steady State Study
‘Maximum’ Field (mT) | Expected | Measured
Pancake 1 | 129 | 115 (89%)
Pancake 2 | 137 | 105 (77%)
Pancake 3 | 93 | 72 (77%)
Pancake 4 | 93 | 68 (73%)
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid
75 % of the expected maximum field

## Slide 17: Chemical Etching
Chemically (FeCl3 etching) remove both side of the tape to increase resistance
Magnetic stirrer
Ohmmeter
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 18: Chemical Etching
Stack 01
Program shut down for a few minutes
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 19: Chemical Etching
Stack 01
200
0.5
< 0.05
Resistance @77K increased by 4 order of magnitude after etching
What about IC ?
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 20: Chemical Etching
Stack 01
  Cu removed in ~30min
  Ag removed (?) in ~ 1h
Etching seems to have no effect on IC need to be determined
Further experiments required to confirm
N. Bykovskiy and al. 2019
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid
Two tapes soldered to each other

## Slide 21: Chemical Etching Pancake Properties
Stack 01
Pancake 1 | raw | 5.2 | 10.1
 | etched | 0.4 | 268
Pancake 2 | raw | 4.8 | 11.5
 | etched | < 0.04 | > 1384
Pancake 3 | raw | 1.6 | 43.5
 | etched | < 0.02 | > 3480
Pancake 4 | raw | 3.1 | 22.5
 | etched | < 0.02 | > 3480
Pancake 1 | raw | 5.2 | 10.1
 | etched | 0.4 | 268
Pancake 2 | raw | 4.8 | 11.5
 | etched | < 0.04 | > 1384
Pancake 3 | raw | 1.6 | 43.5
 | etched | < 0.02 | > 3480
Pancake 4 | raw | 3.1 | 22.5
 | etched | < 0.02 | > 3480
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid
Time constant decreased by a factor 100

## Slide 22: Chemical Etching Pancake Properties
Stack 01
‘Maximum’ Field (mT) | Measured | 
Pancake 1 129 | Non etched Etched | 115 (89%)
 |  | 98 (76%)
Pancake 2 137 | Non etched Etched | 105 (77%)
 |  | 104 (76%)
Pancake 3 93 | Non etched Etched | 72 (77%)
 |  | 50 (54%)
Pancake 4 93 | Non etched Etched | 68 (73%)
 |  | 52 (56%)
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid
- 15 % of from the non-etched maximum field

## Slide 23: Conclusion
Stack 01
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid
These conclusions can only be assessed for Theva TPL 4421 tapes :
IC of the tape degrades by less than 5% after 2h in solder bath
We have no control of current distribution in the pancake
  It is difficult to define a critical current for the pancake
  The magnetic field produced is about 25% lower than expected
Chemical etching increases the transverse resistance by about 4 order of magnitude and does not seem to affect IC
  Concerning the pancakes it reduces the time constant by at least a factor 100
  The magnetic field is reduced by another 15%
    It is not clear whether that is the effect of etching, or the presence of defects already here highlighted by the removal of the stabilizer
  Thermo-mechanical tests are needed to characterize the properties of an etched stack

## Slide 24: Conclusion
Stack 01
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid
On going work :
New winding tool has been machined and assembled for further pancake production (F. Sanda, A. Kolehmainen, A. Dudarev, A. Dallocchio)

## Slide 25: Conclusion
Stack 01
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid
On going work :
New winding tool has been machined and assembled for further pancake production (F. Sanda, A. Kolehmainen, A. Dudarev, A. Dallocchio
Problematic of the joints
  Tape to inner/outer ring
  Tape to outer ring
    Layer jump

## Slide 26
Thank you for your attention
M. Abdel Hafiz
& Cooling Solenoid working group

## Slide 27: Temperature influence on IC Preparing samples
Sample Holder
Sample holder :
G10 insulating plate (~ 1 mm)
Both sides :
  Cu coating (~75 )
  SnPb coating
  Extremity etched for clamping voltage tapes
Sample Preparation
Sample holder
Al blocs
Thermcouple
Heater
Heater
Sample preparation :
Screw Al blocs to sample holders
Heat up to 200°C to melt SnPb (~10 min)
Insert tape within groove (~ 1 min)
Wait for cooling down (~10 min)
Voltage tapes
Bloc and heaters @200°C for 25 minutes for test
Preparing sample does not degrade IC of measured length
Coating sample does not visibly affect IC
  @77K
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid
Sample cycled :
Preparing sample
IC measurement @ 77K
Heated in solder bath @200 °C
Cycling process

## Slide 28: Temperature influence on IC Experiment
Sample cycled :
Preparing sample
IC measurement @ 77K
Heated in solder bath @200 °C
Cycling process
Solder bath
Crack ?
Degadation of Theva TPL tape < 2% after 2h @200°C in SnPb bath
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 29: Pancake Properties
Critical Current (A) | Expected | Measured
Pancake 1 | 75 | 54
Pancake 2 | 72 | 86
Pancake 3 | 76 | 53
Pancake 4 | 76 | 143
M. Abdel Hafiz | Experimental tests for winding technology of Final Cooling Solenoid

## Slide 30: Etching effect on IC
Single tape
How much time needed to remove copper from side ?
  Lengthwise resistance measured in FeCl @ room temperature
  Length sink in FeCl solution ~10 cm
N. Bykovskiy and al. 2019
  Cu removed in ~30min
  Ag removed (?) in ~ 1h
IC measured @77K at the end of R measurements (~ 1h20)
Single tape still superconductive after removing Cu and Ag(?) (1h20) in FeCl
Further experiments required to confirm
According to N. Bykovskiy, depends on the tape
Degradation < 20%

## Slide 31: Mandrel
Mandrel thermal shrinkage be lower than tape
  Only lengthwise (tape) thermal shrinkage found
  Materials considered : Invar, Titanium, Niobium,
    Very low shrinkage
    High electrical resistivity ()
    Easy to coat with SnPb
Chart: Thermal Shrink
| 299.28449419999998 | 292.72781880000002 | 289.33798830000001 | 279.3952362 | 272.61557520000002 | 269.67847289999997 | 259.96246029999998 | 250.02271150000001 | 239.85772470000001 | 230.8249338 | 220.2117236 | 209.3740263 | 199.66927569999999 | 189.7400379 | 179.36107509999999 | 169.88831949999999 | 159.96658969999999 | 149.59513490000001 | 139.67715899999999 | 129.53995159999999 | 120.0799595 | 110.1724947 | 100.4955234 | 90.595566570000003 | 79.79465811 | 76.419843459999996
HTS | 0 | 0.00010229 | 0.00015518 | 0.00031017 | 0.00041585 | 0.00046159 | 0.00061266 | 0.00076654 | 0.00092311 | 0.0010611 | 0.0012218 | 0.001384 | 0.001527 | 0.0016708 | 0.0018181 | 0.0019494 | 0.0020831 | 0.0022185 | 0.0023434 | 0.0024653 | 0.0025738 | 0.0026811 | 0.002779 | 0.0028715 | 0.0029635 | 0.0029913
SuNAM | 0 | 9.3146e-05 | 0.00016014 | 0.00028928 | 0.00039874 | 0.00045696 | 0.00059868 | 0.00075438 | 0.00090963 | 0.0010535 | 0.001213 | 0.0013469 | 0.0014981 | 0.0016499 | 0.0017891 | 0.0019212 | 0.0020493 | 0.0021851 | 0.0023075 | 0.0024274 | 0.0025351 | 0.0026426 | 0.0027472 | 0.0028458 | 0.0029328
Fujikura | 0 | 8.5742e-05 | 0.00011643 | 0.00024315 | 0.0003226 | 0.00037951 | 0.00049744 | 0.0006246 | 0.00075172 | 0.00088187 | 0.0010058 | 0.0011348 | 0.0012623 | 0.0013817 | 0.0015022 | 0.0016286 | 0.0017358 | 0.0018476 | 0.0019577 | 0.0020637 | 0.0021646 | 0.0022583 | 0.0023466 | 0.0024289 | 0.0025044 | 0.0025262
SuperPower | 0 | 9.8959e-05 | 0.0001342 | 0.00028236 | 0.00037862 | 0.00043535 | 0.00059019 | 0.00072539 | 0.0008764 | 0.0010197 | 0.0011676 | 0.0013125 | 0.0014573 | 0.0015927 | 0.001727 | 0.0018511 | 0.0019796 | 0.0020948 | 0.0022033 | 0.0023174 | 0.0024191 | 0.0025146 | 0.0026174 | 0.0027122 | 0.0027953 | 0.0028275
Copper | 0 | 0.00015321 | 0.00030046 | 0.00062984 | 0.00098243 | 0.0014246 | 0.0017625 | 0.0020848 | 0.0023439 | 0.002564 | 0.0027252 | 0.0029257 | 0.0030234 | 0.0030964 | 0.0031634
Ti | 3.04e-07 | 0.00018796 | 0.000832 | 0.0014727
Hastelloy | 0 | 0.00039218 | 0.00051348 | 0.0005903 | 0.00078841 | 0.0010431 | 0.0012089 | 0.0014474 | 0.001593 | 0.0016819 | 0.0017709 | 0.0019245 | 0.0020499 | 0.0020863 | 0.0022358 | 0.0023976 | 0.002531 | 0.0026321 | 0.0027412 | 0.0028464 | 0.0029313 | 0.0030121 | 0.0032466 | 0.0032749 | 0.0032345 | 0.0032264 | 0.0032345 | 0.0032709
Invar | -6.1631e-06 | 2.8456e-06 | 1.352e-05 | 2.5747e-05 | 3.9414e-05 | 5.4409e-05 | 7.0618e-05 | 8.7928e-05 | 0.00010623 | 0.0001254 | 0.00014533 | 0.00016591 | 0.00018702 | 0.00020855 | 0.00023039 | 0.00025241 | 0.0002745 | 0.00029655 | 0.00031844 | 0.00034006 | 0.00036129 | 0.00038202 | 0.00040212 | 0.0004 | 0.0004 | 0.0004 | 0.0004 | 0.0004 | 0.0004 | 0.0004 | 0.0004

## Slide 32: Layout
Different areas in pancake
  Mandrel (invar)
  Copper/Hastelloy tape (inner)
  HTS tape inwards
  HTS tape outwards
  Copper/Hastelloy tape (outer)
Joints
  Connections should handle 200°C during winding
  Spot welding Hastelloy/Hastelloy and gluing copper/copper are retained methods
    Introducing local default
    Is it mechanically fragile ?
  These steps can all be done before winding ( not necessarally preferably )
Winding direction

## Slide 33: First turns
First turns with hastelloy/copper tape (without HTS)
  Redistributing stress
  Electrical connection
  Calculations to estimate n° of turns and acceptable stresses (?)
  Resistance ~ 0.1 per turn
Winding direction

## Slide 34: Inward tape joint
Winding direction
Welded spot

## Slide 35: HTS to HTS joint
Where to perform layer jump ?
  At the begining to save material in case of failling ?
  At lowest magnetic field location to reduce stresses ?
Can be glued
Resistance < 2 for 5 mm contact
Winding direction
Glued spot

## Slide 36: Outward tape joint
Winding direction
Welded spot

## Slide 37: Last turns
Last turns with hastelloy/copper tape (without HTS)
  Allow machining
    For a deviation of 10 per tape  1 mm per 100 turn
  Electrical connection
  Resistance ~ 0.2 per turn
End of the winding with bare hastelloy tape
  Removes the drop of solder
  See the two last pancakes
Winding direction

## Slide 38: Sum up
Welding to bare hastelloy tape to finish winding

## Slide 39: Homogeneity
Current flow quasi homogeneous in inner part
Current flow linearly decreases along the first turn
Current in
Last turn current flow
Current

## Slide 40: Homogeneity
Current flow quasi homogeneous in inner part
Current flow linearly increases along the first turn
Current in
Last turn current flow
Current
Current out
Last turn current flow
Current

## Slide 41: Homogeneity
Current in
Last turn current flow
Current
Current out
Last turn current flow
Current
Last turn current flow
Equivalent current in double pancake
Issue for field homogeneity ?
Acceptable tolerance ?

## Slide 42: Pancake 2 – Compare Time constant
Etching
  Parts protected with silicon coating
  Whole pancake drowned into iron chloride
  Cleaned into sodium becarbonate
  Dried with pressurized air
  Cleaned with acetone
  Cleaned with water
  Dried with pressurized air
 | Pancake 2 after etching |  |  | 
 | Charge | Discharge | Charge 2 | Discharge 2
5 A | 41.8 | 28.2 | 42.2 | 29.8
10 A | 40.6 | 51.4 |  | 
20 A | 30.4 | 43.1 |  | 
30 A | 36.4 | 40.7 | 34.1 | 41.1
40 A | 50.4 | 45.4 | 44.8 | 41.2
50 A | 51.8 | 50.5 |  | 
 | Pancake 2 after etching |  |  | 
 | Charge | Discharge | Charge 2 | Discharge 2
5 A | 41.8 | 28.2 | 42.2 | 29.8
10 A | 40.6 | 51.4 |  | 
20 A | 30.4 | 43.1 |  | 
30 A | 36.4 | 40.7 | 34.1 | 41.1
40 A | 50.4 | 45.4 | 44.8 | 41.2
50 A | 51.8 | 50.5 |  | 
 | Pancake 2 | 
 | Charge | Discharge
5 A | 4.87 | 4.92
10 A | 4.70 | 5.05
20 A | 4.78 | 5.02
50 A | 4.60 | 4.83
 | Pancake 2 | 
 | Charge | Discharge
5 A | 4.87 | 4.92
10 A | 4.70 | 5.05
20 A | 4.78 | 5.02
50 A | 4.60 | 4.83

## Slide 43: Last time presentation
 | Time Constant
Double Pancake | 4.6
Pancake A | 1.6
Pancake B | 3.1
Double Pancake | 4.6
Pancake A | 1.6
Pancake B | 3.1
Where do these differences come from ?

## Slide 44: Ansys simulation
Variation of central field within mm from center