## Slide 1: Bond Winding process & Impgregnation mold concept
N.Peray
26/02/2025

## Slide 2
Splice
Reaction mold
Splicing
Instrumentation
Impregnation mold

## Slide 3
Splice configuration
Nb3Sn
NbTi
Cu
(Lead stabilizer)
Cu
(splice cover)

## Slide 4
Splice
Reaction mold
Splicing
Instrumentation
Impregnation mold

## Slide 5
Reaction mold : Head spacer ?
Reaction mold base
Central post
Nb3Sn coil
Head spacer
At room temperature
Reaction mold base
Central post
Nb3Sn coil
Head spacer
During reaction cycle
Gap due to differential thermal expansion
With head spacer
Without head spacer

## Slide 6
Splice
Reaction mold
Splicing
Instrumentation
Impregnation mold

## Slide 7
Splicing tool
Insulating shims
Setting shim

## Slide 8
Splice
Reaction mold
Splicing
Instrumentation
Impregnation mold

## Slide 9
Instrumentation
V-Taps
Quench heater
Strain gages
Other ?
How many ?
Where?

## Slide 10
Splice
Reaction mold
Splicing
Instrumentation
Impregnation mold

## Slide 11
Impregnation needs :
To obtain a uniform stress at each interface, coils geometry should be the closest to perfection possible.
Due to the behavior of the cable during reaction, the position of the cable in the head cannot be fully guarantied.
Meaning that distance between cables and the pad in the head can vary and need to be filled for the final assembly.
Coil overlenght | Total shim thickness*
mm | mm
1 | 0.12
2 | 0.24
3 | 0.37
4 | 0.49
5 | 0.61
6 | 0.73
7 | 0.85
8 | 0.97
9 | 1.10
10 | 1.22
11 | 1.34
12 | 1.46
13 | 1.58
14 | 1.71
15 | 1.83
16 | 1.95
17 | 2.07
18 | 2.19
19 | 2.32
20 | 2.44
*Shim thickness to be split in two if equally spread at each end

## Slide 12
Option 1 : Filling the gaps before impregnation
Fiber glass or EP GC/GM
Seal web

## Slide 13
Option 2 : Adaptative mold
The gaps between the coil and the pad will need to be shimmed after impregnation
Custom spacer
Similar in some point to the technic used on TFD

## Slide 14
Option 3 : Impregnated pad
Machined after reaction to fit the coil overlength
Final pad
ESC Coil* or any filler
*If ESC coil, it needs to be fitted to the coil shape/overlength

## Slide 15
Thanks for your attention