## Slide 1
BOND 14T
Ceramic coatings
Ariel Haziot
February 25th, 2025

## Slide 2
Outline
Alumina plasma spray coating
  Used in 11T for headspacers
  Used at LBNL
Ceramic coating Armeco
  Applied on magnet parts at PSI
  In development at LBNL

## Slide 3
Plasma spray coating
Insulation of spacers for 11T:
  Al2O3 by plasma coating does not withstand the reaction (peels off)
  Vitreous Enamels: no R&D available
  Al2O3 by PVD coating gives promising results, currently under development with the Danish Technological Institute (DAI 7534740)
From 11T review
Did not go through at the end.
Explored again by C. Scheuerlein

## Slide 4
Plasma spray coating
Tests at LBNL:
Initial findings suggest that:
plasma sprayed surfaces have good potential when used in Nb3Sn coil fabrication
It has been shown to survive the heat treatment and cryogenic thermal cycles without detrimental effects.

## Slide 5
Outline
Plasma spray coating
  Used in 11T for headspacers
  Used at LBNL
Ceramic coating Armeco
  Applied on magnet parts at PSI
  In development at LBNL

## Slide 6
Ceramic coating - Armeco
ceramic coating on box channel
Various commercial ceramic coatings were testedas an alternative to line of sight coating methods
Aremco SGC4000-HT was chosen as a suitable coating
  temperature resistance to 760 °C, requires glazing at 720 °C
  40 V/μm dielectric breakdown strength
  simple dilution with alcohol (adjustable viscosity)
  suitable for spraying (fine particles), dip-coating
  good adhesion to stainless steel
  survives the reaction cycle
coating

## Slide 7
Ceramic coating - Armeco
https://www.aremco.com/wp-content/uploads/2018/05/A05_S1_18_Electrical.pdf

## Slide 8
Ceramic coating - Armeco
paraffin oil
electrode
electrode
stainless steel
coating
Layer thickness measured with a Testboy 70
Voltage applied with a Megger MIT515 in steps

## Slide 9
Ceramic coating - Armeco
layer thickness (μm) | breakdown voltage (V) | expected DBS value (V)
11 | 490 | 444
21 | 750 | 822
32 | 1160 | 1244
Aremco SGC4000-HT in paraffin oil
layer thickness (μm) | breakdown voltage (V)
93 | >5000*
65 | >5000*
BOX wax in paraffin oil
36-40 V/μm
>76 V/μm
150
8.2
* 5kV is the limit of the Megger MT515
(Freund 1982)

## Slide 10
Ceramic coating - Armeco
Comparison with other materials
Material | DBS (V/μm)
S2-Glass, AGY, RT | 13*
Stycast 2850FT + 23LV, RT | 14.8*
MY750, RT | 27.5*
BOX wax immersed, RT | >76
Aremco SGC-4000HT, RT | 36
*values from datasheet

## Slide 11
Ceramic coating - Armeco
deep channels, aspect ratio 1:2.5
even coating – controllable thickness
smooth finish possible with
additional water glass coat
used as secondary insulation in addition to the glass fiber

## Slide 12
Ceramic coating - Armeco

## Slide 13
Ceramic coating - Armeco