## Slide 1: 12T cosθ FALCOND dipole program – Mechanical mockup 2 (LMK 2 collared coil) March 11th, 2025
Sachin Gowrishankar, Arnaud Foussat, Nicola Sala on behalf of HFM WP3.1 team
Notes: Hello everyone, in the context of the 12T cos theta FALCOND program, today, I’ll present the work done on the mechanical mockup 2 (abbreviated as LMK 2), which is a collared coil mockup.

## Slide 2: Outline
Motivation & objectives of LMK 2
Details of LMK 2
Vertically & horizontally split yokes
Summary & next steps
Notes: The following is the outline of the presentation. First, I introduce the motivation & objectives of LMK 2. This is followed by the design details of the mockup. Then, we compare 2 yoke configurations of the same mockup – vertical & horizontal split. Finally, a summary of the work is given along with the next steps that are planned.

## Slide 3: Motivation for LMK 2
Utilize existing 11T Nb₃Sn coils, collars & shell; study stopper integration for future 12T FALCOND coils.
Validate aluminum stopper and welded shell on cosϴ collared aperture.
Explore a cost-effective design for 12T-13T long magnets.
Objectives
Compare horizontal vs. vertical yoke split, focusing on vertical due to 11T collar limitations.
Validate assembly with shell preload scaled to a 12T field-equivalent load (~ 3.5 MN/m).
Instrumented load test @ R.T & cold; benchmark coil and structure stress using FE models.
Reference 11 T model [2016-2021]
LMK 2 mockup [2024]
Shell
Coils
Collar pack
Weld
Yoke
Alu-stopper
Vertically split yokes
Notes: The motivation for LMK 2 is to use the existing 11T coils, collars & shell. Only modify the yoke to accommodate a mechanical stopper. Study the behavior of this new structure. Apply this knowledge to future 12T FALCOND coils. Validate the concept of aluminum stopper & welded shell on the cos theta collared aperture. Explore a potential cost-effective design for high field long magnets in the 12-13T range.

## Slide 4
Design description
Why aluminum stopper?
NOT overstress coils during assembly (shell welding) at R.T.
Maintain coil pre-stress at COLD
Geometry
= 60 mm
= 15 mm
= 600 mm
= 114 mm
= 15 mm
Design parameters
Yoke-collar gap (nominal = 0 mm).
Yoke-yoke half gap.
Yoke-stopper gap (= 0 mm always).
2. Yoke-yoke half gap
Parting plane
1. Yoke-collar gap
3. Yoke-stopper gap = 0 mm
Shim = 0.4 mm (nominal)
LMK 2 mockup [2024]
  (CTEalu = 4.2 mm/m).
Notes: The idea is NOT to pre-stress the coils too much when the shell halves are pressed and welded. In case the shell is loaded off the nominal load, the stopper takes the load and NOT the coils. Why specifically aluminum? – Has high CTE of 0.42%. At cold, alu shrinks and disappears. The strain energy stored in the shell at R.T is released to the coils through the structure. This helps to maintain the coil pre-stress at COLD.

## Slide 5
Reference 11T – FE model description
0 mm
Parting plane
0.1 mm
Key points
Bonded inner & outer coil layers.
Vertically split yokes.
Tapered yokes.
For all contacts,
= 0.6 mm
Yoke-collar gap = 0 mm (nominal).
Rigid - deformable contact: yoke-yoke
Symmetry: yoke & shell
Symmetry: collars & pole
Rigid-deformable contact: coil-ground
Material legend
Nb3Sn coils
Copper wedges
Iron yoke
Stainless steel shell, collars, pole
Material properties [11T, 2016-2021]
11T coils (Nb3Sn)
  E = 31 GPa, CTE = 3.88 mm/m.
Stainless steel 316LN (shell)
  E = 210 GPa, CTE = 2.84 mm/m.
  = 250 MPa.
Geometry
Contacts & B.C.s
Yoke-collar gap = 0 mm (nominal)

## Slide 6
Reference 11T – Results summary
Key
[Collaring]
[Spring back]
[Welding]
[Cool down]
4K
[Powering]
[MPa]
[COLD]
[POW]
Pole detaches here
R.T.

## Slide 7
LMK 2 mockup – FE model description
Parting plane
Key points
Bonded inner & outer coil layers.
Vertically split yokes.
Straight yokes.
For all contacts,
= 0.6 mm
Yoke-collar gap & yoke-yoke half gap are design parameters.
Material legend
Nb3Sn coils
Copper wedges
Iron yoke
Stainless steel shell, collars, pole
Material properties [11T, 2016-2021]
11T coils (Nb3Sn)
  E = 31 GPa, CTE = 3.88 mm/m.
Stainless steel 316LN (shell)
  E = 210 GPa, CTE = 2.84 mm/m.
  = 250 MPa.
Geometry
Contacts & B.C.s
Yoke-collar gap
Yoke-yoke half gap
Rigid - deformable contact: yoke-yoke
Symmetry: yoke & shell
Symmetry: collars & pole
Rigid-deformable contact: coil-ground
Aluminum (stopper): E = 70 GPa, CTE = 4.2 mm/m.

## Slide 8
Sensitivity of yoke-collar gap
For = 0.6 mm, yoke-yoke half gap = 0.2 mm, yoke-collar gap is varied from [0 mm – 0.3 mm].
Assembly @ R.T. (shell welding)
  As the gap increases, coil load decreases, stopper load increases, and reduced coil resistance causes the yokes to close, increasing yoke load.
Cold @ 4K
  For larger gaps, yokes close and DO NOT pre-stress the coils!
X
Y
Yoke-collar gap
= + +
Stopper disappears (CTE = 0.42%)
As a next, vary yoke-yoke half gap for yoke-collar gap = 0.15 mm.

## Slide 9
Sensitivity of yoke-yoke half gap
Parting plane
Yoke-stopper gap = 0 mm
Yoke-collar gap = 0.15 mm
Yoke-yoke half gap
For yoke-collar gap = 0.15 mm, yoke-yoke half gap was studied for [0.1 mm, 0.2 mm, 0.3 mm].
Important to maintain contact between collar & yoke @ COLD.
Pole detaches here
Yokes close too early here
10% contact

## Slide 10
Results for yoke-collar = 0.15 mm, yoke-yoke = 0.3 mm
2.3 MPa
(COLD – R.T.) is positive for LMK 2 and negative for reference 11T.
Pole-coil contact is higher for LMK 2 after assembly @ R.T.
Parting plane
0.3 mm
0.15 mm
0 MPa

## Slide 11
Results for yoke-collar = 0.15 mm, yoke-yoke = 0.3 mm
General stress state
Pole-coil contact
Shell
[MPa]
[MPa]
[POW]
[POW]
[POW]
[Pa]
[MPa]
[R.T.]
[R.T.]
[MPa]
10% contact
6 MPa

## Slide 12
Comparison with horizontal split yokes
= 0.6 mm
= 0.6 mm
[Pa]
[R.T.]
[R.T.]
Little contact
More contact
[Pa]
Yoke-collar = 0.15 mm, yoke-yoke = 0.3 mm
Yoke-collar = 0 mm (nominal), yoke-yoke = 0.2 mm
Vertical split
Horizontal split
X
Y
X
Y

## Slide 13
Comparison with horizontal split yokes
Lack of contact between yoke-collar (bottom) @ R.T. leads to less pre-stress at COLD.
(COLD – R.T.) of -25 MPa is seen for both horizontal split and for reference 11T.
2.3 MPa
1.7 MPa
0 MPa

## Slide 14
Summary & next steps
  Vertical split configuration seems a right candidate for LMK2 construction to validate the concept of minimized (COLD – R.T.) and protection of the coils @ R.T.
  The outcome of the study shows: for yoke-collar = 0.15 mm, yoke-yoke = 0.3 mm, (COLD – R.T.) = +5 MPa, with a 10% pole-coil contact @ POW.
  As a next step, to find an operating point where the residual pressure on pole-coil is larger.
  Horizontal split configuration seems less effective to implement on non-optimised 11T collars, although it gives reasonable results.

## Slide 15
APPENDIX

## Slide 16
Sensitivity of yoke-collar gap
Parting plane
Yoke-stopper gap = 0 mm
Yoke-collar gap
Yoke-yoke half gap = 0.2 mm
Pole detaches here
For gap = 0 mm (nominal), stress is too high at R.T. & COLD.

## Slide 17
[MPa]
Coil Peak Stress:
Results (Reference 11T model)

## Slide 18
[MPa]
General Stress State:
Results (Reference 11T model)