## Slide 1: In-situ SEY determination with the LHC Vacuum Pilot Sector and PyECLOUD
Quentin DUONG
TE – VSC – VSM
quentin.duong@cern.ch
01/07/2025
Dr. Vincent BAGLIN (CERN) CERN supervisor
Dr. Gaël SATTONNAY (IJCLab-Paris Saclay University) Doctoral supervisor

## Slide 2: Outline
Experimental description
Electron-cloud simulation with the PyECLOUD program
determination using the number of bunches at injection
TE – VSC – VSM

## Slide 3: Experimental Description
TE – VSC – VSM

## Slide 4: General VPS layout
TE – VSC – VSM
  Vacuum Pilot Sector (VPS)
  Location: close to LHCb
  2 beamlines physically separated
  Installed in 2015 in its latest version:
    1.4 m-long NEG coating
    1.4 m-long thick a-C coating ~500 nm
    1.4 m-long bulk Cu « New »
    1.4 m-long bulk Cu « Old » (installed in 2014)

## Slide 5: Electron cloud build-up
  Electron cloud = Primary + Secondary electrons
  Primary electrons:
    Photoelectrons induced by photoelectric effect
    Free electrons induced by residual gas ionisation (bunch, photons, or electrons induced)
TE – VSC – VSM
  Two main material properties for ecloud:
  Photoelectron Yield (PEY)

## Slide 6: Electron cloud build-up
  Electron cloud = Primary + Secondary electrons
  Primary electrons:
    Photoelectrons induced by photoelectric effect
    Free electrons induced by residual gas ionisation (bunch, photons, or electrons induced)
TE – VSC – VSM
  Two main material properties for ecloud:
  Photoelectron Yield (PEY)

## Slide 7: Electron cloud build-up
  Electron cloud = Primary + Secondary electrons
  Primary electrons:
    Photoelectrons induced by photoelectric effect
    Free electrons induced by residual gas ionisation (bunch, photons, or electrons induced)
  Secondary electrons: induced by primary electrons, accelerated by successive bunches, hitting the surface
TE – VSC – VSM
  Two main material properties for ecloud:
  Photoelectron Yield (PEY)
  Secondary Electron Yield (SEY, )

## Slide 8: Electron cloud build-up
  Electron cloud = Primary + Secondary electrons
  Primary electrons:
    Photoelectrons induced by photoelectric effect
    Free electrons induced by residual gas ionisation (bunch, photons, or electrons induced)
  Secondary electrons: induced by primary electrons, accelerated by successive bunches, hitting the surface
TE – VSC – VSM
  Two main material properties for ecloud:
  Photoelectron Yield (PEY)
  Secondary Electron Yield (SEY, )
  Two main material properties for gas desorption:
  Photon-Stimulated Desorption (PSD)
  Electron-Stimulated Desorption(ESD)

## Slide 9: Electron cloud build-up
  Electron cloud = Primary + Secondary electrons
  Primary electrons:
    Photoelectrons induced by photoelectric effect
    Free electrons induced by residual gas ionisation (bunch, photons, or electrons induced)
  Secondary electrons: induced by primary electrons, accelerated by successive bunches, hitting the surface
TE – VSC – VSM
  Two main material properties for ecloud:
  Photoelectron Yield (PEY)
  Secondary Electron Yield (SEY, )
  Two main material properties for gas desorption:
  Photon-Stimulated Desorption (PSD)
  Electron-Stimulated Desorption(ESD)

## Slide 10: Electron cloud build-up
  Electron cloud = Primary + Secondary electrons
  Primary electrons:
    Photoelectrons induced by photoelectric effect
    Free electrons induced by residual gas ionisation (bunch, photons, or electrons induced)
  Secondary electrons: induced by primary electrons, accelerated by successive bunches, hitting the surface
TE – VSC – VSM
  Two main material properties for ecloud:
  Photoelectron Yield (PEY)
  Secondary Electron Yield (SEY, )
  Two main material properties for gas desorption:
  Photon-Stimulated Desorption (PSD)
  Electron-Stimulated Desorption(ESD)
  Side effects observable with VPS: electron density & pressure rise, and heat load

## Slide 11: VPS instrumentation overview
TE – VSC – VSM
RGA
gas
  Total & partial pressure gauges
  Direct e-cloud measurement
  Electron currents
  Electron energy
  Indirect e-cloud measurement
  Pressure rise
  Temperature rise

## Slide 12: VPS instrumentation overview
TE – VSC – VSM
RGA
gas
  Total & partial pressure gauges
  Direct e-cloud measurement
  Electron currents
  For this presentation, only electron pickups are used.

## Slide 13: Electron cloud response of copper during injection
TE – VSC – VSM
Fill 8872 (04/06/2022, 13:42)
  At injection, the intensity seems to follow a linear evolution after a certain number of bunches are injected.

## Slide 14: Electron cloud response of copper during injection
TE – VSC – VSM
Fill 8872 (04/06/2022, 13:42)
  At injection, the intensity seems to follow a linear evolution after a certain number of bunches are injected.

## Slide 15: Electron cloud response of copper during injection
TE – VSC – VSM
Fill 8872 (04/06/2022, 13:42)
Linear
regime
Transitory
regime
Transitory
regime
Linear
regime
  At injection, the intensity seems to follow a linear evolution after a certain number of bunches are injected.

## Slide 16: Electron cloud response of copper during injection
TE – VSC – VSM
Fill 8872 (04/06/2022, 13:42)
  At injection, the intensity seems to follow a linear evolution after a certain number of bunches are injected.
  Two interesting parameters: linear coefficient
Linear
regime
Transitory
regime
Transitory
regime
Linear
regime

## Slide 17: Electron cloud response of copper during injection
TE – VSC – VSM
Fill 8872 (04/06/2022, 13:42)
  At injection, the intensity seems to follow a linear evolution after a certain number of bunches are injected.
  Two interesting parameters: linear coefficient and the linear regime threshold
Linear
regime
Transitory
regime
Transitory
regime
Linear
regime

## Slide 18: Electron cloud response of copper during injection
How do and change with ?
TE – VSC – VSM
Fill 8872 (04/06/2022, 13:42)
Linear
regime
Transitory
regime
Transitory
regime
Linear
regime

## Slide 19: Electron-cloud simulation with the PyECLOUD program
TE – VSC – VSM

## Slide 20: SEY curve modelisation
TE – VSC – VSM
  SEY = Reflected + True Secondary Electrons (TSE)
e-
Reflected e-
TSE
Beam pipe

## Slide 21: SEY curve modelisation
TE – VSC – VSM
  SEY = Reflected + True Secondary Electrons (TSE)
e-
Reflected e-
TSE
Beam pipe
define the decrease

## Slide 22: SEY curve modelisation
TE – VSC – VSM
  SEY = Reflected + True Secondary Electrons (TSE)
  TSE energy distribution modelled by a lognormal function:
e-
Reflected e-
TSE
Beam pipe
define the decrease
~mediane
~width

## Slide 23: PyECLOUD simulation principle
TE – VSC – VSM
Beam Intensity Estimation
Primary Electron Generation
Electric Field Computation
Macroparticle Motion
Secondary Electron Generation
p+
Beam pipe
Bunch
[G. Iadarola, ECLOUD’12, 2012]
  2D time-iterative electron density algorithm

## Slide 24: PyECLOUD simulation principle
TE – VSC – VSM
Beam Intensity Estimation
Primary Electron Generation
Electric Field Computation
Macroparticle Motion
Secondary Electron Generation
p+
Beam pipe
Ionisation electrons
Photo-electrons
e-
[G. Iadarola, ECLOUD’12, 2012]
  2D time-iterative electron density algorithm
(for Ebeam > 2 TeV)

## Slide 25: PyECLOUD simulation principle
TE – VSC – VSM
Beam Intensity Estimation
Primary Electron Generation
Electric Field Computation
Macroparticle Motion
Secondary Electron Generation
p+
Beam pipe
« Macroparticle »
Ionisation electrons
Photo-electrons
[G. Iadarola, ECLOUD’12, 2012]
  2D time-iterative electron density algorithm
(for Ebeam > 2 TeV)

## Slide 26
TE – VSC – VSM
Beam Intensity Estimation
Primary Electron Generation
Electric Field Computation
Macroparticle Motion
Secondary Electron Generation
p+
Beam pipe
[G. Iadarola, ECLOUD’12, 2012]
  2D time-iterative electron density algorithm
PyECLOUD simulation principle

## Slide 27: PyECLOUD simulation principle
TE – VSC – VSM
Beam Intensity Estimation
Primary Electron Generation
Electric Field Computation
Macroparticle Motion
Secondary Electron Generation
Beam pipe
[G. Iadarola, ECLOUD’12, 2012]
  2D time-iterative electron density algorithm

## Slide 28: PyECLOUD simulation principle
TE – VSC – VSM
Beam Intensity Estimation
Primary Electron Generation
Electric Field Computation
Macroparticle Motion
Secondary Electron Generation
Beam pipe
[G. Iadarola, ECLOUD’12, 2012]
  2D time-iterative electron density algorithm

## Slide 29: PyECLOUD simulation principle
TE – VSC – VSM
Beam Intensity Estimation
Primary Electron Generation
Electric Field Computation
Macroparticle Motion
Secondary Electron Generation
Beam pipe
[G. Iadarola, ECLOUD’12, 2012]
  2D time-iterative electron density algorithm

## Slide 30: PyECLOUD simulation principle
TE – VSC – VSM
Beam Intensity Estimation
Primary Electron Generation
Electric Field Computation
Macroparticle Motion
Secondary Electron Generation
Beam pipe
Secondary electrons
  2D time-iterative electron density algorithm
[G. Iadarola, ECLOUD’12, 2012]

## Slide 31: PyECLOUD simulation principle
TE – VSC – VSM
Beam Intensity Estimation
Primary Electron Generation
Electric Field Computation
Macroparticle Motion
Secondary Electron Generation
  2D time-iterative electron density algorithm
  Main results to extract:
  Energy distribution at the beam pipe wall
  Electron-cloud build-up at the nanosecond scale
  Electron-induced power deposition at the nanosecond scale
[G. Iadarola, ECLOUD’12, 2012]
Beam pipe
Secondary electrons

## Slide 32: determination using the number of bunches at injection
TE – VSC – VSM

## Slide 33: assessment methodology
Which parameter to use: and ?
Identify a filling pattern
Launch PyECLOUD computation for different
Identify which best matches the measurements
TE – VSC – VSM
At injection (450 GeV), there’s no photoelectron.
Electron-cloud = Electrons from gas ionisation + Secondary electrons

## Slide 34: Which parameter to use? Case of
TE – VSC – VSM

## Slide 35: Which parameter to use? Case of
TE – VSC – VSM

## Slide 36: Which parameter to use? Case of
TE – VSC – VSM

## Slide 37: Which parameter to use? Case of
TE – VSC – VSM

## Slide 38: Which parameter to use? Case of
TE – VSC – VSM
  is to be used to assess !

## Slide 39: Identify a filling pattern
TE – VSC – VSM
  For a same filling pattern, increasing the bunch population (from 1.35E11 to 1.50E11 protons per bunch) decreases .
  Lower can be observed!
ppb = protons per bunch

## Slide 40: Identify a filling pattern
TE – VSC – VSM
  For a same filling pattern, increasing the bunch population (from 1.35E11 to 1.50E11 protons per bunch) decreases .
  Lower can be observed!
  Filling patterns used to obtain the next results:
  > 1000 bunches
  > 1.05 x 1011 protons per bunch (ppb)
  Used many times in 2022
ppb = protons per bunch

## Slide 41: Launch PyECLOUD computation for different
TE – VSC – VSM
Bunches
Wall linear electron density
1 LHC revolution:

## Slide 42: Launch PyECLOUD computation for different
1 LHC revolution:
TE – VSC – VSM
Bunches
Wall linear electron density
Wall surface electron intensity
  The cumulative number of electrons divided by the beam revolution time and the pickup surface is computed to get the surface intensity as a function of the number of injected bunches.
beam pipe radius

## Slide 43: Identify which best matches
TE – VSC – VSM
bunches

## Slide 44: Identify which best matches
TE – VSC – VSM
bunches

## Slide 45: Identify which best matches
TE – VSC – VSM
bunches

## Slide 46: Identify which best matches
TE – VSC – VSM
bunches

## Slide 47: Identify which best matches
TE – VSC – VSM
bunches

## Slide 48: Identify which best matches
TE – VSC – VSM
bunches

## Slide 49: Identify which best matches
TE – VSC – VSM
bunches
  under ~1.16 cannot be assessed by this technique with this filling scheme.
limit

## Slide 50: SEY dose dependence after LS2 (long deconditioning time)
TE – VSC – VSM
  The conditioning effect can be illustrated by this assessment method.
  Both copper Stations exhibit the same conditioning trend, reaching = 1.3 within less than 1 mC/mm² and = 1.2 by the end of 2022.
  The NEG Station conditions faster and decreases below = 1.2.
  The of amorphous Carbon Station couldn’t be assessed as below the limit = 1.16.

## Slide 51: Conclusion
TE – VSC – VSM
  in-situ assessment is possible with VPS measurements and PyECLOUD simulations, provided conditions are fulfilled for electron-cloud build-up:
  Dense filling pattern
  Highly populated bunches
  High number of bunches
  Not too-low
  Small variations of bunch population and may lead to switch on/off the electron build-up:
  Increasing the bunch population allows lower investigation.
  Small deconditioning may lead to significant electron-cloud intensity increases.
  Surface conditioning could be observed during the year 2022:
  Copper could condition down to = 1.3 within less than 1 mC/mm²
  NEG conditioned faster than copper
  Amorphous Carbon couldn’t be assessed as under = 1.16