## Slide 1: Simulation of 3D sensors for 8” 3D project
G. Kramberger, Jožef Stefan Institute

## Slide 2: Small pitch narrow - column sensors (square cell)
IME capability – aspect ratio
30x30 mm2 cell
1.2 mm column
100 V, 1014 cm-3
30x30 mm2 cell
4 mm column
100 V, 1014 cm-3
|E| [V/mm]
|E| [V/mm]
Can we progress from “solid state ionization chamber” to semiconductor “wire proportional chamber”?

## Slide 3: Design of the sensor – full 3D simulation
Small square cell size detector was investigated - a single sided process assumed:
30x30 mm2
25x25 mm2
20 mm gap
1 mm column diameter
25/30 mm
20 mm
50 mm
25/30 mm
2R~1 mm
25/30 mm
1x1 and 2x2 cells were simulated
5e13 cm-3 doping levels
50 and100 V, -20oC
CFD~25% , shaping electronics with ~0.6 ns peaking time
n+
p+
p

## Slide 4: Potential distribution
5 mm from the top
25 mm from the top
5 mm from the bottom
Absolute value of the electric field
Absolute value of the potential
5 mm from the bottom
25 mm from the top
5 mm from the top
|E| [V/mm]
|E| [V/mm]
|E| [V/mm]
U [V]
U [V]
U [V]

## Slide 5: Potential and electric field simulation
XZ cross-section
The meshing of the sensor is important – otherwise non-realistic fields can be obtained
Note the high peak region close to the tip – a more realistic shape – rounded will be done soon
U [V]
U [V]
|E| [V/mm]
|E| [V/mm]

## Slide 6: Signal simulation
“Imaginary transfer function” – something that integrates as long as the drift takes – similar rise time as recent ASICs (e. g. ALTIROC)
Simulations show some, but not significant, dependence of ToA spread on the choice of the transfer function
Response to a “dirac” pulse
Holes
Electrons
Total

## Slide 7: Simulated drift paths
There is clear difference between the drift paths :
  those ending at the tip of the junction column will have a different gain due to different peak fields
  there will be an intrinsic difference in gain for tracks over the surface of the cell (different gain for different tracks – that can have an adverse effect on the timing )
How much is the distance between the back plane and the tip is a matter of optimization – break down voltage vs. gain difference vs. timing vs. the yield and processing.
Using a single cell in simulations has a “wrong” weighting field

## Slide 8: Simulation of half of the HL-LHC pixel cell - 25x25 mm2 cell
Neff=3e13 cm-3
Vbias=70 V
We get some gain, but not excessive (few times)
The gain is such that it compensates smaller signal
For thick sensors of small pitch there will be a lot of charge sharing – reducing the efficiency and time resolution
Thin small cell with gain would lead to superb performance
2R~1 mm
Uw=1
Uw=0
Thick sensor with large small pitch problem – charger sharing:
position resolution
reduction of efficiency
worse time resolution
larger data rate
Simulated volume – 50x50 mm2

## Slide 9: Simulation of the 25x25 mm2 cell
po1 2=-85.838394 (-39.406490, -46.431905)
pos 2=-62.629642 (-46.090750, -16.538891)
pos 3=-62.629642 (-46.090750, -16.538891)
pos 4=0.182072 (2.141266, -1.959194)

## Slide 10: Example of field calculation
Field calculations show that there should be charge multiplication at the junction columns
5 mm from the top
5 mm from the bottom
5 mm from the top
5 mm from the bottom
|E| [V/mm]
|E| [V/mm]
U [V]
U [V]

## Slide 11: Simulation of CC and ToA
Large dispersion of CC across the cell:
variation of the gain from 2 to 4
Variation of the ToA with CFD~25% of ~20 ps is larger that without it (distortion component alone) which is around 10 ps
ToA distribution
Collected charge distribution
~1 MIP is 3400 e
Q [e]
ToA [s]

## Slide 12: CC and ToA without diffusion
No diffusion
Q [e]
ToA [s]

## Slide 13: Hexagon

## Slide 14: Hexagon trench detectors
100x100x200 mm3
columns-6 mm, trench-4 6 mm
Neff=-2e12 cm-3
50V bias
A BNL design for gamma ray detector – proposed already in 2004 by Z. Li.
central collecting electrode is completely isolated by hexagon – no cross talk to neighbors
Very short:
  collection time
  full depletion voltage
Holes
Electrons
Total
n+ columns
p+ trench
p bulk

## Slide 15: Example of field calculation
This is in fact a 2D problem – no z dependence of potential/field
We will use 2D simulation to improve the details.
Next steps in simulations:
  not full through electrodes (processing details)
  narrow columns – devices with gain
|E| [V/mm]
U [V]

## Slide 16: ToA and Charge collection
ToA distribution spread 140 ps
Very homogenous charge collection efficiency
Very much as expected
Q [e]
ToA [s]
Q [e]

## Slide 17: Simulation verification – TPA comparison
Assumptions:
electronics with 500-600 ps peaking time
10 mm “cigar” shape of TPA in z
p-type isolation not yet implemented (no oxide charge)
Simulation bining 4x4 mm2
RMS measured 305 ps
RMS simulated 340 ps