## Slide 1
HTS current terminals design proposal
Giuseppe Scarantino,
Mahmoud Abdel Hafiz

## Slide 2: HTS current leads design
Cu clamps
IN Cu disk
13x pre-coated HTS tapes IN
13x pre-coated HTS tapes OUT
OUT Cu block
Cu clamp
G10 support cylinder
Coil support plate
Electrical contacts  low temperature solder (InSn). External tightening on the tape/Cu joints with bolted clamps.

## Slide 3: Coil support plate
Wedge-shaped element to place the HTS tapes in contact with the pancake.
0.2 mm gap to be filled with InSn solder.
External support.
0.2 mm gap to be filled with InSn solder.
CERN Polymer Lab recommended printing it in PEI ULTEM:
Melting temperature: 215 deg C.
Suitable for cryogenic applications.

## Slide 4: HTS leads inner support
TOP
BOTTOM
Hole to connect with the top Cu disk
20 mm hole, 15 mm deep to access the coil center for instrumentation.
Support element for Hall probe installation will be placed in this gap.
The HTS current leads will be placed along the cylinder. We want to avoid tape movements by mishandling the pancake and by screening currents induced stresses. On the other hand, we want to reduce thermal stresses during cooldown phase.
Possible solutions could be: - Kapton tape to place the leads around the cylinders; - add grooves on the cylinder to fit the tapes and use epoxy to impregnate them; - consider using a brass cylinder and solder the tapes there (?)

## Slide 5: Coil + Terminals Modelling (I)
Jc scaling tape from [1]: “Shanghai Superconductor Low Field High Temperature 2G HTS”.
NOTE: in self-field at 77 K  min. Ic = 219 A. From SST tape datasheet  260 A.
Assuming this tape performance  operational current (I_op): 55 A  15% minimum Ic margin.
Surface: Current Margin (I_op = 55 A)
Arrow Volume: Magnetic Flux Density
0.25 T center field
[1] University of Victoria Wellington, Robinson HTS critical current database, Shanghai Superconductor Low Field High Temperature 2G HTS data, 2021. [Online]. Available: https://htsdb.wimbush.eu
Coil hoop stress
(energization)

## Slide 6: Coil + Terminals Modelling (II)
To avoid quenches in the HTS terminals  number of terminals > 4.
Test with 7 HTS terminals in the IN/OUT part, respectively.
Assuming this tape performance  operational current (I_op): 55 A  15% minimum Ic margin.
Surface: Current Margin (I_op = 55 A)
Arrow Volume: Magnetic Flux Density
Stress concentration assuming fixed BCs
[1] University of Victoria Wellington, Robinson HTS critical current database, Shanghai Superconductor Low Field High Temperature 2G HTS data, 2021. [Online]. Available: https://htsdb.wimbush.eu
I_terminal = I_op/N_terminal
I_terminal = I_op/N_terminal*
 Assuming that 4 out of 7 terminals are not carrying any current.

## Slide 7: Equally spaced input current feeding
Are there any advantages?