## Slide 1
HTS current terminals design proposal
Giuseppe Scarantino,
Mahmoud Abdel Hafiz

## Slide 2: HTS current leads design (old)
Previous design based on ULTEM former with wedge-shaped ring for sliding the tapes in contact with the coil.
 complex solution, uncertainty on the quality of the soldering…

## Slide 3: *New* HTS current leads design
R. Unterrainer instrumentation plate design
3D printed pieces: PLA, ULTEM, PEEK
Easy to manufacture and install in the instrumentation plate

## Slide 4: *New* HTS current leads design
From first joint tests, understand it is important to apply pressure during soldering.
After soldering in a oven, remove the copper clamps and mount the coil + tapes to the 3D printed supports
8x HTS tapes IN / OUT
Mechanical contact to the Cu rings  pressure + Indium foil.

## Slide 5: Backup

## Slide 6: Non-uniformely distributed tapes