## Slide 1: Winding machine upgrade
R. Unterrainer
Final Cooling Solenoid

## Slide 2: Current Set Up

## Slide 3: Upgrade Plan
Pre-cleaning stage
  Copper Oxide Etching Bath
    Citric Acid/Sodiumpersulfate
    brushing
  Washing (deionized water)
  Drying + final cleaning
    Acetone/Isopropyl Alc.
    Brushing
New flux station
  Foam
  Spray
Wave solder / submerged pre-tinning

## Slide 4: Upgrade Plan
Pre-cleaning stage
  Copper Oxide Etching Bath
    Citric Acid/Sodiumpersulfate
    brushing
  Washing (deionized water)
  Drying + final cleaning
    Acetone/Isopropyl Alc.
    Brushing
New flux station
  Foam
  Spray
Wave solder / submerged pre-tinning
+ housing for N2/Ar/O2 atmosphere

## Slide 5: Upgrade Plan
Pre-cleaning stage
  Copper Oxide Etching Bath
    Citric Acid/Sodiumpersulfate
    brushing
  Washing (deionized water)
  Drying + final cleaning
    Acetone/Isopropyl Alc.
    Brushing
New flux station
  Foam
  Spray
Wave solder / submerged pre-tinning
Main topic of this meeting
+ housing for N2/Ar/O2 atmosphere

## Slide 6: What do we want to solder?
REBCO (rare earth barium copper oxide)
  Stainless steel/Hastelloy substrate
  Thin buffer layers
  1-5 mum of high temperature superconductor (HTS)
  Electrical stabilizer
    1-2 mum silver
    5-30 mum Cu finish
  Overall dimensions (LxWxH)
    Up to 1 km x 12/15 mm x 0.08 mm (80 mum)

## Slide 7: Wave Solder
Prerequisites
  “Small” setup/simple wave
  Homogeneous coating thickness on both sides
    Wave needs to have enough height
    Potentially thinking about adding additional surface finishing tech. (HASL/former)
  Coating tapes of up to 15 mm width (Wave height?)
  Multi-solder compatible (Titanium/Coatings? Which alloy)
  Good temperature control (>200 C destructive influence on tape)
  High throughput and low maintenance needs (easy solder dross removal)
  Minimalistic design (prototyp))

## Slide 8: Wave Solder
ej. height
Turn tape into vertical pos
Cleaning stages not drawn

## Slide 9: V3
Hot winding coils

## Slide 10: Seho

## Slide 11: Seho

## Slide 12: Seho

## Slide 13: Seho
No silicone!

## Slide 14: Seho
Flood gates
Almost no tin left
Thermal control

## Slide 15: Seho
Flood gates

## Slide 16: Microptik

## Slide 17: Microptik