## Slide 1: Sn-Pb thermal strain
4x90mm
4x60mm
CTE = 25 [um/(mºC)]
Thermal strain at 180ºC = 0.00395 :
4mm
4mm
1mm
4.018mm
1.0045mm
4.018mm

## Slide 2: Volume change behaviour during solidification of Sn-Pb alloy
4x90mm
From article : Predicted volume change behavior accompanying the solidification of binary alloys
Book : Metallurgical and Materials Transactions B
Solder we have: ISO-Tin S-Sn63Pb37E-DIN EN -> eutectique

## Slide 3: New pin with insulation

## Slide 4: New pin with insulation
CTE copolymer ~ 109 [um/mºC]
CTE stainless steel = 17.8 [um/mºC]

## Slide 5: Pre-compression with and without mandrel
2D simulation with mandrel of thickness 4.8[mm] bonded to the inner radius of the coil, offset with disk = -0.1mm
Disk going from 200ºC to 22ºC and coil, connectors and mandrel staying at 22ºC
In the case with the mandrel and the case when the mandrel is supressed the resulting hoop stress in the Ha tape of the coil is the same -> -102.48[Mpa]
When mandrel and coil are at 200ºC, pre-compression is higher in the coil
Mandrel and coil at 200ºC
Mandrel and coil at 22ºC

## Slide 6: Pre-compression and energization with and without mandrel
Without mandrel
Mandrel and coil are heated up to 200ºC
When energization happens mandrel is switched to «dead» status
Final hoop stress in the coil stays the same

## Slide 7: Pre-compression 150ºC with solder layer - update
Gap value linked to inconsistence in the hoop stress

## Slide 8: Pre-compression 150ºC with solder layer - update
REBCO shear strength ~ 10MPa ?
Sn-Pb solder alloy shear strength = 42.7MPa

## Slide 9: Pre-compression with solder layer - update
Gap 0.08mm

## Slide 10: Pre-compression with solder layer - update
Gap 0.02mm

## Slide 11: Pre-compression and energization with solder layer – gap 0.1mm
Without precompression
With precompression
Above limit !!
Above limit !!