## Slide 1: Cumulative stresses of REBCO tape during winding
03/10/2025

## Slide 2: The problem
Anticlastic curvature due to Poisson’s effect during bending
Courtesy G. Vernassa
Stresses due to:
Winding tension
Bending of the tape

## Slide 3: Content
Benchmark of FEM model with analytical results (G. Vernassa)
FEM modelling of cumulative stresses

## Slide 4: Model geometry and materials
material | total thick. / um | E / GPa | ν
Copper | 40 | 85 | 0.35
Hastelloy | 50 | 197 | 0.3
YBCO | 2.5 | 155 | 0.3
YBCO layer facing inwards

## Slide 5: Comulative stresses (longitudinal tension only)
Constant winding tension F=50N
*Cu mandrel with internal radius of 25mm and outer radius of 30mm
Benchmark data
(G. Vernassa)
COMSOL results

## Slide 6: Longitudinal stresses (no longitudinal tension – bending only)
12 mm tape
4 mm tape
Benchmark analytical calculation
(G. Vernassa)
COMSOL results
σ

## Slide 7: Longitudinal strain (no longitudinal tension – bending only)
12 mm tape
4 mm tape
Benchmark analytical calculation
(G. Vernassa)
COMSOL results
ε

## Slide 8: Radial displacement (no longitudinal tension – bending only)
12 mm tape
4 mm tape
Benchmark analytical calculation
(G. Vernassa)
COMSOL results

## Slide 9: Cumulative stresses
(bending and winding tension combined)

## Slide 10: Modelling approach
Model configuration:
Cubic elements
Contacts – initial configuration, no friction, penalty method
Only 3 material layers – Cu-Fe-Cu
Orthotropic properties for materials, so the activation scale factor only changes properties in azimuthal direction, keeping the tapes undeformed in the z-direction before activation
External radial strain when layer is activated:
,where - longitudinal strain from winding tension
- longitudinal strain from bending
- longitudinal strain to correct the change in radius
inactive layers
activated layers
;
, where – winding tension force
- Yung’s modulus of the material layer in tape
- area of the material layer in the tape
– radial coordinate in material frame
– neutral bending axis in material frame
- the radial displacement at the midpoint of previous tape, prior to the activation of the corresponding layer (state variable for this in COMSOL)
mandrel
Material activation in combination with external strain.

## Slide 11: Cumulative stresses (both longitudinal tension and bending)
4mm tape
Fe mandrel – ID 50mm, OD 60mm
50N longitudinal tension
No friction between tapes

## Slide 12: comparison (4mm tape)
z=1.5[mm]
z=0[mm]
Tension only
Tension + bending at the centre
Tension + bending 0.5mm from edge

## Slide 13: Cumulative stresses (both longitudinal tension and bending)
12mm tape
Fe mandrel – ID 50mm, OD 60mm
50N longitudinal tension
No friction between tapes

## Slide 14: comparison (12mm tape)
z=0[mm]
Tension only
Tension + bending at the centre

## Slide 15: Removal of the mandrel & radial precompression
To model the soldering of the tapes, the Adhesion contact condition is applied, which introduces adhesive elastic traction at the interface between the tapes.
The mandrel is gradually removed by reducing its diameter
Gradually 200MPa radial precompression applied at the outer winding boundary

## Slide 16: Cumulative stresses – removal of the mandrel
4mm tape
Might be a problem??
(only first <100 layers)

## Slide 17: Cumulative stresses – removal of the mandrel
12mm tape

## Slide 18: Radial precompression

## Slide 19: Cumulative stresses – radial precompression
200MPa radial precompression
4mm tape

## Slide 20: Cumulative stresses – radial precompression
200MPa radial precompression
12mm tape

## Slide 21: Hoop strain (in the superconductive layer, measured at the tape centre)

## Slide 22: Conclusions
~8 um max. curvature
Edges of the first 100 inner layers may be subjected to positive radial stress - (Max. ~15MPa for 4mm and ~10MPa for 12mm)
Anticlastic curvature effects are minimal; thus, the initial axial stress in the winding can be assumed constant for complete solenoid modelling.
Bending and tension changes the hoop strain distribution
Temperature effects currently not included (now )

## Slide 23: Thank you! :)