## Slide 1: Inner joints manufacturing
Jorge GUARDIA (EN-MME Main Workshop)
Muon Collider final cooling solenoid
07-11-2025

## Slide 2: Inner joints requirements
Transfer current between pancakes
Help thermal transfer with cooling fluid
Do not induce stress on pancakes (differential thermal expansion)
Easy to manufacture
Two possible materials:
Copper -> Excellent in all requirements, except for its too high thermal expansion coefficient
Superconducting tape
Two joining methods:
Soldering
Contact pressure
Pancake coil
Separator (to be defined)
Pancake coil
Inner joint
*Internal radial spring not depicted

## Slide 3: Copper joints: Reducing thermal stresses
Optimise copper thickness
Optimise geometry
  Remove material to lower rigidity of the copper foil
  → Chemical etching
Effect of porosity and pore size distribution on elastic modulus of foams
International Journal of Mechanical Sciences 261 (2024) https://doi.org/10.1016/j.ijmecsci.2023.108661

## Slide 4: Possible geometries, manufacturable with etching
High precision: For 0.2 mm thick copper foil, the minimum slot/hole size is ~0.3 mm
*Internal radial spring not depicted

## Slide 5: Conclusions
Consider copper chemical etching for the inner joints
Define minimum copper thickness required for the current
Define assembly method (solder/ contact pressure)
Define cooling channels requirements
Optimise the geometry with FEM simulations, keeping in mind fabrication and assembly constrains