## Slide 1
J. Ferradas Troitino & S. Izquierdo Bermudez,
5-m long block
Update on design
TE-MSC-LMF
March 2025

## Slide 2
Introduction
Updates and model checks
Rods design
2D Magnetic results
2D Mechanical results
2D Mechanical results – Bladders
2D Mechanical results – Str. limit
3D Mechanical results
Next steps
Outline

## Slide 3
Introduction
Updates and model checks
Rods design
2D Magnetic results
2D Mechanical results
2D Mechanical results – Bladders
2D Mechanical results – Str. limit
3D Mechanical results
Next steps
Outline

## Slide 4: Intro - Mechanical analysis
Figures of merit
Coil stresses
Coil contact pressure
Stress limits in the structure
Coil displacements
Coil strain
σVM < 120 MPa at RT
σVM < 150 MPa at cold
Roughly:
εz < 2000 µstr
Roughly:
All components below yield limits. We check S1 for brittle materials in first order
Try to maintain an average contact pressure > 5 MPa while respecting the stress limits
Check the coil displacements during powering

## Slide 5: 14 T Magnet design
Conductor parameters
40 strands x 0.85 mm – 5 mm smaller in width than BOND
14 T Conductor
Conductor parameters |  | L-BOND | BOND
Strand diameter | (mm) | 0.85 | 1.10
Layout |  | RRP 108/127 | RRP 162/169
Effective filament diameter | (µm) | 55 | 64
Jc at 4.2 K and 15 T , no self-field | (A/mm^2) | > 1280 | 1200
Cu/NonCu ratio |  | 1.2 | 0.9
No. of strands in cable |  | 40 | 40
Bare cable thickness | (mm) | 1.525 | 1.98
Bare cable width | (mm) | 18.150 | 23.045
Bare cable thickness (reacted - 4.5%) | (mm) | 1.594 | 2.06
Bare cable width (reacted - 1.2%) | (mm) | 18.363 | 23.275
Insulation thickness | (mm) | 0.15 | 0.15
Insulated cable width (reacted) | (mm) | 18.663 | 23.575
Insulated cable thickness (reacted) | (mm) | 1.894 | 2.36
Astrand | (mm2) | 0.567 | 0.950
Asc | (mm2) | 0.258 | 0.500
Acu | (mm2) | 0.310 | 0.450
Check | (mm2) | 0.567 | 0.950
ACTION ITEM: As soon as conceptual design is fixed, contact SCD for the cable (RMC-QXF)

## Slide 6: 14 T Magnet design
Magnet ID card
Name |  | 5m NO IRON | 5m | Bond_14T Single
 |  |  | OR = 225 | Baseline
Aperture | (mm) | 35 | 35 | 50
Field | (T) | 0.02 | 12.02 | 14.00
Field integral | (T m) |  |  | 15.10
Magnetic length | (m) |  | 0.00 | 1.08
Coil length | (m) |  |  | 1.31
Number of apertures | (adim) |  | 1 | 1
Distance between apertures | (mm) |  | - | -
Yoke outer diameter | (mm) |  | 450 | 540
Shell outer diameter | (mm) |  |  | 640
Cable data |  |  |  | 
Material |  | Nb3Sn | Nb3Sn | Nb3Sn
Process |  | RRP | RRP | RRP
No. strands | (adim) | 40 | 40 | 40
Strand diameter | (mm) | 0.850 | 0.850 | 1.100
Cu/NonCu | (adim) | 1.2 | 1.2 | 0.9
RRR | (adim) | 150 | 150 | 150
Bare cable thickness (R) | (mm) | 1.59 | 1.59 | 2.06
Bare cable width (R) | (mm) | 18.363 | 18.363 | 23.275
Insulation thick radial (5 Mpa) | (mm) | 0.150 | 0.150 | 0.150
Insulated cable surface | (mm2) | 35.35 | 35.35 | 55.64
Filling factor | (adim) | 0.292 | 0.292 | 0.360
Coil design |  |  |  | 
Insulated cable surface (one aperture) | (mm2) | 5514 | 5514 | 11572
Equivalent coil width | (mm) | 36.7 | 36.7 | 53.4
Coil efficiency | (T mm / A) | 0.00060 | 0.00073 | 0.00073
N. layers | (adim) | 2 | 2 | 2
N. turns/pole | (adim) | 39 | 39 | 52
Cable length/pole | (m) |  |  | 136
Operational parameters |  |  |  | 
Current (Inom) | (kA) | 0.035 | 15.800 | 20.005
Peak Field | (T) |  | 12.82 | 14.85
Bp/B0 |  |  | 1.067 | 1.061
Short sample current @ 1.9 K | (kA) |  | 19.627 | 24.199
Short sample current @ 4.5 K | (kA) |  | 17.496 | 21.602
Short sample field @ 1.9 K, Bp | (T) |  | 15.44 | 17.55
Short sample field @ 4.5 K, Bp | (T) |  | 13.98 | 15.93
j overall7 | (A/mm2) | 1 | 447 | 360
j strand | (A/mm2) |  | 696 | 526
j superconductor | (A/mm2) |  | 1531 | 1000
Loadline fraction @1.9 K | (%) |  | 80.50 | 82.7
Loadline fraction @4.5 K | (%) |  | 90.3 | 92.6
Stored energy/m | (MJ/m) |  | 0.382 | 1.031
Inductance/m | (mH/m) |  | 2.64 | 4.72
Stored energy | (MJ) |  | 0.00 | 1.35
 |  |  | Rref | Rref
Field quality |  |  | 11.67 | 16.67
Harmonic b2 @ Inom | (10-4) |  | 0.00 | 0.00
Harmonic b3 @ Inom | (10-4) |  | -0.18 | -3.49
Harmonic b4 @ Inom | (10-4) |  | 0.00 | 0.00
Harmonic b5 @ Inom | (10-4) |  | -0.45 | 2.78
Harmonic b7 @ Inom | (10-4) |  | 0.76 | 0.88
Protection |  |  |  | 
Coil energy density | (J/mm3) |  | 0.0692 | 0.0891
j copper | (A/mm2) |  | 1276 | 1111
Mechanics |  |  |  | 
Forces x | (MN/m) |  | 3.295 | 5.937
Forces y | (MN/m) |  | -1.362 | -2.680
Force z | (MN) |  | 0.382 | 0.958
Fx/2*Wcable | (MPa) |  | 88.3 | 125.9

## Slide 7
Slide from Ariel

## Slide 8
Introduction
Updates and model checks
Rods design
2D Magnetic results
2D Mechanical results
2D Mechanical results – Bladders
2D Mechanical results – Str. limit
3D Mechanical results
Next steps
Outline

## Slide 9: 2D Models
New version with the 40 strands MQXF cable
Based on the 14 T BOND model
Log (05/03/2025)
  Yoke outer radius chosen based on the bore field loss
  Vpad height sized to accommodate the flared end:
    75 mm from Y=0 to end of coil (preliminary) + 5 mm Vfiller + 25 mm margin (ESC leads, tooling holes, etc) = 106 mm → 110 mm
Zoom at midplane shim
225 mm
110 mm
Chart: B0 vs Ryoke
| 350 | 300 | 275 | 250 | 225 | 200
B0 | 12.1838 | 12.1811 | 12.1691 | 12.1309 | 12.0161 | 11.8401
Design | 11.5 | 12.5

## Slide 10: 2D Models
1 short vertical bladder
1x long vertical bladder + 1x short vertical bladder in the yoke
1 x long vertical bladder in Hpad

## Slide 11
2D Roxie magnetic model
44.976
50
57.323
110
59.948
R=20
R=225
R=17
X0: 42 Y0: 50.5
104.948
115
20
20
20
95

## Slide 12: 2D Models
33.198 mm
42.668 mm
19. 613 mm
19.738 mm
39.351 mm

## Slide 13: 2D Models
4 mm
17.5 mm
12.03 mm
59.948 mm
5.25 mm
39.351 mm
Ground insulation attributed to coil top and bottom.
Ground insulation around the shoe not modelled / included in the shoe (0.25 mm)

## Slide 14: 2D Models
110 mm
59.948 mm
45.024 mm
20 mm
Vertical SS filler = 5 mm
57.323 mm
65.024 mm
50 mm
95 mm
Th = 0.625 mm
44.976 mm

## Slide 15: 2D Models
20 mm
40 mm
20 mm

## Slide 16: 2D Models
D = 34 mm
X0 = 42 mm
Y0 = 157 mm
25 mm
114.948 mm
115 mm
225 mm
Yoke gap = 2.5 mm
20 mm
110 mm
Key th. = 5 mm
Key width = 20 mm
Vkey: X0 = 23.5 mm
Hkey: Y0 = 10 mm
Min Vkey X0 = 37mmm/2 (bladder physical length) + 1 mm assy. gap + 3 mm groove width + 1 mm gap = 23.5 mm
Min Hkey Y0 = 0 mm
No space for bladder at midplane due to coil size

## Slide 17: 2D Models
Yoke L = 110 mm
95 mm
3 mm thick bladder (nominal, to be verified) -> groove depth ~ 2 mm, groove indent width ~ 3 mm
3 mm
2 mm
3 short bladders:
3 x 39 mm (with 2 mm gap) + 4 x 3 mm (groove) = 129 mm
2 long bladders:
2 x 56 mm (with 2 mm gap) + 3 x 3 mm (groove) = 121 mm
2 short bladders:
2 x 39 mm (with 2 mm gap) + 3 x 3 mm (groove) = 87 mm
1 short +1 long bladders:
1 x 39 mm (with 2 mm gap) + 1 x 56 mm (with 2 mm gap)+ 3 x 3 mm (groove) = 104 mm
1 long bladder:
56 mm (with 2 mm gap) + 4 x 3 mm (groove) = 68 mm
Adding the key with 1 mm per side = 90 mm
We have 5 mm available space
Short bladders = 37 mm (34 mm active)
Long bladders = 54 mm (51 mm active)
For OR = 225 mm we can only put 2 short bladders (or 1 long+1short)

## Slide 18: 2D Models
10 mm
6.5 mm = 1.5 mm bladder physical + 1 mm gap + 3 mm groove width + 1 mm key gap
51 mm long active bladder
17 mm
½ short active bladder
6. 5 mm from end of active bladder to key. We need 6.5 mm, so we have 0 mm margin.
Bladder options
7.5 mm

## Slide 19: 2D Mechanical analysis – Mat. Props.
MQXF Model |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Coil |  |  |  | Stainless Steel |  |  |  | AlBr |  |  |  | Iron |  |  |  | Aluminum |  |  |  | G10 |  |  |  | Nitronic |  |  |  | Ti |  |  |  | HiMn Steel |  | 
 | 4.3 | 293 |  |  | 4.3 | 293 |  |  | 4.3 | 293 |  |  | 4.3 | 293 |  |  | 4.3 | 293 |  |  | 4.3 | 293 |  |  | 4.3 | 293 |  |  | 4.3 | 293 |  |  | 4.3 | 293
Ex | 20 | 20 |  | Ex | 210 | 193 |  | Ex | 120 | 110 |  | Ex | 224 | 213 |  | Ex | 79 | 70 |  | Ex | 30 | 30 |  | Ex | 225 | 210 |  | Ex | 130 | 130 |  | Ex | 210 | 193
Pr | 0.3 | 0.3 |  | Pr | 0.28 | 0.28 |  | Pr | 0.3 | 0.3 |  | Pr | 0.28 | 0.28 |  | Pr | 0.34 | 0.34 |  | Pr | 0.3 | 0.3 |  | Pr | 0.28 | 0.28 |  | Pr | 0.3 | 0.3 |  | Pr | 0.28 | 0.28
Alpx | 1.35E-05 |  |  | Alpx | 9.83E-06 |  |  | Alpx | 1.08E-05 |  |  | Alpx | 6.82E-06 |  |  | Alpx | 1.45E-05 |  |  | Alpx | 2.44E-05 |  |  | Alpx | 9.00E-06 |  |  | Alpx | 6.03E-06 |  |  | Alpx | 5.55E-06 | 
Th. Strain | 3.89E-03 |  |  | Th. Strain | 2.84E-03 |  |  | Th. Strain | 3.12E-03 |  |  | Th. Strain | 1.97E-03 |  |  | Th. Strain | 4.18E-03 |  |  | Alpy | 2.44E-05 |  |  | Th. Strain | 2.60E-03 |  |  | Th. Strain | 1.74E-03 |  |  | Th. Strain | 1.60E-03 | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Alpz | 8.34E-06 |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Th. Strain | 7.04E-03 |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Th. Strain | 7.04E-03 |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Th. Strain | 2.41E-03 |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 20: 2D Mechanical analysis – Stress criteria
RMM

## Slide 21
Introduction
Updates and model checks
Rods design
2D Magnetic results
2D Mechanical results
2D Mechanical results – Bladders
2D Mechanical results – Str. limit
3D Mechanical results
Next steps
Outline

## Slide 22: 2D Mechanical analysis
Aluminum |  |  |  |  |  | Stainless steel |  |  |  | 
Cryogenic temp. |  |  |  |  |  | Cryogenic temp. |  |  |  | 
σyield Al | 533 | MPa |  |  |  | σyield Al | 610 | MPa |  | 
Fz | 0.38 | MN | Per magnet end |  |  | Fz | 0.38 | MN | Per magnet end | 
Fz per rod | 0.19 | MN | Fz /4 |  |  | Fz per rod | 0.19 | MN | Fz /4 | 
0.7*σyield Al | 373.1 | MPa |  |  |  | 0.7*σyield Al | 427 | MPa |  | 
Aneeded | 511.659 | mm2 |  |  |  | Aneeded | 447.073 | mm2 |  | 
Rrod | 13 | mm |  |  |  | Rrod | 12 | mm |  | 
12 T = 4* D = 30 mm rods
Tie rods dimensioning:
Recall:
Stored energy/m | (MJ/m) | 0.38
ADD 3D ROXIE FORCES

## Slide 23: 2D Mechanical analysis
4* D = 37 mm rods

## Slide 24: 2D Models
Two type of axial displacements:
Relative movement of the coil with respect to the structure. It depends on the overall stiffness of the structure, i.e., independent of the level of axial pre-load in the ends.
Relative movement of the coil ends with respect to the pole. It depends on the level of pre-load.
Main Parameters Governing the Longitudinal Motions
Recall – For an element in tension/compression, stiffness (extensive property) decreases with the length.
  Keeping the same diameter, the rod stiffness is almost the same for (i) BOND in Al and (ii) L-BOND in SS.
  (Ess/EAl ~ 2.7 , Llong/Lshort = 5.5/2 ~ 2.75)
In the table, coil elongation with friction assumes only 5% of the total force acting.
In BOND (Al-rods, no friction) the rods carry 34% of the e.m. forces
G. Vallone, et. al., Mechanical Design Analysis of MQXFB, the 7.2 m long-β quadrupole for the High-Luminosity LHC Upgrade, IEEE Trans. Appl. Supercond., vol. 26, no. 4, 2016.
*Coil stiffness includes the coil block and Ti-pole (no wedge)
Parameter | Unit | BOND | L-BOND
e.m. Force Nominal Current | MN | 1.031 | 1.031
Coil Stiffness | MN/mm | 0.393 | 0.118
Rod radius | mm | 20 | 20
Rod area | mm2 | 1257 | 1257
Number of rods |  | 4 | 4
Al. Rod Stiffness | MN/mm | 0.20 | 0.07
SS. Rod Stiffness | MN/mm | 0.53 | 0.19
Coil Length | m | 1.50 | 5
Magnet Length | m | 2 | 5.5
Coil Elongation |  |  | 
No friction, no rods | mm | 2.627 | 8.755
No friction, Al. rods | mm | 1.744 | 5.428
No friction, SS. rods | mm | 1.120 | 3.329
Friction, Al. rods | mm | 0.087 | 0.271
Friction, SS. rods | mm | 0.056 | 0.166
TO BE UPDTED

## Slide 25: 2D Models
G. Vallone, et. al., Mechanical Design Analysis of MQXFB, the 7.2 m long-β quadrupole for the High-Luminosity LHC Upgrade, IEEE Trans. Appl. Supercond., vol. 26, no. 4, 2016.
Just for reference, MQXF values

## Slide 26
Introduction
Updates and model checks
Rods design
2D Magnetic results
2D Mechanical results
2D Mechanical results – Bladders
2D Mechanical results – Str. limit
3D Mechanical results
Next steps
Outline

## Slide 27: New 2D Magnetic results
Magnet |  | ROXIE | ANSYS
Current | [kA] | 15.8 | 15.8
Bpeak | [T] | 12.82 | 12.63
Bap | [T] | 12 | 12
Fx (quadrant) | [MN/m] | 3.295 | 3.24
Fy (quadrant) | [MN/m] | -1.362 | -1.353
Fx/CableW | [MPa] | 88 | 87
*ROXIE computation including self-field

## Slide 28: 2D Magnetic results

## Slide 29
Introduction
Updates and model checks
Rods design
2D Magnetic results
2D Mechanical results
2D Mechanical results – Bladders
2D Mechanical results – Str. limit
3D Mechanical results
Next steps
Outline

## Slide 30: 2D Mechanical analysis
Bonded coil components
Frictional contacts anywhere else (µ = 0.2)
  Including in between the midplane shim and the coil-pole-rail
Isotropic material properties (Annex)
Criteria
Use same modelling assumptions as MQXF, which we know well
Target similar coil peak stress limits at warm/cold as MQXF:
  RT below 110 - 120 MPa
  CD below 150 MPa
For reference, our MQXF reference preload gives in the model:
  RT peak azimuthal stress = 80 MPa
  CD peak azimuthal stress = 110 MPa
Gap = 100 µm
Merged areas: the two poles together and the two coil layers (removes contacts)
Side note – If instead of gluing the coil areas we put a contact, some sliding is allowed (based on contact stiffness) even if the contact is bonded. For last case, the upper layer can slightly slide and could be a bit more preloaded. Contact pressure at 12 T improves.

## Slide 31: 2D Mechanical analysis
Coil H&S Requirement #1: The conductor strain shall never exceed 500 microstrain (0.05%) in any part of the coils during any handling or shipping operation.
This requirement is based on the assumption that permanent degradation may occur above 2000 microstrain (0.2%) of applied tension at room temperature [1] and uses a safety margin of 4.

## Slide 32: 2D Mechanical analysis
Displacement sum
Horizontal displacement

## Slide 33: 2D Mechanical analysis
Peak at RT = 70 MPa
Peak at CD = 142 MPa
Peak at 14 T = 112 MPa
Transverse stress (Horizontal)
Contact pressure at 12 T

## Slide 34: 2D Mechanical analysis
Peak at RT = 65 MPa
Peak at CD = 142 MPa
Peak at 14 T = 106 MPa
VM Equivalent stress
Contact pressure at 12 T

## Slide 35: 2D Mechanical analysis
Total displacement
Difference in Usum (Powering – CD)
33 µm
75 µm

## Slide 36: 2D Mechanical analysis
Horizontal displacement
Difference in Ux (Powering – CD)
+ UX
8 µm
75 µm

## Slide 37: 2D Mechanical analysis
VM Equivalent stress
Peak at RT = 112 MPa
Peak at CD = 225 MPa

## Slide 38: 2D Mechanical analysis
VM Equivalent stress

## Slide 39: 2D Mechanical analysis
VM Equivalent stress

## Slide 40: 2D Mechanical analysis
VM Equivalent stress

## Slide 41: 2D Mechanical analysis
Mechanical structure behavior
 |  | 0 Deg | Avg.
Shell az. stress at RT 0 Deg | [MPa] | 56.3 | 23.5
Shell strain at RT 0 Deg | [µstr] | 804.9 | 
Shell az. stress at cold 0 Deg | [MPa] | 199.9 | 69.1
Shell strain at cold 0 Deg | [µstr] | 2530.6 | 
Step | σ_θ,shell 0° [Mpa] | σ_θ,shell 90° [Mpa] | σ_θ,shell 45° [Mpa] | Avg. σ_hor.,coil [Mpa] | Avg. σ_θ,shell [Mpa] | Coil Max Seqv [Mpa] | Coil Min Sx [Mpa] | F_hor.,pole [kN/m] | F_θ,shell [kN/m] | F_pole/F_e.m. [%]
After RT pre-load | 56 | 34 | 56 | -48 | 24 | 66 | -71 | 1848 | 1766 | 0.55
At 1.9 K | 200 | 130 | 169 | -82 | 69 | 142 | -142 | 3342 | 3891 | 1.20
Chart: Fx / F e.m.
| Keys | CD | Powering
Pole | 0.5704 | 1.0313 | 0.31968
Shell | 0.54509 | 1.2008 | 1.2205
Vpad+Vfiller+Pocket | -0.025316 | 0.16948 | -0.099156
Pole (frictionless) | 0.5159 | 1.2609 | 0.35125
Shell (frictionless) | 0.5159 | 1.261 | 1.3512
Vpad + Vfiller + Pocket (frictionless) | 0 | 0 | 0

## Slide 42
Introduction
Updates and model checks
Rods design
2D Magnetic results
2D Mechanical results
2D Mechanical results – Bladders
2D Mechanical results – Str. limit
3D Mechanical results
Next steps
Outline

## Slide 43: 2D Mechanical analysis
Same model, but now we simulate the bladder pumping.
We show results for the last horizontal bladder operation.
Bladder positioning:
  1 long + 1 short bladders in the split yoke (horizontally)
  One long bladder in the Hpad (per quadrant)
  Half short bladder in the vertical pad
Bladder pressure and opening:
  Vertically: 400Bar – 150 µm opening – 50 µm interference
    Clearance = 100 µm
  Horizontally: 300 Bar – 800 µm opening – 500 µm interference
    Clearance = 300 µm
Short bladders = 37 mm (34 mm active)
Long bladders = 54 mm (51 mm active)

## Slide 44: 2D Mechanical analysis
Displacement sum
Horizontal displacement

## Slide 45: 2D Mechanical analysis
Displacement sum (with bladders) – After loading
Displacement sum (without bladders) – After loading

## Slide 46: 2D Mechanical analysis
Peak at RT = 46 (70 prev.) MPa
Peak at CD = 142 MPa
Peak at 14 T = 112 MPa
Transverse stress (Horizontal)
Contact pressure at 12 T

## Slide 47: 2D Mechanical analysis
Peak at RT = 42 (65 prev.) MPa
Peak at CD = 142 MPa
Peak at 14 T = 105 MPa
Contact pressure at 12 T
VM Equivalent stress

## Slide 48: 2D Mechanical analysis
VM Equivalent stress
Peak at RT = 257 MPa
Peak at CD = 235 MPa

## Slide 49: 2D Mechanical analysis
VM Equivalent stress

## Slide 50: 2D Mechanical analysis
VM Equivalent stress

## Slide 51: 2D Mechanical analysis
VM Equivalent stress

## Slide 52: 2D Mechanical analysis
Mechanical structure behavior
Chart: Fx / F e.m.
| Keys | CD | Powering
Pole | 0.38691 | 1.0292 | 0.3174
Shell | 0.49134 | 1.1991 | 1.219
Vpad+Vfiller+Pocket | 0.10443 | 0.16994 | -0.09841

## Slide 53: 2D Mechanical analysis
No bladder simulation
With bladder simulation
Trivially, a frictionless bladder simulation gives the same result as the no bladder one (frictionless as well)
 |  | 0 Deg | Avg.
Shell az. stress at RT | [MPa] | 84.5 | 27.9
Shell strain at RT | [µstr] | 1207.2 | 
Shell az. stress at cold | [MPa] | 200.5 | 69
Shell strain at cold | [µstr] | 2537.4 | 
Chart: Fx / F e.m.
| Keys | CD | Powering
Pole | 0.38691 | 1.0292 | 0.3174
Shell | 0.49134 | 1.1991 | 1.219
Vpad+Vfiller+Pocket | 0.10443 | 0.16994 | -0.09841
Chart: Fx / F e.m.
| Keys | CD | Powering
Pole | 0.5704 | 1.0313 | 0.31968
Shell | 0.54509 | 1.2008 | 1.2205
Vpad+Vfiller+Pocket | -0.025316 | 0.16948 | -0.099156
Pole (frictionless) | 0.5159 | 1.2609 | 0.35125
Shell (frictionless) | 0.5159 | 1.261 | 1.3512
Vpad + Vfiller + Pocket (frictionless) | 0 | 0 | 0
 |  | 0 Deg | Avg.
Shell az. stress at RT 0 Deg | [MPa] | 56.3 | 23.5
Shell strain at RT 0 Deg | [µstr] | 804.9 | 
Shell az. stress at cold 0 Deg | [MPa] | 199.9 | 69.1
Shell strain at cold 0 Deg | [µstr] | 2530.6 | 

## Slide 54
Introduction
Updates and model checks
Rods design
2D Magnetic results
2D Mechanical results
2D Mechanical results – Bladders
2D Mechanical results – Str. limit
3D Mechanical results
Next steps
Outline

## Slide 55: 2D Mechanical analysis
Peak at RT = 125 MPa
Peak at CD = 184 MPa
Peak at 19.6 kA= 155 MPa
Transverse stress (Horizontal)
Contact pressure at 19.6 kA
We check the structure limit– focus on coil, brittle iron and shell (the other components have margin)
19.6 kA (14.4 T), 0.9 mm interference (0.6 previously), 500 Bar vertically, 450 bar horizontally

## Slide 56: 2D Mechanical analysis
Peak at RT = 120 MPa
Peak at CD = 182 MPa
Peak at 19.6 kA = 144 MPa
VM Equivalent stress
We check the structure limit– focus on coil, brittle iron and shell (the other components have margin)
19.6 kA (14.4 T), 0.9 mm interference (0.6 previously), 500 Bar vertically, 450 bar horizontally
Contact pressure at 19.6 kA

## Slide 57: 2D Mechanical analysis
VM Equivalent stress

## Slide 58: 2D Mechanical analysis
VM Equivalent stress

## Slide 59: 2D Mechanical analysis
VM Equivalent stress

## Slide 62
Thank you very much for your attention!

## Slide 65: MQXF Criteria
Pole-coil contact in pole-turns midpoint
pcont ≥ 2 MPa
Max bladder pressure
< 50 MPa
Bladder should open the interf=interfnom + 100μm
σeq coil max ≤ 150-200 MPa at
4.3K and 155 T/m
  ≤ 100 MPa at 293K
All components σ ≤ Rp 0.2
For iron at 4.3K (brittle)
σI ≤ ~200 MPa
Material | Rp 0.2 [MPa] | 
 | 293 K | 4.3 K
Al 7075 | 480 | 690
SS 316 LN | 286 | 930
NITRONIC 40 | 353 | 1240
MAGNETIL | 180 | 723
Ti 6Al 4V | 827 | 1654

## Slide 66: Material options for the pole
Material | 0.2 % YS RT (MPa) | Saturation (T) | Comments
430 Stainless Steel | 310 | 1.47 | * Structural steel, easy to find in the market
Magnetil | 180 | 2.18 | * LHC production
Armco | 180 | 2.15 | * HiLumi production
Co-Alloys |  |  | *Issue for radio protection
Fe-Ni alloy > 50 |  |  | 
Permalloy 45 |  |  | * The addition of Nickle improves the strength but decreases ductibility
AISIS 1010 Carbon Steel | 220-350 (305) | 2.05 | * Used in LHC experiments
Mumetal | 280 |  | 
Ti
armco
Ti
armco
ST430
Most promising options:

## Slide 67: 2D Mechanical analysis – Stress criteria