## Slide 1: Roberto Prieto García PhD. 4th meeting CERN-US
CERN, 28th March 2025

## Slide 2: DCB Results
28/03/2025
GIc for 0/0 interface before thermal treatment. Values found in literature point to GIc60 [J/m2]
Flexural modulus (back-calculated modulus) expected to be around 200 GPa according to TDS.

## Slide 3: DCB Results. Nonconformities.
28/03/2025
Precrack does not open until very high forces
Presence of high stiffness at the beginning of the test.

## Slide 4: DCB Results
28/03/2025
GIc for 0/0 interface after thermal treatment. There is an increment of GIc (), instead of a decrease as presented on previous studies.
Flexural modulus (back-calculated modulus) expected to be around 200 GPa according to TDS.

## Slide 5: DCB Results. Nonconformities.
28/03/2025
Precrack does not open until very high forces
No presence of high stiffness at the beginning of the test.

## Slide 6: DCB Results
28/03/2025
GIc for 0/0 interface after thermal treatment. There is an increment of GIc (), instead of a decrease as presented on previous studies.
Flexural modulus (back-calculated modulus) expected to be around 200 GPa according to TDS.

## Slide 7: DCB Results. Nonconformities.
28/03/2025
Precrack does not open until very high forces
No presence of high stiffness at the beginning of the test.