## Slide 1: Innovative bulge test setup for beam vacuum windows characterisation
Valentina Giovinco
M. Morrone, J.A. Ferreira, C. Garion
07/04/2024

## Slide 2
Introduction
Bulge test setup
Si3N4 membranes characterization
Bulge test setup enhancement for larger membranes
Ti-6Al-4V window dimensioning
Conclusions
Summary

## Slide 3
Introduction
Bulge test setup
Si3N4 membranes characterization
Bulge test setup enhancement for larger membranes
Ti-6Al-4V window dimensioning
Conclusions
Summary

## Slide 4
Absorbers and vacuum are alternated in the final cooling → Windows
Low energy beam: 20 to 5 MeV
    Thin windows (<15 µm to lose <1% of the energy)
    Small windows (10×RMS, RMS=0.6 mm at 5Hz)
Si3N4 windows
        Commercially available with a thickness < 1µm
        Bulk material has excellent mechanical properties
Introduction
Thin vacuum windows for the Muon Collider
Design of a beam window
Determination of the mechanical properties under operating conditions
Bulge test
@ T=77÷425 K, p=0÷8 bar

## Slide 5
Introduction
Bulge test setup
Si3N4 membranes characterization
Bulge test setup enhancement for larger membranes
Ti-6Al-4V window dimensioning
Conclusions
Summary

## Slide 6: Bulge test setup Experimental technique
d
Setup: sample fixed along the edges and uniformly pressurized from one side.
Measurement: maximum deflection of the membrane as a function of the applied pressure.
Objective: determine the mechanical properties of freestanding membranes.
Membrane
Stress /Strain state central section
Bulge equation
- )+
Plane-strain modulus
Initial residual stress
Poisson’s coefficient
Young’s modulus
[6, 7, 8]
Method: analytical models are available to post-process experimental data. The Vlassak method has been applied to study rectangular membranes (aspect ratio > 4:1).
Frame
Stress and strain

## Slide 7
Bulge test setup Mechanical assembly
Temperature control: the copper cylinder can be cooled or heated to change the temperature of the sample by conduction.
Helium injection: maintains pressure stability at T=77K by avoiding phase transition.
Leak tightness: ensured by Viton O-ring or flat gaskets.
1 | Steel flange for viewport connection
2 | Steel flange with integrated sapphire viewport
3 | Vacuum feedthrough
4 | Vacuum pump connection
5 | Steel flange with inner thread
6 | Viton gasket (x4)
7 | Copper flange with sample slot
8 | Cylindrical copper support
9 | Pressure cell

## Slide 8
Sample
COPPER FLANGE
Viewport
STEEL FLANGE
Bulge test setup Mechanical assembly
PT100 slots
STEEL FLANGE

## Slide 9: Bulge test setup Instrumentation
1. Optical sensor
2. Servomotor stage
He
3. Pressure control system
4. Piezo gauge
5. PT100s
INLET
VALVE
OUTLET
VALVE
Vacuum pump
DAQ developed and installed by Rodrigo Ferreira (TE-VSC)
Optical sensor (confocal chromatic): measures membrane deflection.
Servomotor stage: enable horizontal movement of the optical sensor to probe the membrane surface.
Pressure control system: regulates pressure during testing.
Piezo gauge sensor: measures applied pressure to the membrane.
PT100s: measure membrane and system components temperature.

## Slide 10
Bulge test setup Three temperature configurations

## Slide 11
Bulge test setup Sample mounting
Sample structure: a freestanding membrane supported by a silicon frame.
Sample mounting: bonding to a special slot created on the dedicated flange; it allows good repeatability of sample placement.
Sample orientation: two different ways to mount the membrane were investigated:
POSITIVE ORIENTATION
NEGATIVE ORIENTATION
Orientation | Adhesive | Temperature | Pressure @ failure
NEGATIVE | Acrylic glue (instantaneous) | RT | < 1 bar
POSITIVE | Acrylic glue (instantaneous) | RT | ~2 bars
Positive orientation prevents delamination phenomena.

## Slide 12
CREEP
STATIC
FATIGUE
FRACTURE TOUGHNESS
BULGE TEST SETUP: TESTS
Bulge test setup Capabilities
Irwin’s formula
Coffin-Manson (LCF):
Basquin (HCF):
Rectangular shape
Circular shape
σ1 > σ2 > σ3
T1 > T2 > T3
VM Stress

## Slide 13
Introduction
Bulge test setup: small membranes
Si3N4 membranes characterization
Bulge test setup: big membranes
Ti-6Al-4V window dimensioning
Conclusions
Summary

## Slide 14: Si3N4 membranes: bulge tests @RT Setup
Freestanding silicon nitride (Si3N4) membranes
Membrane dimension: 15 mm x 3 mm
Membrane thickness: 1000 nm
Frame dimension: 19 mm x 7 mm
Frame thickness: 200 µm
Membrane shape: rectangular
Testing temperature: Room Temperature (≈293K)
Number of sample tested: 5
Pressure load rate: 100 mbar/min
Adhesives: LOCTITE EA9492, 3M DP190, MG 832HT
Data post-processing: analytical procedure+FEM
Room temperature measurements setup
Helium bottle
DAQ system

## Slide 15: Si3N4 membranes: bulge tests @RT Initial condition
The initial deformation of the membrane must be evaluated (and compensated) before each cycle
A repeatable behavior of the membrane is measured after many cycles (Nmax=40)
The mechanical hysteresis measured by bulge tests is attributed to the glue, as demonstrated by FEM.
Adhesive=3M DP190
x1
x

## Slide 16: Si3N4 membranes: bulge tests @RT Material properties
Membrane properties: calculated from the pressure-deflection curve obtained using the LOCTITE EA9492 adhesive.
displacement @ p=250mbar
@ p=250mbar
Young’s modulus | E | 230±10 | GPa
Initial Residual Stress | σ0 | 10±5 | MPa
Poisson’s coefficient | ν | 0.1 | /
Ultimate pressure | pu | 3±1* | bar
Ultimate tensile stress | σxx,u | 2 ±0.4** | GPa
Adhesive=LOCTITE 9492
*Remember this is for rectangular membranes!
**Indirect measure from pu, under the hp of complete elastic material behaviour!

## Slide 17
Si3N4 membranes: bulge tests @CT
Setup
Freestanding silicon nitride (Si3N4) membranes
Membrane dimension: 15 mm x 3 mm
Membrane thickness: 1000 nm
Frame dimension: 19 mm x 7 mm
Frame thickness: 200 µm
Membrane shape: rectangular
Testing temperature: Cold Temperature (≈77K)
Number of sample tested: 4
Pressure load rate: 100 mbar/min
Adhesives: LOCTITE EA9492, 3M DP190
Data post-processing: analytical procedure+FEM
Cold temperature measurements setup
N2 Dewar
Helium bottle
DAQ system

## Slide 18: Si3N4 membranes: bulge tests @CT
Young’s modulus | E | 380±15 | GPa
Initial Residual Stress | σ0 | -850±30 | MPa
Poisson’s coefficient | ν | 0.1 | /
Ultimate pressure | pu | 5±1 | bar
Ultimate tensile stress | σxx,u | 3 ±0.4 | GPa

## Slide 19
Si3N4 membranes: bulge tests @HT
Membrane shape: rectangular
Testing temperature: Hot Temperature (=425K)
Number of sample tested: 3
Pressure load rate: 100 mbar/min
Adhesives: MG 832HT
Data post-processing: analytical procedure+FEM
Helium bottle
DAQ system
High temperature measurements setup
Membrane dimension: 15 mm x 3 mm
Membrane thickness: 1000 nm
Frame dimension: 19 mm x 7 mm
Frame thickness: 200 µm
Freestanding silicon nitride (Si3N4) membranes

## Slide 20: Si3N4 membranes: bulge tests @HT Material properties
FEM simulation: the flange+adhesive+sample system response during heating + bulge test is simulated to:
  1. Estimate the residual stress in the membrane after heating: simulation results match the experimental measurements.
σxx @T=150°C
Young’s modulus | E | 230±10 | GPa
Initial Residual Stress | σ0 | 230±20 | MPa
Poisson’s coefficient | ν | 0.1 | /
Ultimate pressure | pu | 2±0.5 | bar
Ultimate tensile stress | σxx,u | 1.5 ±0.2 | GPa
x
y

## Slide 21: Si3N4 membranes: bulge tests @HT Material properties
FEM simulation: the flange+adhesive+sample system response during heating + bulge test is simulated to:
  2. Estimate the Young’s modulus of the membrane determined by bulge test: simulation reveals that the experimentally measured lower membrane stiffness (E=180GPa) is an artifact due to the compliance of the rest of the system.
displacement @p=250mbar
x
y
Young’s modulus | E | 230±10 | GPa
Initial Residual Stress | σ0 | 230±20 | MPa
Poisson’s coefficient | ν | 0.1 | /
Ultimate pressure | pu | 2±0.5 | bar
Ultimate tensile stress | σxx,u | 1.5 ±0.2 | GPa

## Slide 22: Si3N4 membranes: three temperature summary Material properties
PARAMETER |  | THIN MEMBRANE |  |  | BULK | UNIT
 |  | 77 K | 293 K | 425 K | 293 K | 
Young’s modulus | E | 380±15 | 230±10 | 230±10 | 120÷241 | GPa
Initial Residual Stress | σ0 | -850±30 | 10±5 | 230±20 | / | MPa
Poisson’s coefficient | ν | 0.1 | 0.1 | 0.1 | 0.23÷0.28 | /
Ultimate pressure | pu | 5±1 | 3±1 | 2±0.5 | / | bar
Ultimate tensile stress | σxx,u | 3±0.4 | 2 ±0.4 | 1.5 ±0.2 | 0.06÷0.525 | GPa

## Slide 23: Si3N4 membranes: fatigue tests
 f =0.1 Hz
p
pm =500 mbar
Δp =1 bar
t =10 s
Membrane dimension: 15 mm x 3 mm
Membrane thickness: 1000 nm
Frame dimension: 19 mm x 7 mm
Frame thickness: 200 µm
Freestanding silicon nitride (Si3N4) membranes
PARAMETER | STATIC | DYNAMIC
Pressure rate, Δp/Δt | 1.6 mbar/s | 200 mbar/s
t
Membrane shape: rectangular
Testing temperature: Room and Cold Temperatures
Adhesives: LOCTITE EA9492
Software (miCon-L)
Pressure control system
OUTLET VALVE
INLET VALVE
PIEZO GAUGE

## Slide 24: Si3N4 membranes: fatigue tests @RT (f=0.1 Hz)
Si3N4 deforms purely elastically
Nmax=1.75E+04 cycles
Δp=1 bar, Emax(%) ≈15%
Δd=84 µm, Emax(%) ≈15%

## Slide 25: Si3N4 membranes: fatigue tests @RT (f=0.1 Hz)
Nmax=1.75E+04 cycles
Δp=1 bar, Emax(%) ≈15%
Δd=84 µm, Emax(%) ≈15%
The diagram of all cycles overlap extremely well
Si3N4 deforms purely elastically

## Slide 26: Si3N4 membranes: fatigue tests @RT (f=0.1 Hz)
Nmax=1.75E+04 cycles
Δp=1 bar, Emax(%) ≈15%
Δd=84 µm, Emax(%) ≈15%
The diagram of all cycles overlap extremely well
Si3N4 deforms purely elastically

## Slide 27: Si3N4 membranes: fatigue tests @RT (f=0.1 Hz)
Nmax=1.75E+04 cycles
Si3N4 deforms purely elastically
Δp=1 bar, Emax(%) ≈15%
Δd=84 µm, Emax(%) ≈15%
The diagram of all cycles overlap extremely well

## Slide 28: Si3N4 membranes: fatigue tests @RT (f=0.1 Hz)
Nmax=1.75E+04 cycles
Si3N4 deforms purely elastically
Δp=1 bar, Emax(%) ≈15%
Δd=84 µm, Emax(%) ≈15%
The diagram of all cycles overlap extremely well

## Slide 29: Si3N4 membranes: fatigue tests @RT (f=0.1 Hz)
Nmax=1.75E+04 cycles
Si3N4 deforms purely elastically
Δp=1 bar, Emax(%) ≈15%
Δd=84 µm, Emax(%) ≈15%
The diagram of all cycles overlap extremely well

## Slide 30: Si3N4 membranes: fatigue tests @RT (f=0.1 Hz)
Nmax=1.75E+04 cycles
Si3N4 deforms purely elastically
Δp=1 bar, Emax(%) ≈15%
Δd=84 µm, Emax(%) ≈15%
The diagram of all cycles overlap extremely well
Very good stability of the setup over long periods of time

## Slide 31: Si3N4 membranes: fatigue tests @CT (f=0.1 Hz)
Nmax=9.6E+02 cycles
Si3N4 deforms purely elastically
Δp=1 bar, Emax(%) ≈16%
Δd=65 µm, Emax(%) ≈30%

## Slide 32: Si3N4 membranes: fatigue tests @CT (f=0.1 Hz)
Nmax=9.6E+02 cycles
Si3N4 deforms purely elastically
Δp=1 bar, Emax(%) ≈16%
Δd=65 µm, Emax(%) ≈30%
The diagram of the displacement cycles oscillates due to system:
Thermal deformation (T=67÷77K)
Vibration (liquid N2 injection)

## Slide 33: Si3N4 membranes: fatigue tests @CT (f=0.1 Hz)
Nmax=9.6E+02 cycles
Si3N4 deforms purely elastically
Δp=1 bar, Emax(%) ≈16%
Δd=65 µm, Emax(%) ≈30%
The diagram of the displacement cycles oscillates due to system:
Limited number of cycles at cold to preserve instrumentations
Thermal deformation (T=67÷77K)
Vibration (liquid N2 injection)

## Slide 34
Introduction
Bulge test setup
Si3N4 membranes characterization
Bulge test setup enhancement for larger membranes
Ti-6Al-4V window dimensioning
Conclusions
Summary

## Slide 35: Bulge test setup enhancement for larger membranes Design of a new holder flange
DISK1
FLANGE
Socket head screw Ø6mm
DISK 2
CIRCULAR MEMBRANE
Different material and size of membranes can be tested:
A circular shape of membrane can be easily obtained.
The use of three pieces (flange + disks) allows to test different membrane apertures by only changing the disks (cheap and easy manufacture).

## Slide 36
Introduction
Bulge test setup
Si3N4 membranes characterization
Bulge test setup enhancement for larger membranes
Ti-6Al-4V window dimensioning
Conclusions
Summary

## Slide 37: Ti-6Al-4V window dimensioning A new window for the TT2-FTA line
Membrane aperture: from 44 mm to 65 mm
FE model: axisymmetric
            Experimental setup
            Technical reference drawing
Membrane thickness: from 50 µm to max 100 µm

## Slide 38: Ti-6Al-4V window dimensioning Exprimental tests
Bulge test: thickness=75 µm
Bulge test: thickness=100 µm
σ0=15MPa
d0=0.2mm
The FE model assumes ideal initial conditions (d0, σ0=0).
The analytical model considers real initial conditions.
The simulated curves closely match the experimental curves.
The FE model is accurate!
Fatigue test: thickness=75 µm

## Slide 39: Ti-6Al-4V window dimensioning FE simulation results
Effect of the thickness
A trade-off between mechanical properties and beam transparency of the material is represented by the 75 µm thick Ti-6Al-4V membrane.
Thickness=75 µm
Equivalent Von Mises Stress (MPa)
σVM,centre=281 MPa
σVM,max=876 MPa
σVM>800 MPa for less than 7% of the thickness
A thickness of 50 µm does not ensure membrane integrity during operation.
A thickness of 100 µm keeps the membrane well below the yield stress limit.
A thickness of 75 µm is slightly below the yield stress limit.

## Slide 40
Introduction
Bulge test setup
Si3N4 membranes characterization
Bulge test setup enhancement for larger membranes
Ti-6Al-4V window dimensioning
Conclusions
Summary

## Slide 41: Conclusions
Design, development and validation of a bulge test setup to test thin membranes at 77 K, 293 K and up to around 500 K.
Definition of the bulge test procedure for the characterisation of thin membranes at different temperatures by static and dynamic tests, including fatigue, creep and fracture toughness tests.
Characterisation of Si3N4 membranes at 77 K, 293 K and 425 in terms of determination of the mechanical properties and fatigue resistance of the membranes.
Characterization and testing of different types/size of membrane, including Ti-6Al-4V at 293 K.

## Slide 42
Thank you for your attention!

## Slide 43: Confocal chromatic sensor
A polychromatic light source illuminates the surface of the object.
The light is focused at different distances depending on the wavelength and only the light of a very narrow wavelength range is focused on the surface to be measured, with the remaining light concentrically distributed around this focus point onto a larger area.
By determining the wavelength of the focused light, which is reflected back into the optical system, very precise distance measurements are possible (nm resolution).

## Slide 44: Potential other applications of the bulge test setup Gasket profile
A
B
C
D
A
B
C
D
r (mm)
d (µm)
x
y
r
PROBLEM
Leakage in a vacuum system.
SOLUTION
The confocal chromatic sensor was used to trace the profile of a copper gasket and assess that the knife depth is within the tolerance range
Δdmax≈310 µm
Δdmax≈334 µm
Δdmax≈296 µm
Δdmax≈300 µm
Contact persons: Gregory Cattenoz and Marios Kyprianidis (TE-VSC)
NOMINAL CASE
Flange
DN600mm
Notes: .

## Slide 45: FEM simulations @HT Load and boundary conditions
Symmetry (along x)
Symmetry (along y)
Frictionless support
p
HEATING
BULGE TEST

## Slide 46: FEM simulations Material properties
COPPER
E=169 GPa
(constant with temperature)
SILICON
SILICON NITRIDE

## Slide 47: FEM simulations Material properties
GLUE: 3M DP190
GLUE: MG 832HT
E=4 GPa
(constant with temperature)

## Slide 48: Beam windows for final cooling
Absorbers (i.e., LH2, LiH) and vacuum are alternated in the final cooling  Windows
Low energy beam: 20 to 5 MeV
Thin windows (<15 µm to lose <1% of the energy)
Small windows (10×, =0.6 mm at 5Hz)
 |  | 5 MeV | 20 MeV
Be | Stopping power [MeV×cm²/g] | 11.2 | 4.0
 | Linear stopping power [MeV/cm] | 21 | 7.3
C | Stopping power [MeV×cm²/g] | 12.2 | 4.3
 | Linear stopping power [MeV/cm] | 25 | 8.7
Si3N4 | Stopping power [MeV×cm²/g] | 11.8 | 4
 | Linear stopping power [MeV/cm] | 37 | 13
SiC | Stopping power [MeV×cm²/g] | 11.2 | 4.0
 | Linear stopping power [MeV/cm] | 36 | 13
Possible material candidates  Be, C, Si3N4, SiC, …
Bethe-Bloch equation to calculate the stopping power at low energy (100keV to 100 MeV) [3]:

## Slide 49
According to simulations, the max displacement of the membrane @RT should be lower than @CT.
The diagram shows that due to the effect of the adhesive at high pressure (p>300mbar) simulated data deviates from the experimental curve @RT.
Experiments show that at Δp=1bar the max displacement of the membrane @RT is higher than @CT: this is confirmed by both static and dynamic tests.
Simulations vs experiments

## Slide 50
Bulge test setup Sample mounting
Before cooling
After cooling
Inspection performed by Ignacio Santillana (EN-MME)
OPTICAL MICROSCOPE IMAGES
Membrane failure during cooldown.
Possible causes and solutions:
  Substrate/sample thermal deformation mismatch:
    Increase the slot size of the copper flange
    Change the substrate material
  Glue degradation at cold:
    Test different glues
Adhesive=Araldite Rapid

## Slide 51
Bulge test setup Sample mounting
Before cooling
After cooling
OPTICAL MICROSCOPE IMAGES
Adhesive=Araldite Rapid
Membrane failure during cooldown.
Possible causes and solutions:
  Substrate/sample thermal deformation mismatch:
    Increase the slot size of the copper flange
    Change the substrate material
  Glue degradation at cold:
    Test different glues
INVAR disc (t=2 mm)
COPPER flange
Brazing performed by Alexandre Gerardin (EN-MME)

## Slide 52
Bulge test setup Sample mounting
Thermal efficiency ✓
Sample-flange contraction ✓
Thermal efficiency X
Sample-flange contraction ✓
Thermal efficiency ✓
Sample-flange contraction X
Copper flange
Invar flange
Invar-copper flange
Invar-copper flange designed to house the sample for low and high temperature measurements:
  CTEINVAR ≈ CTESi  Low thermal stress on the sample during heating/cooling
  High kCu Effective heating/cooling of the sample
FE simulation results: stationary flange temperature reached after the copper cylinder is fully in contact with liquid N2 (=77K)
ECu =130 GPa
kCu =400 W m-1 K-1
CTECu=16 ppm °C-1
EINVAR=140 GPa
kINVAR=15 W m-1 K-1
CTEINVAR=2.5 ppm °C-1

## Slide 53: Bulge test Adhesives for different temperature tests
Sample/substrate adhesion depends on:
  1. Substrate properties  SURFACE ENERGY TEST
    The higher the surface energy, the better the adhesion properties of the substrate
    Different materials/preparation surfaces have been tested
    Disperse and polar components have been determined for each surface similar components means better adhesion
SP: sand paper P: plasma cleaning O: oxidized
1
1
2
2
Tests performed by Vincent Schenk and Sebastien Clement (TE-MSC)

## Slide 54: Bulge test Adhesives for different temperature tests
Epoxy bi-component adhesives | Cure | Pressure @ failure |  | 
 |  | CT=77K | RT=293K | HT=420K
Araldite RAPID | 2h @RT | < 1bar | 5±1 bar | 1.5 bar *
Araldite STANDARD | 24h @RT | 1.5 bar | 5±1 bar | 1.5 bar *
STYCAST 2850FT CAT27 | 4h @120°C | Not tested | Not tested | 3.5 bar *
LOCTITE ABLESTIK 286 | 24h @RT | Not tested | Not tested | broken
3M DP190 | 24h @RT | 5±1 bar | 5±1 bar | broken
LOCTITE EA 9492 | 3dd @RT | 3±1 bar | 4±1 bar | broken
MG 832HT | 24h @RT | broken | 3±1 bar | 2 bar
*not repeatable because of the high deformation of the membrane during heating
ADHESIVE PERFORMANCE
Sample/substrate adhesion depends on:
  2. Adhesive properties  BULGE TESTS
    Adhesives affect the mechanical response of the membrane
    The adhesion quality has been defined by determining the maximum pressure at membrane failure
    Adhesives have been tested at different temperatures to evaluate high and low temperature resistance
1 bar≈0.5 kg/membrane
5 bar≈2.5 kg/membrane
15 mm
3 mm

## Slide 55: Si3N4 membranes: bulge tests @RT FEM vs ESPERIMENTS
Adhesive type: bi-component epoxy resin  LOCTITE EA9492, MG 832HT, 3M DP190
Adhesive effect: compensated by FEM  the adhesive+sample system response during bulge test is simulated to demonstrate and evaluate the influence of the adhesive on the measurement
 no influence of LOCTITE EA9492.
3M DP190, M E=180GPa
3M DP190, M E=230GPa
LOCTITE+M E=230GPa
ELOCTITE EA9492=6.7 GPa, t3M DP190 =0.2mm
E3M DP190u =0.5 GPa, t3M DP190 =0.2mm
Young’s modulus | LOCTITE 9492 | 230 | GPa
Young’s modulus | 3M DP190 | 180 | GPa