## Slide 1: Considerations of Q6 quench level
Arjan Verweij

## Slide 2
RQ6
8 circuits in the LHC: L3B1, L3B2, R3B1, R3B2, L7B1, L7B2, R7B1, R7B2
Each circuit contains 6 MQTLH magnets operated at 4.5 K with length=1.3 m and Iult=490 A
Lmag=0.12 H, Lcirc=0.72 H
Qstored, circuit=0.6 kJ (at 40 A), 86 kJ (at 490 A)
Circuit has EE (R=0.7 Ohm) and Rpar=0.2 Ohm over each magnet
Impregnated coil wound from ‘wire 3’ (bare: 1.13 mx0.6 mm, 60 mm PVA enamel coating, Cu/SC=1.75)
PS: Note that all multi-kA magnets are wound from a Rutherford cable (22 to 46 strands)

## Slide 3
Question from Anton:
Do you remember why the MQTL quench levels are so much lower than the MQY and MQM ones?
Unfortunately I cannot run the QP3 code anymore, but could be foreseen if needed.

## Slide 4
Minimum Quench Energy (MQE) is governed by the enthalpy margin between 4.5 K and the current sharing temperature (TCS).
At injection, TCS is the same for all magnets (about 9 K) as well as Cu/SC ratio, so the MQE is very similar.
Short heat deposition
(up to 1 ms)
Injection
Nominal
At nominal, the MQTL operates with higher margin (so higher TCS) so the MQE is higher.

## Slide 5
Minimum Quench Power (MQP) is governed by the cooling from the coil to the helium bath.
The QP3 model predicts that the cooling is better for the MQY and MQM due to the helium channels in the insulation and the wider conductor (causing and averaging effect for heating and TCS, due to very good heat diffusion inside the conductor).
Long heat deposition
(above 2 s)
Injection
Nominal

## Slide 6
Minimum Quench Energy (MQE) is given by the combined effect of enthalpy of the conductor, enthalpy of the helium inside the cable (for MQM and MQY), averaging advantages (for MQM and MQY) and cooling.
Intermediate heat deposition (1 ms to 2 s)
Injection
Nominal

## Slide 7
We have no experimental data of the MQE for the MQTL. The theoretically calculated MQE is correct for short durations (<1 ms) but might be quite wrong for intermediate and long durations.
It is very likely that the MQE of the 8x6 magnets in the LHC are rather similar (within 25%).
Quench tests can be safely done for the MQTL when operated at low current (<50 A).
I suggest starting with an energy power deposition equal to the calculated theoretical value and, if no quench is observed, increase the power in steps of maximum a factor 2.
Once a quench is observed you might of course, if needed, add intermediate powers to improve the accuracy.
Some remarks