## Slide 1: EODU, Mixers and Plans for 2012
B. Baumbaugh, C. Broughton, C. Burke, J. Conti, K. Daily, J. Freeman, A. Heering, D. Karmgard,
S. Los, J. Marchant, M. O’Brien, P. Rose, R. Ruchti,
I. Schmidt, J. Taylor, M. Vigneault

## Slide 2: Mixer Study Objectives
High light transmission
Uniformity of distribution of illumination
Light reduction per photo element

## Slide 3: Mixers - 1
Mixer formats
  Single structures
    Varying cross sections, materials and properties
  Multi-element structures
    Use in HO and HB ODU
    Intention is to expand application to HE ODU

## Slide 4: Mixers - 2
Single structures
  Cores
  Aperture surface preparations
  Thicknesses
  End finishing

## Slide 5: Mixers - 3
Test Setups
  1. CCD imaging
      Uniformity studies
      Pulseheight histogramming technique
  2. P/N diode current sensing
      Transmission measurement
  3. Beam tests

## Slide 6: HO Mixers

## Slide 7: Test Station for Current Measurements

## Slide 8: Current Measurements

## Slide 10: Test Station for CCD Imaging

## Slide 11: CCD Testing

## Slide 12: CCD Imaging

## Slide 13: Mixer characterization – on the right track

## Slide 14: Mixer Characterization – illustrating problems…

## Slide 15: Mixer Characterization - recent

## Slide 16: HO Mixers – Current Studies
Chart: 
| 0.0 | 0.0 | 1.0 | 2.0 | 3.0 | 4.0 | 5.0
row 4-1 | 1 | 0.91579 | 0.90526 | 0.88947 | 0.87368 | 0.84737 | 0.81053
row 4-2 | 1 | 0.9 | 0.88421 | 0.85789 | 0.83684 | 0.80526 | 0.75263
row 4-3 | 1 | 0.91053 | 0.9 | 0.88947 | 0.87368 | 0.85789 | 0.83158
row 4-4 | 1 | 0.91579 | 0.91053 | 0.9 | 0.88421 | 0.86842 | 0.83684
row 3-3 | 1 | 0.91579 | 0.90526 | 0.88947 | 0.87895 | 0.86842 | 0.85263
row 3-4 | 1 | 0.91053 | 0.90526 | 0.89474 | 0.88421 | 0.85789 | 0.83684
row 4-1 | 1 | 0.91579 | 0.89474 | 0.88421 | 0.86842 | 0.84737 | 0.82105
row 4-2 | 1 | 0.90355 | 0.88832 | 0.8731 | 0.83249 | 0.7868 | 0.72081
row 4-3 | 1 | 0.90355 | 0.88832 | 0.8731 | 0.84264 | 0.81218 | 0.77665
row 4-4 | 1
row 5-1 | 1
row 5-2 | 1
Row 1
Row 2
Row 3
Row 4
Row 5
- 1
- 2
- 3
Row 2 - 4

## Slide 17: Transmission measurements

## Slide 18: HO Mixer Disks
C1: 4/5 mm thick, 4mm dia
A.HO.0.01Al4, e, b, j 78%
A.HO.0.04Al5, e, b, j 77%
D.HO.0.01 Delrin4, e, b, j 78%
D.HO.0.04 Delrin5, e, b, j 78%
C1: 4mm thick 4mm dia
D.HO.0.02 Delrin, e, b, P3 82%
D.HO.0.03 Delrin, e, b, P3 85%

## Slide 19: HO Mixer Disks
SGS: 4/5 mm thick, 3.25mm dia
D.HO.1*2.01 Delrin4, b, P3 84%
D.HO.1*2.02 Delrin4, b, P3 84%
D.HO.1*2.03 Delrin4, b, P3 81%
D.HO.1*2.04 Delrin5, b, j 77%
A.HO.1*2.04 Al5, bond, j 82%

## Slide 20: HB Structure

## Slide 21: HB Structure

## Slide 22: HB Mixer Plates
SGS, 4/5mm thick, 3.25mm dia
A.HB.11 Al4, bond, P3 89%
A.HB.12 Al4, bond, P3 89%
A.HB.13 Al4, bond, P3 89%
A.HB.14 Al4, bond, P3 87%
A.HB.15 Al4, bond, P3 89%
A.HB.05 Al5, bond, j 82%

## Slide 23: Lessons learned…
Square cross sections are better avoided – machining and surface issues; corners…
Cylindrical thick-clad fiber mixers have good characteristics…
  Excellent surface properties
  Thick cladding keeps light away from support/mounting structure
  Excellent light transmission
  Challenges – dimensional tolerances and bonding
Would be good to have SiPM of circular shape to match the cylindrical mixers

## Slide 24: Cross section issues…

## Slide 25: HE RBX

## Slide 26: HE RBX

## Slide 27: HE RM

## Slide 28: HE RM

## Slide 29: A possible approach to HE RBX

## Slide 30: Thoughts for 2012/2013
Redesign the HE RBX – working prototype in 18 months (summer 2013)
  RM
    Four QIE cards (12 channel)
    One control card
    Compatibility with HB and HE – goal to use same cards
Built RM for H2 beam tests for summer/fall 2012
    These would be existing RM, but HPD replaced by SiPM
    For studying depth sampling in HE
    Make a full complement (4) of HE/RM with SiPM readout