## Slide 1: Test Plan – New Interlayer Materials
Javier Osuna – TE-MSC-SMT

## Slide 2: Interlayer Study in 2023 (Slide by R.Piccin)

## Slide 3: New Interlayer Materials
Silicate 600
>94% SiO2, <4% Al2O3
0.6 mm thick
600 g/m2
Satin 1/7 Weave
Silicate 1100
>94% SiO2, <4% Al2O3
1 mm thick
1100 g/m2
Satin 1/7 Weave
Ceramic 135
28% SiO2, 72% Al2O3
0.21 mm thick
135 g/m2
«Toile» (Satin) Weave
S2-Glass 493
65% SiO2 , 25% Al2O3, 10% MgO
0.25, 0.175 mm thick
258, 212 g/m2
Plain Weave

## Slide 4: New Interlayer Materials
Silicate 600
>94% SiO2, <4% Al2O3
0.6 mm thick
600 g/m2
Satin 1/7 Weave
Silicate 1100
>94% SiO2, <4% Al2O3
1 mm thick
1100 g/m2
Satin 1/7 Weave
Ceramic 135
28% SiO2, 72% Al2O3
0.21 mm thick
135 g/m2
«Toile» (Satin) Weave
S2-Glass
65% SiO2 , 25% Al2O3, 10% MgO
0.25, 0.175 mm thick
258, 212 g/m2
Plain Weave

## Slide 5: New Interlayer Materials
Silicate 600
>94% SiO2, <4% Al2O3
0.6 mm thick
600 g/m2
Satin 1/7 Weave
Silicate 1100
>94% SiO2, <4% Al2O3
1 mm thick
1100 g/m2
Satin 1/7 Weave
Ceramic 135
28% SiO2, 72% Al2O3
0.21 mm thick
135 g/m2
«Toile» (Satin) Weave
S2-Glass
65% SiO2 , 25% Al2O3, 10% MgO
0.25, 0.175 mm thick
258, 212 g/m2
Plain Weave

## Slide 6: New Interlayer Materials
Silicate 600
>94% SiO2, <4% Al2O3
0.6 mm thick
600 g/m2
Satin 1/7 Weave
Silicate 1100
>94% SiO2, <4% Al2O3
1 mm thick
1100 g/m2
Satin 1/7 Weave
Ceramic 135
28% SiO2, 72% Al2O3
0.21 mm thick
135 g/m2
«Toile» (Satin) Weave
S2-Glass
65% SiO2 , 25% Al2O3, 10% MgO
0.25, 0.175 mm thick
258, 212 g/m2
Plain Weave

## Slide 7: New Interlayer Materials
Silicate 600
>94% SiO2, <4% Al2O3
0.6 mm thick
600 g/m2
Satin 1/7 Weave
Silicate 1100
>94% SiO2, <4% Al2O3
1 mm thick
1100 g/m2
Satin 1/7 Weave
Ceramic 135
28% SiO2, 72% Al2O3
0.21 mm thick
135 g/m2
«Toile» (Satin) Weave
S2-Glass
65% SiO2 , 25% Al2O3, 10% MgO
0.25, 0.175 mm thick
258, 212 g/m2
Plain Weave

## Slide 8: About the Silicate/Ceramic Fibres

## Slide 9: New Binder Material
Resbond Binder
Ethylene Glycol + Al2O3 particles
24h RT Curing or 4h at 65 °C
CTD1202
Cyclosiloxanes + Polymethylsiloxane
Initial Cure 1h 80 °C
Post Cure 2h 150 °C
Heat Treat >550 °C

## Slide 10: New Binder Material
Resbond Binder
Ethylene Glycol + Al2O3 particles
24h RT Curing or 4h at 65 °C
CTD1202
Cyclosiloxanes + Polymethylsiloxane
Initial Cure 1h 80 °C
Post Cure 2h 150 °C
Heat Treat >550 °C

## Slide 11: New Binder Material
Resbond Binder
Ethylene Glycol + Al2O3 particles
24h RT Curing or 4h at 65 °C
CTD1202
Cyclosiloxanes + Polymethylsiloxane
Initial Cure 1h 80 °C
Post Cure 2h 150 °C
Heat Treat >550 °C

## Slide 12: Questions to Answer
Does Resbond ‘bind’ the fibre tissues? (priority) before moving on.
Does Resbond also produce a brittle, low-strength phase after reaction HT?
Do we obtain a better-performing interlayer with ceramic fibres?
  Young’s Modulus
  Flexural Strength
  DC Breakdown
Does Alumina ceramic behave differently to Silicate?

## Slide 13: Flexural Properties - Test Matrix
3mm Plates | S2 Glass (Desized) | Silicate 600 | Silicate 1100 | Ceramic
Binder + HT | X | X |  | X
No Binder + No HT |  | X |  | X
No Binder + HT |  | X |  | X
3mm Cured Stack | S2 Glass (Desized) | Silicate 600 | Silicate 1100 | Ceramic
Binder – No Impregnation | X | X |  | X
Ceramic vs glass fibres, effects of reaction on binder and fibres.
Interlayer performance during winding. (does it bind?) (keep note of binder amount)
Initial rough test, visual to see if it stays together at least.
Flexural Test

## Slide 14: Electrical Properties - Test Matrix
0.5mm Plates | S2 Glass (Desized) | Silicate 600 | Silicate 1100 | Ceramic
No Binder + HT |  | X |  | X
Binder + HT | X | X |  | X
Ceramic vs glass fibres, effects of reaction on binder and fibres.
DC Breakdown Test in Oil

## Slide 15: Summary of Test Samples
3mm composite plates for flexural tests, x7
3mm cured stack for interlayer winding test, x3
0.5mm composite plates for DC breakdown test, x5
Minimum number of impregnations: 7
0.5mm composite plate for electrical tests
3mm composite plate for mechanical tests

## Slide 16: Additional Slides