## Slide 1: Progress Report of the MCBRD Magnets3 () (2025.04.14)
Yingzhe Wang

## Slide 2: Progress of series production
 | Nickname CERN | Manufacturer | Remarks | Status | Location
MCBRD05 |  |  |  | On the way to CERN | -
AP1 | MCBRD_CB18 | BAMA | 532A, 42 quenches | 394A (3 quenches); 422A (+6 quenches) | 
AP2 | MCBRD_CB19 | BAMA | 530A, 68 quenches | 394A (7 quenches); 422A (+10 quenches) | 
MCBRD06 |  |  |  |  | CERN
AP1 | MCBRD_CB14 | BAMA | 530 A (30+34 quenches) |  | 
AP2 | MCBRD_CB21 | BAMA | 530 A (119quenches) |  | 
MCBRD07 |  |  |  | On the way to CERN | 
AP1 | MCBRD_CB20 | BAMA | 530A (68 quenches) |  | 
AP2 | MCBRD_CB23 | BAMA | 530A (76 quenches) | 3.2KV-20.4GΩ | 
 | MCBRD_CB22 | BAMA | 489A (124 quenches), put in quarantine | 3.2kV-71GΩ | IHEP
MCBRD08 |  |  |  |  | 
 | MCBRD_CB24 | BAMA | 530 A(147 quenches) | 3.2kV-35GΩ | IHEP
 | MCBRD_CB25 | BAMA | 501A(20 quenches) | 3.2kV-49.9GΩ | IHEP
MCBRD09 |  |  | Yoke lamination will be ready by the end of May |  | 
 | MCBRD_CB26 | BAMA |  | 3.2kV-93.2GΩ | IHEP
 | MCBRD_CB27 |  | Waiting for VPI |  | 
MCBRD10 |  |  | Yoke lamination will be ready by the end of August |  | 
 | MCBRD_CB28 |  |  |  | 
 | MCBRD_CB29 |  |  |  | 
CB24 reached 530A after 147 quenches.
CB25 reached 500A after 20 quenches.
Training of CB25 stopped due to some insulation problem of Vtaps.

## Slide 3: Training history of CB25

## Slide 4: Training history of CB24

## Slide 5: Training history of all apertures
CB25

## Slide 6: lhcmcbrd0064