## Slide 1: Beam Instrumentation in TCC8 before BDF Failure scenarios on the Target
Mike Parkin
27/3/25

## Slide 2: Scenarios required to provide inputs for the target and beam instrumentation requirements
No dilution – beam at centre
Full spill @4e13 ppp (8mm vs 16mm σ)
Full spill @5e13 ppp (16 mm σ)
Full spill @4e13 ppp (16 mm σ) from cold
Dilution failure
1, 2 and 3 turns + dilution stop @4e13 (16mm σ)
Effects the beam interlock and beam instrumentation, & to check consequence on target
0.16s
0.50s
0.40s
0.26s
(+0.25s)
0.21s
(+0.5s)
0.15s from beam freeze
(+0.75s beam already swept for)
Beam parameters:
Intensity 4e13ppp
Energy 400GeV
Dilution pattern 4 turns per pulse
pulse time 1s
cycle time 7.2s
Model uses: (except when from cold)
Steady state + 1s beam pulse
with 6.2s cooldown
+ beam pulse stationary in centre
0.65s
Block 16 will be optimized somewhat,
With this in mind, a reaction on the order of 0.1s allows all blocks to remain within stress & temperature limits (which themselves have margins)

## Slide 3: Slide from TSAC #1 Generic heat load after full pulse 8mmσ
415°C-
52°C-
Max temperature
160MPa-
-97MPa-
Max principal stress
0MPa
blocks 1-14
blocks 1-14
block 15
block 16 will be optimised
The US 600mm of target
Beam
Beam
Block 16 will be optimized

## Slide 4: Beam at centre 16mm σ at start of pulse 4e13ppp
16mm beam
Ø250mm core
4e13ppp
50mm sweep radius
Temperature limit for time based formation of WO2
400°C
Normal running limit
Stress limit
150MPa
HAS MARGIN OF ×2!
Surface temperature soft limit 400°C reached at 0.18s (block 15)
Temperature limit 700°C reached at 0.50s (block 5)
Stress limit reached at 0.66s (block 15)
Stress limit reached at 0.705s (block 2)
Conclusion: Beam should be prevented from reaching target after 0.5s at centre (temperature)
Model uses:
Steady state + 1s beam pulses with 6.2s cooldown
+ beam pulse stationary in centre
Formation of WO3
700°C
TIME BASED LIMIT
Temperature limit references:
EDMS 2648378
Kubaschewski & Hopkins, 1960
Gulbransen, Andrew & BVassart 1963

## Slide 5: Beam at centre at start of pulse
Chart: Beam failure to centre from start of pulse 50mm sweep radius. Core ø250mm
| 16mm sigma, 4e13ppp | 16mm sigma, 5e13ppp | 8mm sigma, 4e13ppp
Temperature limit | 0.5 | 0.403 | 0.164
Stress limit | 0.705 | 0.545 | 0.169
0. 4s after beam begins at centre
0. 54s after beam begins at centre
Selected blocks (1/4 model)
16mm σ, 5e13ppp
Beam
Beam
Conclusion: Beam should be prevented from reaching target after time at centre
0.1s to allow all blocks to remain within stress & temperature limits (which themselves have margins)

## Slide 6: Beam freezing during sweep σ = 16mm, 4e13ppp.
0. 1s after beam begins at centre
0. 15s after beam begins at centre
Selected blocks 16mm σ, 4e13ppp
Beam
Unit: Pa
Beam
A normal pulse is 4×sweeps, total time 1s.
Chart: Beam failure during sweep time 0s = start of beam failure/freeze 50mm sweep radius. Core ø250mm
| after 1 sweep | after 2 sweeps | after 3 sweeps
Temperature limit | 0.52 | 0 | 0
Stress limit | 0.264 | 0.205 | 0.15
* Temperature limit not reached by end of pulse.
*
*