## Slide 1
N. Sammut & M. Buzio
With special thanks to
L. Bottura, F. Boattini, R. Beltron,
U. Martinez Hernandez, G. Deferne, D. Drevard, M. Dantas
Material Properties
for Accelerator Magnets
June 2025

## Slide 2: Measurement Principle
List of symbols
log-mean radius
, number of excitation/sensing turns
test specimen cross-section
sensing-coil area
excitation current
induced voltage
magnetic flux
Toroidal ring test method for soft ferromagnetic materials DC characterization, based on the fluxmetric method (transformer configuration).
The standard IEC 60404-4 [3] provides guidelines for the characterization at room temperature and the operational procedures
[1] K.N. Henrichsen, “Permeameter”, Proceedings of the Second International Conference on Magnet Technology, 1967
[2] P. Arpaia, M. Buzio, L. Fiscarelli, G. Montenero, L. Walckiers, 2010 IEEE Instrumentation & Measurement Technology Conference Proceedings, 2010
[3] IEC 60404-4, “Magnetic materials - Part 4: Methods of measurement of DC magnetic properties of magnetically soft materials”, International Electrotechnical Commission, 2000
IEC-compliant test specimen

## Slide 3: Measurement Principle

## Slide 4: Measurement Principle
Custom-winding permeameter
Fewer excitation turns can be used to measure low magnetic fields (<10 A/m) by using conveniently high currents at high frequencies
Dynamic characterization possible in the kHz range for some materials (skin effect is ignored for now)
Typical maximum field limited to 10~20 kA/m at RT for thermal reasons (depending on the current density that you can have in the conductor and the cooling used)
Manual winding of the coils allows to cover a wide range of sample sizes, aspect ratios and winding turn counts

## Slide 5: Sample Preparation
50 µm Kapton rings
250 µm steel rings
ring stack
excitation/detection windings
Sample 1: FeCo only
Sample 2: FeCo interleaved with Kapton

## Slide 6: Sample Preparation
Sample 1: - FeCo only
- inner diameter: 75.5mm
- outer diameter: 82.8mm
- lamination thickness: 0.25mm
- mounting: FeCo rings stacked vertically fixed with tape
- number of rings: 40 FeCo rings
- sensing wire: 0.8mm diameter; 3 turns
- excitation wire: 0.8mm diameter; 10 turns
- Area of coiling around sample: 5mm*10.5mm
Sample 2: - FeCo interleaved with Kapton
- inner diameter: 75.5mm
- outer diameter: 82.8mm
- lamination thickness: 0.25mm
- mounting: FeCo rings stacked vertically with Kapton tape in between laminations cradled in a 3D printed PLA casing
- number of rings: 40 FeCo rings interleaved with 39 Kapton tape between laminations
- sensing wire: 0.8mm diameter; 3 turns
- excitation wire: 0.8mm diameter; 10 turns
- Area of coiling around sample: 7.5mm*14.5mm

## Slide 7: Test Setup
DCCT (120A/10V)
Zero-Flux Multi-Aperture
Current Comparator MACC
AE Techron 2120 current amplifier
Keysight 33500B Waveform Generator
multimeter
DCCT power supply
PC & NI mioDAQ
Sample
PC

## Slide 8: Test Campaign (December 2024)

## Slide 9: First Results – Excitation Curves
First results: 52 different current pulses up to 1.2 T, 28 kT/s Example: 100 A, 16 ms current pulse, FeCo rings only
Drop sharper than rise → clearer final decay transient

## Slide 10: First Results – Eddy Current Time Const
- Notice the low difference in time constant
- Maybe penetration is stopped by the skin effect, or the ring chemical treatment?
- Maybe there is no reason to insulate the laminations?
- Maybe the eddy currents are anyway confined to the outer rings?

## Slide 11: First Results – Hysteresis

## Slide 12: First Results – Permeability

## Slide 13: Conclusion
- These results demonstrates the capability of the test setup to achieve field ramp rates well above the target range
Further Work
- LabVIEW programme to replace function generator to generate input voltage to current amplifier
- use of faster DAQ system for better voltage offset estimation (integrator drift correction)
(currently 500 kS/s or use AI simultaneous mode 1MS/s))
- improve current control to achieve higher fields (eliminate current plateau decay)
- Full (bipolar) hysteresis loop tests
- results comparison with independently tested sample (to check system integrity)
- reproducibility tests
- Series material tests