## Slide 1
Progress on
FEA Magnetic Loss Evaluation in the Frequency Domain Based on
Experimental identification
E.Simoni1,P.Viarouge2 ,F.Boattini3
1HEIA-FR, Switzerland,
2LEEPCI, Université Laval, Canada, CERN Visc
3CERN SY-EPC
mmWG Meeting June 26th 2026

## Slide 2: Outline
  Dipole magnet optimal design tool
  FEA Frequency-Domain Magnetic Loss Evaluation Method
  Superposition of Magnetic Losses via Time-Harmonic FEA & Bertotti Model
  Limits of Harmonic Loss Superposition Improvement by Experimental Correction
  Magnetic Material Bench Test
  Measurement Process & Implementation in Real-Time Simulink on Speedgoat
  Preliminary Results with Sinusoïdal Excitation
  Conclusion & Perspectives

## Slide 3: Dipole Topology
Dipole Magnet geometry defined by 19 variables
M235-35A
M235-35A

## Slide 4: Dipole Optimal Design Environment
Copper & magnetic losses in pulsed regime are computed using time-harmonic FEA simulations.
The frequency-domain approach ensures minimal FEA runs per optimization step, offering much faster computation than time-domain simulations
Constrained NLO
GRG or Evolutionary
Input Dimensioning Variables
Electromagnetic Model
(FEA)
Thermal & Cooling Model
Mechanical Model
19 geometrical variables
Max Current density
Current pulse width
Pulse Cycle period
Harmonic content of Unit Current pulse on.
Material Parameters
Extraction Current
Air gap, pole & yoke inductions
Stored Magnetic Energies
Copper Loss
Magnetic Loss
Water Temperature & speed
Cooling Thermal Time Constant
Mass &Volume
Electrical Equivalent Circuit
Dimensioning Model
Output Performance Variables
Constraints evaluation:
Design specifications to respect
Objective function evaluation:
(Different possible optimization scenarios)

## Slide 5: Superposition of Magnetic Losses via Time-Harmonic FEA and Bertotti Model
Assumptions:
  Bertotti model:identified from sinusoidal tests)
  Time Harmonic FEA assumes linear magnetic materials (saturation modelled by frozen permeability approach)
Procedure:
  Decompose excitation current i(t) on into harmonics: → ,
  For each , perform FEA with
  FEA computes magnetic flux density Bₙ in each mesh of the core
  Evaluate losses using Bertotti model:
  Integrate losses over core volume via FEA postprocessing:
  (Optional) Apply experimental correction factor ( for specific excitation signal see next slides)
  Compute average steady-state Copper losses on
  Advantages:
  Physically grounded and compatible with FEA tools like FEMM,…..

## Slide 6: Limits of Harmonic Loss Superposition Improvement by Experimental Correction
Why the Superposition Method Is Not Sufficient by Itself:
  Bertotti model is valid only for sinusoidal excitation
  Superposition assumes no interaction between harmonics
  Real materials exhibit nonlinear coupling → underestimated losses
Experimental Correction Strategy: Use a measurement bench with a material sample to:
  Identify Bertotti model coefficients for sinusoidal excitation
  Apply directly real waveform on material sample & directly measure total loss
  Measure loss for each harmonic separately
  Compute correction factor: (from Bertotti model)
Result:
  Bertotti remains usable
  Superposition becomes physically valid after correction
  Enables accurate prediction for distorted signals with experimental correction factor: (Ex: triangular pulse)

## Slide 7: Overview of the test bench
The sample excitation signal shape, frequency & amplitude can be defined by the user

## Slide 8: Measurement Process Using the Test Bench
Calculation of :
Calculation of :
Voltage × current product
Sliding average
Integration of secondary voltage
Removal of Flux DC component
Gain dependent on toroid cross-section & secondary winding turns
Calculation of
Gain dependent on toroid average perimeter & excitation winding turns
Excitation Signal generation
Soft-Start
Detection of steady state regime
()
Example: sinusoidal tests

## Slide 9: Implementation with Real-Time Simulink
Amplitude & frequency control
current and thermal protection

## Slide 10: Preliminary Results with Sinusoïdal Excitation
Mag loss in Toroïdal sample
Atarget | f (Hz) | Nper | Pmag (W)
0.09 | 140 | 13 | 0.841
0.1 | 200 | 19 | 1.366
0.134 | 400 | 10 | 3.535
0.134 | 400 | 15 | 3.534
0.15 | 800 | 32 | 6.168
0.2 | 800 | 32 | 9.521
B(H) Curves
Bmax (T) | 0.917 | Hmax (A/m) | 980
Bmin (T) | -0.903 | Hmin (A/m) | -990
Sample Bmax tests
  For
  At max current possible before protection (~24.8 A)
Annealed or non-annealed Vacoflux??

## Slide 11: Conclusion & Perspectives
Simplified Time Harmonic FEA Methodology :
  for Mag loss computation under steady-state pulsed regime
  suitable for implementation in iterative design optimization with computational efficiency
  Harmonic Loss Superposition Improvement by Experimental Correction
Magnetic material Test Bench:
  Versatile test bench
  Enables identification of Bertotti parameters and correction factor for waveform shape
Next steps
  Design of material samples is mandatory for model cross-validation
  Test the Tekron Amplifier in current control mode
  Test Speedgoat acquisition with 100 kS/s (using DMA)
  Automated B–f Characterization Process
  …
Actual sample

## Slide 13
Steady-state obtained on on with Time-domain FEA
Time-domain FEA demonstrated that a harmonic decomposition is required to account for the transient extinction of eddy currents in the conductors.