## Slide 1: Current Leads and Superconducting Transmission
Amalia Ballarino, CERN
04/06/2025

## Slide 2: Outline
Transmission of electrical current from room temperature to the cryogenic environment (current leads) and transmission of electrical current at cryogenic temperature (bus-bar and superconducting links)
  Conventional and superconducting current leads
  Superconducting materials
  Cryogenic options for the cooling
  Impact of electrical circuit
Optimization of cryogenic and electrical performance
Protection
The material presented in these slides is discussed in
https://inspirehep.net/literature/1341662 (CAS Proceedings)
where references can also be found

## Slide 3: Current Leads in a Magnet Circuit

## Slide 4: Circuit with a Single Magnet

## Slide 5: Magnets Individually Powered

## Slide 6: Powering of the LHC Machine
The LHC main lattice circuits are fed from the even points, left and right

## Slide 7: LHC Main Dipole Circuit

## Slide 8: Current Leads
Current leads are usually the dominant source of heat leaking into the magnet(s) cryostat
Objective of a current lead design: minimisation of the heat leak introduced by the transmission of a given current and of the cryogenic cost of the electrical transmission
Sources of heat: thermal conduction from room temperature to the cryogenic environment and ohmic loss

## Slide 9: Thermal Conductivity in Metals (1/2)

## Slide 10: Thermal Conductivity in Metals (2/2)
1/2
Ke derived from Boltzmann
transport equation
(1.381×10−23 J/K)

## Slide 11: Wiedemann-Franz Law (1/2)

## Slide 12: Wiedemann-Franz Law (2/2)

## Slide 13: Optimization of a Current Lead

## Slide 14: Conduction Cooled Current Leads
Steady state, mono-dimensional, Wiedemann-Franz Law

## Slide 15: Conduction Cooled Current Leads

## Slide 16: LHC Dipole Correctors Current Leads

## Slide 17: LHC Dipole Correctors Current Leads

## Slide 18: Self-Cooled Current Leads (1/3)
x
System of non-linear second-order partial differential equations – mono dimensional configuration

## Slide 19: Self-Cooled Current Leads (2/3)
QC,min(LN2) = 23 W/kA

## Slide 20: Electrical Resistivity and Thermal Conductivity

## Slide 21: Self-Cooled Current Leads (3/3)
VC = Vapour (self) cooled
SS = Stainless Steel
Cu ETP = Copper Electrolytic Tough Pitch
Notes: Cu ETP: a highly pure copper variety, refined through electrolysis

## Slide 22: Temperature Profile of Optimized Self-Cooled Current Lead

## Slide 23: Conventional vs HTS Current Leads

## Slide 24: HTS Current Lead: Resistive Part (1/4)
The most efficient cooling schemes for HTS leads are based on independent cooling of the resistive and HTS parts. For a self-cooled HTS current lead, the reduction in exergetic cost of the refrigeration is only  15 %

## Slide 25: HTS Current Lead: Resistive Part (2/4)
Cu with RRR = 70

## Slide 26: HTS Current Lead: Resistive Part (3/4)

## Slide 27: HTS Current Lead: Resistive Part (4/4)

## Slide 28: LHC and ITER Current Leads

## Slide 29: HTS Current Lead: HTS Part

## Slide 30: HTS for Current Leads

## Slide 31: Conventional vs HTS Current Leads

## Slide 32: Thermal Conductivity of Bi-2223

## Slide 33: High Temperature Superconductors
Ag Matrix
Bi-2223 filaments
Ag is a good thermal conductor !
Metallic substrate
Buffer layers
REBCO layer

## Slide 34: Silver-Gold Alloy
N.B. The thermal conductivity of an alloy is not a weighted average
of its elemental constituents - the bonding structure strongly affects the heat transfer
Alloying of silver with gold to reduce the thermal conductivity of the matrix wrt pure silver

## Slide 35: Ic(T) Dependence – BSCCO 2223

## Slide 36: Ic(B) Dependence – BSCCO 2223
77 K

## Slide 37: Operating Temperature - THTS

## Slide 38: LHC Current Leads: Saving

## Slide 39: LHC HTS Current Leads

## Slide 40: LHC HTS Current Leads

## Slide 41: LHC HTS Current Leads in the Tunnel

## Slide 42: Persistent Current Mode Operation

## Slide 43: Protection of Current Leas and Bus-Bar
A conventional self-cooled current lead needs to be protected against thermal run-away
The resistive and the HTS part of a HTS lead need to be protected against respectively thermal run-away and resistive transition (quench)
In most cases, the superconducting bus needs to be protected against resistive transition

## Slide 44: Protection of Current Leas and Bus-Bar
When one magnet quenches, quench heaters are fired for this magnet. Resistance is switched in the circuit
The current in the quenched magnet decays in about 200 ms – it flows through the bypass diode
Ex. LHC Dipole circuit

## Slide 45: Protection of Current Leas and Bus-Bar
Ex. LHC Dipole circuit
The time constant of the LHC Main Dipole circuit is 107 s. This “rapid” current decay is obtained by switching an external resistance into the circuit
If the leads or bus-bar quench, the time constant for the discharge is given by the circuit (107 s for the LHC Main Dipole chain)

## Slide 46: Protection of Bus-Bar
Ex. LHC Dipole circuit
Bus-Bar: Nb-Ti Rutherford Cable with copper stabilizer

## Slide 47: Protection of HTS Part of LHC Current Leads
NB: The long time constant of a circuit may make the use of HTS leads not appropriate. Ex. ATLAS toroid current leads (20.5 kA) are conventional (slow discharge of the circuit:   3 hours)

## Slide 48: Energy Stored in LHC Dipole Magnets

## Slide 49: Protection of LHC Bus-Bar

## Slide 50: Protection of LHC Bus-Bar

## Slide 51: Superconducting Links
HL-LHC Configuration
LHC Configuration
SC Links

## Slide 52: Superconducting Links for HL-LHC

## Slide 53: Superconducting Links for HL-LHC
Itot up to 117 kA DC
Room Temperature cables – instead of SC Link - would not be an option because of power consumption and volume
Removal of current leads from the LHC tunnel

## Slide 54
Thanks for your attention !