## Slide 1: VTRx+ Quality Assurance Programme: A Focus on Optical Alignment
Hannah Fabik
EP-ESE-BE
April 30, 2025

## Slide 2: Agenda
Introduction to the VTRx+
Outline of the QA process
Analysis of failures
Alignment tolerances
Alignment algorithm verification
Functional test results
Conclusion

## Slide 3: The VTRx+ module
A high-speed optical transceiver module developed for HL-LHC upgrades in CMS and ATLAS.
4 transmitter channels, 1 receiver channel
Operating conditions between -35°C and 65°C
Small size (20 mm x 10 mm x 2 mm)
Radiation-hard (1 MGy total dose)

## Slide 4: Production has been ongoing for over 2 years
Production status as of Batch 20.

## Slide 5: Quality Assurance Programme

## Slide 6: The QA programme has multiple stages
Pre-Production Qualification
Production Qualification
Lot Acceptance
Static & dynamic transmitter
Static & dynamic receiver
Temperature
Magnetic field
Irradiation
Static & dynamic transmitter
Static & dynamic receiver
Burn-in
Visual inspection
Static & dynamic transmitter
Static & dynamic receiver
Additional Tests
Temperature
Alignment
CERN
Manufacturer
Complete

## Slide 7: Functional tests use a custom test system
Static tests are measured through the optical power meter.
Dynamic tests are measured through the oscilloscope.

## Slide 8: Temperature tests are conducted in a similar way
Static and dynamic measurements are made at each temperature.
Temperatures measured: -35°C, 25°C, 65°C

## Slide 9: Important Optical Parameters for the Transmitter
Typical optical power [W] is the output power at 6 mA bias current.
Optical modulation amplitude (OMA) [W] is the difference in power between the high and low power levels.

## Slide 10: Important Optical Parameters for the Receiver
Responsivity [A/W] is the amount of current output in response to the amount of light input.
Sensitivity [dBm] is the attenuation that produces a bit error rate of 1e-10 dBm.

## Slide 11: A sudden drop in yield…

## Slide 12: In September 2024, production yield started to drop

## Slide 13: Both transmitters and receivers were failing the functional tests
September

## Slide 14: Receiver failures had offset photodiodes
ID 35511
Rx failure
ID 35451
Tx failure

## Slide 15: Modules with larger photodiode offsets tended to fail

## Slide 16: Resolution of photodiode issues
Incorrect detection of VCSEL eye on the placement machine meant reference points were off and thus the target position of the photodiode.
The company has since managed to correct the issue.

## Slide 17: VCSEL – Lens Offset

## Slide 18: OMA is consistently lower than previous batches
Batch 15 was made in September

## Slide 19: Offsets are calculated with a non-destructive method that uses image recognition
Lens marker
Lens
(250 μm,
300 μm)
(-80 μm,
170 μm)
VCSEL corner
VCSEL eye

## Slide 20: Recent batches past batch 15 have greater offsets of the lens
Batch 15 was made in September

## Slide 21: Alignment Tolerances

## Slide 22: Optical components were tested on separate PCBs
The VCSEL array and photodiode were wire-bonded to separate test PCBs.
Thin wires were soldered to the PCB connection interface to allow it to lie flat on the surface.
y
x
Notes: Point out coordinate systems used here and with the ficonTEC
Notice that it is only the VCSEL and photodiode used, no intermediate components

## Slide 23: The lens was left detached from the board so that it could be moved
Lens held by pick-up tool
PCB with component on vacuum tray
OPM
ficonTEC fibre attachment machine

## Slide 24: Measurement setup
VCSEL measurements
Photodiode measurements
VCSEL
OPM
(Mode scrambler)
Source meter
Photodiode
Source meter
(Mode scrambler)
Laser source
Power supply

## Slide 25: An area scan was conducted with the fibre attachment machine
VCSEL optical output power at a bias current of 2 mA.
The lens was moved over a range of 70 μm with a step size of 1 μm at a height of 32 μm up from the board.

## Slide 26: VCSEL Offset Tolerance
Optical path | Maximum offset without detectable loss (μm)
Direct connection | 8.151
Long fibre | 7.492
Mode scrambler | 6.223
The use of a long fibre and mode scrambler closer resembles a realistic scenario in which the VCSEL would be used, therefore the offset tolerance is 6 - 7 μm.

## Slide 27: Photodiode Offset Tolerance
Optical path | Maximum offset without detectable loss (μm)
Direct connection | 10.454
Mode scrambler | 10.630
The photodiode current was not affected by the loss of light modes through the fibre. Its offset tolerance was around 10.5 μm.

## Slide 28: Alignment Algorithm Accuracy

## Slide 29: Modules with known lens offsets were created
-x
+x
-y
+y

## Slide 30: Calculated offsets were within 5 μm of the expected position
X Shift | -2.838 μm
Y Shift | -0.011 μm
Average deviation from expected position
The assembly process could also have introduced errors such that the expected offsets were not achieved.

## Slide 31: Optical parameters dropped significantly after 8 μm offset
Typical optical power shows a much sharper cut off than OMA.

## Slide 32: Expected Temperature Response
The PCB and lens have different coefficients of thermal expansion (~10 ppm/°C and ~50 ppm/°C respectively)
As the module is heated or cooled, the difference causes a small offset in the relative positions.
  40 ppm/°C × 3 mm × 65°C ≈ 8 μm [expansion]
  40 ppm/°C × 3 mm × -35°C ≈ 4 μm [contraction]
Hot
Cold
Shift direction
Lens
Lens Offset Direction | Cold Response | Hot Response
+x | NC | NC
-x | NC | NC
+y | Worse | Better
-y | Better | Worse
+x
+y
Glue
NC = No change
3 mm
Lens
VCSEL
VCSEL
Lens
VCSEL
Lens

## Slide 33: The VCSEL itself also exhibits temperature dependencies
Thermal rollover occurs at high bias currents when the extra current is converted into heat instead of optical power.
This effect is exaggerated by higher ambient temperatures.

## Slide 34: The temperature results match expectations
At -35°C, the VCSELs should perform better than room temperature (ratio > 0).
At 65°C, the VCSELs should perform worse than room temperature (ratio < 0).
Lens Offset Direction | Cold Response | Hot Response
+x | NC | NC
-x | NC | NC
+y | Worse | Better
-y | Better | Worse

## Slide 35: Summary
A drop in production yield was attributed to failures of the receiver and the transmitter
Receiver failures were due to misplaced photodiodes
  Failures typically had offsets of more than 17 μm, measured with the algorithm
  The photodiode’s offset tolerance is 11 μm, measured with the ficonTEC
Transmitter failures were most likely due to misaligned lenses
  The VCSEL’s offset tolerance is 7 μm, measured with the ficonTEC
  Recent batches are more offset, measured with the algorithm
The algorithm which calculates the offset on average off by 3 μm
  Optical parameters declined after 8 μm, measured with the algorithm
  The temperature response of offset modules followed expectations
The QA programme is robust and provides detailed information about the production performance.
  Corrective actions can be taken based off the data gathered during the process.