## Slide 2
Some notes about margins for FCC-hh main dipoles
Ezio Todesco

## Slide 3: Loadline margin
The loadline margin is the most commonly used when making conceptual design
  The loadline fraction is the ratio between operational field and short sample field
  The loadline margin is 1-loadline fraction
  Note that short sample is defined within a certain error
 | Loadline fraction | Loadline margin
LHC dipoles 7 TeV | 0.86 | 0.14 (or 14%)
LHC dipoles 6.8 TeV | 0.84 | 0.16 (or 16%)
MQXF 7 TeV | 0.78 | 0.22 (or 22%)
MBXF (HL-LHC D1) 7 TeV | 0.77 | 0.23 (or 23%)
MBRD (HL-LHC D2) 7 TeV | 0.68 | 0.32 (or 32%)
MCBRD (HL-LHC CCT correctors) 7 TeV | 0.47 | 0.53 (or 53%)

## Slide 4: Loadline margin
The loadline fraction has no physical meaning, but has the advantage of being an observable during test
  A short model magnet reaching
  90% of loadline fraction is
  considered in general as success
  A short model magnet limited
  between 80% and 90% is good,
  but …
  A short model magnet limited
  below 80% is not good

## Slide 5: Loadline margin
The loadline fraction has no physical meaning, but has the advantage of being an observable during test
  Obviously the fact of not
  reaching the critical surface is not
  a sign of intrisic weakness, or lack
  of operational margin since the
  magnet is experiencing much larger
  forces
Quenches
(training)

## Slide 6: Current margin
A margin that has more physical meaning is the current margin
  Unfortunately this is not an observable
  Typically, one has 50% margin or more: this means that if one strand is damaged the whole current can go in the other one
  Note that experimental HEP magnets work usually with 70% margin
 | Loadline margin | Current margin
LHC dipoles 7 TeV | 0.14 | 0.43
LHC dipoles 6.8 TeV | 0.16 | 0.46
MQXF 7 TeV | 0.22 | 0.54
FCC-hh 14 T | 0.20 | 0.60

## Slide 7: Temperature margin
The temperature margin is current sharing temperature minus the operational temperature
  It can be checked that it is >2.6 K for 1.9 K operational temperature, going at 4.5 K
  We plan to have the possibility of testing at variable temperatures, so to better measure the temperature margin and also at 4.5 K operational temperature
 | Loadline margin | Current margin | Temperature margin
LHC dipoles 7 TeV | 0.14 | 0.43 | 1.4 K
LHC dipoles 6.8 TeV | 0.16 | 0.46 | 1.5 K
MQXF 7 TeV | 0.22 | 0.54 | 4.9 K
FCC-hh 14 T | 0.20 | 0.60 | 4.5 K

## Slide 8: Temperature margin
The temperature margin must be large enough to accept the variable temperature of the magnets due to the cryogenic system
  This can be critical at 4.5 K
The temperature margin, when translated in enthalpy margin, gives a measure of which local energy losses (instantaneous) can be tolerated (from the beam or from movements of the coil)
 | Loadline margin | Current margin | Temperature margin
LHC dipoles 7 TeV | 0.14 | 0.43 | 1.4 K
LHC dipoles 6.8 TeV | 0.16 | 0.46 | 1.5 K
MQXF 7 TeV | 0.22 | 0.54 | 4.9 K
FCC-hh 14 T | 0.20 | 0.60 | 4.5 K

## Slide 9: The ReBCO case
For ReBCO, the temperature margin at 0.80 loadline fraction gets twice larger (from 5 to 10 K) than Nb3Sn, but the current margin is reduced by 1/3 (goes down to 32%)
If you want to have the ~50% current margin, you should design for ~ 20 T short sample (~ 30% loadline margin)
 | Loadline margin | Current margin | Temperature margin
LHC dipoles 7 TeV | 0.14 | 0.43 | 1.4 K
LHC dipoles 6.8 TeV | 0.16 | 0.46 | 1.5 K
MQXF 7 TeV | 0.22 | 0.54 | 4.9 K
FCC-hh 14 T | 0.20 | 0.60 | 4.5 K
FCC-hh 14 T HTS | 0.20 | 0.32 | 8.5 K
FCC-hh 14 T HTS | 0.30 | 0.47 | 17.5 K
Thanks to M. Statera and G. Succi

## Slide 11: Some comments
Translate in enthalpy margin
Replace HTS with ReBCO
A 50% margin in current
Separate what needed by magnet / by operation
The training speed up at 1.9 K vs 4.5 K
Margin of HEP experimental magnets: 70% or more
Jc depends on state of strain