## Slide 1: Electron gun & collector for the new AD e-cooler Numerical assessment
Teresa Guillen Hernandez
24/04/2025

## Slide 2: Thermo-mechanical analysis – No tantalum
Deformation along Z - 15 thermal cycles
Bolted connections at 1000 °C and 700 °C ?
Stress relaxation
Self weight
Could we lose the position? Maybe use spot welds?
Total deformation first cycle (operation)
Chart: Maximum equivalent plastic strain evolution in 15 cycles
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19 | 21 | 23 | 25 | 27 | 29
 | 0.024133 | 0.024698 | 0.025628 | 0.026499 | 0.027046 | 0.027461 | 0.027804 | 0.028095 | 0.02835 | 0.028578 | 0.028844 | 0.029065 | 0.029259 | 0.029441 | 0.029544
stabilization
3 % < 304L elongation
First cycle
operation 1mm
shut down 0.087 mm
15 cycle
operation 0.96mm
shut down 0.061 mm
Notes: Material elongation 40-58%

## Slide 3: Thermo-mechanical analysis – No tantalum
Temperature [°C] | 24 | 38 | 93 | 149 | 204 | 260 | 316 | 371 | 427 | 482 | 538 | 593 | 649 | 704 | 760 | 816 | 871
Yield strength [MPa] | 175 | 170 | 149 | 135 | 122 | 114 | 108 | 105 | 101 | 98 | 93 | 87 | 79 | 70 | 68 | 54 | 35
St steel 304L
Material properties at high temperatures
After cooling down – carbide precipitation
  Lower material properties
Inconel ?
Notes: At high temperatures, the grain size increases, so we reduce a lot the material properties.
When cooling down, carbides precipitates will form in the grain boundaries. This means that the material properties will decrease again.
And we have a lot cycles, right? 10 cycles/year during 20 or 40 years
Proposal – used Inconel

## Slide 4: Bake out - 250 °C
Average stresses ceramics - Rankine criteria |  | 
= 16MPa | ⩽ | = 259 MPa
= -38 MPa | ⩽ | = 2900 MPa
Average stresses ceramics - Rankine criteria |  | 
 | ⩽ | 
 | ⩽ | 
While heating
Cool down
Critical areas ceramic – connections with the collars
Deeper analysis once the new design is finalized
Notes: 0.55 MPa on the ceramics due to gravity
Residual -15MPa, 20MPa
0.55 MPa on the ceramics due to gravity, 𝜎_(𝑝_𝑚𝑎𝑥) = 80 MPa 𝜎_(𝑝_𝑚𝑖𝑛) = 117 MPa on the ceramics during operation
Displacements bigger than in operation because the temperatures are higher, even if there are no thermal gradients
Accumulated plastic strain. It is a scalar value of the plastic strains, doesn’t care about the direction. So even if you reverse the plastic strain, is always going up

## Slide 5: Bake out - 250 °C
Cool down

## Slide 6: Conclusions
Operation
  We move 1mm in the longitudinal direction during the first cycle of operation and we don’t go back to the initial position after the cool down
  TOLERANCES ?
  We will not break due to plasticity.
  Bolted connections?
Bake out
  We move 0.44mm in the longitudinal direction after the bake out
  TOLERANCES ?
Steel at high temperatures
  Inconel were we have plasticity or very high temperatures?