## Slide 1
nLGAD Gain suppression on irradiated samples
Main results for paper
June 12th 2025
Jairo Antonio Villegas Dominguez
Salvador Hidalgo Villena
Florent Dougados

## Slide 2
Setup for Laser Power Measurements

## Slide 3
The Power Meter
400-1100 nm wavelength
Integrated Si detector
Accuracy of 5%
Optical Fiber connector
Wavelength
selection
LP = laser power [W]=[J/s]
Unit measured, for a given frequency
Number of photons per pulse
f = frequency
Eγ = number of photons per energy unit [J/photon quanta]

## Slide 4
Laser Power vs frequency
LP = laser power [W]=[J/s]
Unit measured, for a given frequency
Number of photons per pulse
f = frequency
Eγ = number of photons per energy unit [J/photon quanta]
The relationship seems linear, BUT

## Slide 5
Number of photons per pulse
f = frequency
Eγ = number of photons per energy unit [J/photon quanta]
The relationship seems linear, but...
The number of photons per pulse decreases for low frequencies (losses?)
TCT Measurements = 1kHz
Laser Power vs frequency

## Slide 6
The beam size (projection on device Surface)
LP = laser power [W]=[J/s]
A = Laser projection on nLGAD Surface [cm2]
Eγ = number of photons per energy unit [γ/J]
= number of photons per unit area
FWHM = X = 100 um
FWHM = Y = 99 um
FWHM = Beam Diameter
Estimation A = π(FWHM/2)2
Beam Diameter ≠ FWHM
in a Gaussian beam

## Slide 7
The beam size (projection on device Surface)
In all TCT measurements, FWHM <= 350 µm (half of the entrance window diameter = 700 µm)
= number of photons per unit area
Beam Diameter (>90% intensity) > 1.7 x FWHM
in a Gaussian beam
A will be redefined accordingly

## Slide 8
Non irradiated nLGAD

## Slide 9
Gain @ 20ºC - TCT Visible Light 404 nm wavelength
Φ to be redefined
Non irradiated LG14 device
A clear maximum gain for mínimum ϕ is observed
Other phenomena
  Breakdown voltage decrease with increasing ϕ
TCT Blue
404 nm

## Slide 10
Gain @ 20ºC - TCT Visible Light 404 nm wavelength
Φ to be redefined
Non irradiated LG14 device
A clear maximum gain for mínimum ϕ is observed
Other phenomena
  Breakdown voltage decrease with increasing ϕ
TCT Blue
404 nm

## Slide 11
Gain @ 20ºC - TCT IR Light 1060 nm wavelength
Φ to be redefined
Non irradiated LG14 device
A clear maximum gain for mínimum ϕ is observed
TCT IR
1060 nm

## Slide 12
Gain @ 20ºC - TCT IR Light 1060 nm wavelength
TCT IR
1060 nm
Φ to be redefined
Non irradiated LG14 device
A clear maximum gain for mínimum ϕ is observed

## Slide 13
Gain @ 20ºC – IR and Visible Light
Φ to be redefined
Non irradiated LG14 device
Gain suppression is enhanced for low penetrating light (electron multiplication)
Other phenomena
  Gain for IR and visible light are similar for high values of ϕ

## Slide 14
Irradiated nLGADs
Visible Light 404 nm

## Slide 15
Gain @ 20ºC – Visible Light 404 nm wavelength – 2e13 p/cm2
Φ to be redefined
First fluence value: 2e13 p/cm2
A clear maximum gain for minimum ϕ is observed

## Slide 16
Gain @ 20ºC – Visible Light 404 nm wavelength – 3e13 p/cm2
Φ to be redefined
First fluence value: 3e13 p/cm2
A clear maximum gain for minimum ϕ is observed
Other phenomena
  Depletion voltage increases with proton fluence

## Slide 17
Gain @ 20ºC – Visible Light 404 nm wavelength – 3e13 p/cm2
Φ to be redefined
First fluence value: 3e13 p/cm2
A clear maximum gain for minimum ϕ is observed
Other phenomena
  Depletion voltage increases with proton fluence

## Slide 18
Gain @ 20ºC – Visible Light 404 nm wavelength – 1e14 p/cm2
Φ to be redefined
First fluence value: 1e14 p/cm2
A clear maximum gain for minimum ϕ is observed
Other phenomena
  Depletion voltage increases with proton fluence

## Slide 19
Gain @ 20ºC – Visible Light 404 nm wavelength – All fluences
Φ to be redefined
All fluences!
The maximum gain decreases with fluence
Other phenomena
  Depletion voltage increases with proton fluence

## Slide 20
Gain @ 20ºC – Visible Light 404 nm wavelength – All fluences
Φ to be redefined
All fluences!
The maximum gain decreases with fluence
Other phenomena
  As expected, the signal degrades with proton fluence

## Slide 21
Comments after discussion:
Measurements with IR light
Confirming the gain suppression “not applying” before full depletion
Gain reduction observed when sweeping z (3D plot)
UV discarded
Visible light, IR light
  -20ºC and 20ºC