## Slide 1: Electron gun & collector for the new AD e-cooler Numerical assessment
Teresa Guillen Hernandez
22/05/2025

## Slide 2: Objective
Operation
  Relative displacement due to plasticity
  New design of the part in contact with the cathode
    Inox
    Molybdenum
    Inconel
Bake out
  Review BC
  Relative displacement due to plasticity (as in operation)
Ceramics

## Slide 3: Operation new design – materials
First cycle
operation 0.793 mm
shut down 0.0078 mm
St steel 304L
Molybdenum
Inconel
First cycle
operation 0.9359 mm
shut down 0.01156 mm
First cycle
operation 0.793 mm
shut down 0.00096mm
Chart: Ratcheting (15 cycles )
| 1 | 3 | 5 | 7 | 9 | 11 | 13 | 15 | 17 | 19 | 21 | 23 | 25 | 27 | 29
Mo | 0.025972 | 0.030061 | 0.033084 | 0.035623 | 0.037841 | 0.039824 | 0.04167 | 0.043442 | 0.045103 | 0.046723 | 0.048265 | 0.049784 | 0.051265 | 0.052696 | 0.054092
Inox 304L | 0.03392 | 0.032485 | 0.031537 | 0.030944 | 0.032276 | 0.033558 | 0.034901 | 0.036307 | 0.037693 | 0.03905 | 0.040448 | 0.041799 | 0.043155 | 0.044535 | 0.045949
Inconel | 0.018922 | 0.020662 | 0.021604 | 0.022273 | 0.022787 | 0.023185 | 0.023502 | 0.023756 | 0.023964 | 0.024133 | 0.024273 | 0.024388 | 0.024482 | 0.02456 | 0.024624
Stabilization
3 % < 50 % Inconel elongation
Bolted connections at ≈ 500 °C ?
Stress relaxation
Self weight
  Inconel bolts
  Preload = 75% at 500 °C
  ( ≈ 387 MPa Inconel and ≈ 95MPa 304L)
Tolerance 0.8mm but only at room temp?
What happens in operation?

## Slide 4
Bake out - 250 °C
Boundary conditions

## Slide 5: Bake out - 250 °C
250 °C
T room
Relative displacement Z
250 °C: 0.03213 mm
T room: 0.00018 mm
Relative displacement Z
250 °C: 0.04944 mm
T room: 0.00286 mm
Notes: 0.55 MPa on the ceramics due to gravity, 𝜎_(𝑝_𝑚𝑎𝑥) = 80 MPa 𝜎_(𝑝_𝑚𝑖𝑛) = 117 MPa on the ceramics during operation
Displacements bigger than in operation because the temperatures are higher, even if there are no thermal gradients
Accumulated plastic strain. It is a scalar value of the plastic strains, doesn’t care about the direction. So even if you reverse the plastic strain, is always going up

## Slide 6: Bake out - 250 °C
Ceramics with invar collars
250 °C
T room
Attention with sharp edges
Reduce the bake out temp
Rankine criteria |  | 
 | ⩽ | = 259 MPa
 | ⩽ | = 2900 MPa
Rankine criteria |  | 
 | ⩽ | 
 | ⩽ | 
Notes: 0.55 MPa on the ceramics due to gravity, 𝜎_(𝑝_𝑚𝑎𝑥) = 80 MPa 𝜎_(𝑝_𝑚𝑖𝑛) = 117 MPa on the ceramics during operation
Displacements bigger than in operation because the temperatures are higher, even if there are no thermal gradients
Accumulated plastic strain. It is a scalar value of the plastic strains, doesn’t care about the direction. So even if you reverse the plastic strain, is always going up

## Slide 7: Conclusions
Operation
  Tolerances only at room temperature?
  Inconel – no ratcheting and better properties at high temp. (we can trust the properties we are using)
  Bolts – Inconel and preload 75% at the corresponding temp.
Bake out
  Tolerances ?
  Reduce the temp.?
First cycle with Inconel
operation 0.793 mm
shut down 0.001mm
Relative displacement Z
250 °C: 0.03213 mm
T room: 0.00018 mm
Relative displacement Z
250 °C: 0.04944 mm
T room: 0.00286 mm