## Slide 1: Electrical insulation testing of the HL-LHC Cold Powering Systems
C. Barth, M.-P. Careil, A. Ballarino on behalf of WP6a
MSC Technical Forum #15

## Slide 2: Electrical requirements & design criteria
Highest possible voltage during operation:
  Inner Triplets: 914 V
  Matching Sections: 1268 V
  120 A / 200 A correctors: 242 V
Electrical test levels (Components):
  MgB2 cables: in air
    Inner Triplets: 15.0 kV (NOC equivalent: 815 %)
    Matching Sections: 15.0 kV (NOC equivalent: 580 %)
  Vapor cooled current leads: in warm He gas (300 K GHe)
    Inner Triplets: 5.0 kV (NOC equivalent: 550 %)
    Matching Sections: 5.0 kV (NOC equivalent: 400 %)
  IFS system: in air
    Inner Triplets: 5.0 kV (NOC equivalent: 55 %)
    Matching Sections: 5.0 kV (NOC equivalent: 40 %)
  IFS system: in warm He gas (300 K GHe)
    Inner Triplets: 3.1 kV (NOC equivalent: 340 %)
    Matching Sections: 3.1 kV (NOC equivalent: 240 %)

## Slide 3: Electrical requirements & design criteria
Highest possible voltage during operation:
  Inner Triplets: 914 V
  Matching Sections: 1268 V
  120 A / 200 A correctors: 242 V
Electrical test levels (System):
  Full system: in air
    Inner Triplets: 5.0 kV (NOC equivalent: 270 %)
    Matching Sections: 5.0 kV (NOC equivalent: 195 %)
  Full system: in nominal operating conditions (20 K GHe)
    Inner Triplets: 2.3 kV (NOC equivalent: 250 %)
    Matching Sections: 2.3 kV (NOC equivalent: 180 %)
  Full system: in warm He gas (300 K GHe)
    Inner Triplets: 1.1 kV (NOC equivalent: 600 %)
    Matching Sections: 1.1 kV (NOC equivalent: 440 %)
Electrical test levels (120 A / 200 A correctors):
  Conduction cooled leads: in warm He gas (300 K GHe)
    5.0 kV (NOC equivalent: 2060 %)

## Slide 4: Electrical test devices
Spark tester
  Fixed voltage applied with insulated metal ‘curtain’
  Fixed current limit, no measurement, only pass/fail
  One HV output, up to 15 kV
Megger
  Ramp in steps to test voltage, hold test voltage for defined time
  Fixed current limit, insulation resistance measurement
  One HV output, up to 10 kV
WP6a ramping HV tester
  Any combination of voltage ramps & plateaus
  Any combination of current limits, current limit ramps possible
  24 bit, high-speed logging, 50 kHz acquisition, filtered to 1 kHz
  Data analysis script with semi-automatic report generation
  One HV output, up to 15 kV

## Slide 5: Test sequence
Electrical tests during current lead production:
  In-line during HTS cabling: 10 kV, air*
  Vapor cooled lead assembly completion: 5 kV, warm GHe***
  Conduction cooled lead assembly completion: 5 kV, warm GHe***
Electrical tests during MgB2 cable production:
  In-line during cabling: 15 kV, air*
  After cabling: 15 kV, air***
  After reception at CERN: 10 kV, air***
Electrical tests of instrumentation system:
  In-line during wire production: 15 kV, air*
  After bundle forming and insertion in capillaries: 5 kV**
  After IFS completion: 5 kV, air and 3.1 kV, warm GHe**
*Spark Tester **Megger ***WP6a Ramping HV tester ****ELQA team

## Slide 6: Test sequence
Electrical tests during Cold Powering system assembly:
  After MgB2 cable insertion in flexible cryostat: 5 kV, air***
  After DFHX/DFHM splicing & insulation: 5 kV, air***
  After DFX/DFM splicing:
    5 kV, air*** (prototype), skipped for series
  After short-circuits:
    5 kV, air*** (prototype), skipped for series
  After DFX/DFM closure:
    5 kV, air*** (prototype)
    1.1 kV, warm gHe*** (series)
Differences prototype  series
  No 5 kV, air tests on DFX/DFM side as presence of GHe is possible in system stemming from DFHX/DFHM leak tests
  Skipping DFX/DFM tests, after closure final 1.1kV GHe test
*Spark Tester **Megger ***WP6a Ramping HV tester ****ELQA team
GHe presence possible in system due to DFHX/DFHM leak tests

## Slide 7: Test sequence
Electrical tests during Cold Powering system validation:
  Before cold test: 1.1 kV, warm GHe****
  After cold test: 2.3 kV, NOC****
  After cold test: 1.1 kV, warm GHe****
Electrical tests during tunnel installation:
  After system transport & installation, before DFX/DFM assembly: 1.1 kV, warm GHe****
  After DFX/DFM closure: 1.1 kV, warm GHe****
*Spark Tester **Megger ***WP6a Ramping HV tester ****ELQA team
Electrical testing during all stages of Cold Powering System fabrication, assembly, validation and installation
Relies on the great collaboration between WP6a, the ELQA team, the MCF and all involved sections of TE-MSC