## Slide 1: CERN-HFM conductors rationale
L. Bottura
With thanks to L. Oberli, Th. Boutboul, B. Bordini
and “the crowd” in the Superconductors Laboratory
Meeting on 11T dipole conductor
CERN/FNAL
October 4th, 2011

## Slide 2: NED targets
The main goal of NED was to launch the R&D necessary to design and build a Nb3Sn based 15 T magnet
On basis of preliminary magnetic design and protection considerations, NED specifications for the strand were chosen:
  Diameter 1.250 mm
  Eff. filament diameter < 50 µm
  Cu-to-non-Cu ratio 1.25 ± 0.10
  Filament twist pitch 30 mm
  non-Cu JC 1500 A/mm2 @4.2 K & 15 T
  minimum critical current 818 A at 15 T
  RRR (after heat treatment) > 200
Very challenging specifications!
By courtesy of Th. Boutboul

## Slide 3: NED promises
PIT strand: Ic ~ 1400 A, Jc ~ 2500 A/mm2 (12 T) for 675 oC/84 h
Optimization launched at CERN. Results: 320 h @ 625 oC
  12 T and 4.2 K: Ic > 1500 A, Jc > 2700 A/mm2, + 10 %!!
  15 T and 4.2 K: Ic > 818 A (NED spec.), Jc ~ 1500 A/mm2
By courtesy of Th. Boutboul

## Slide 4: NED program results – 1/3
Jc of PIT wire produced within the scope of the NED R&D
Best performance was achieved optimizing the heat treatment for low plateau temperature (625 °C) and long times (320 hrs)
The production has gone through a technology transfer process clearly visible in the measured performance
Clear improvement with present stable manufacturing conditions

## Slide 5: NED program results – 2/3
Excellent RRR values at the beginning of the R&D, much degraded at later times
Optimization of Jc leads to a marked decrease of RRR
This has been traced to the presence of hot-spots in the strand

## Slide 6: NED program results – 3/3
Modified strand architecture to improve the use of the real estate, and increase the optimization margin for JC at acceptable RRR
For any given strand architecture based on react-able barriers there is an intrinsic limit in the maximum RRR achievable

## Slide 7: Magneto-thermal stability
By courtesy of B. Bordini

## Slide 8: Magneto-thermal stability cook-book
Reduce the critical current of the strand to the minimum required for magnet performance (range of 2500 A/mm2, not much above)
Reduce the strand diameter (1 mm and smaller) and the diameter of the multi-filamentary region
Achieve a local RRR of the order of 100

## Slide 9: Effect of RRR on stability – 1/4
Chart: Hours at 695 °C
| 4.0 | 20.0 | 30.0 | 50.0 | 100.0
 | 23.06 | 24.55 | 24.55 | 24.96 | 25.64
 | 48946.3969 | 44039.862 | 42889.9962 | 41126.8685 | 38405.5194
0.8 mm 54/61 RRP® Nb3Sn strand
Samples were prepared using the same strand (copper to non copper ratio ~ 0.92;effective filament size of ~ 80 μm)
Heat treatment chosen in order to obtain different values of the RRR without significantly changing the critical current
By courtesy of B. Bordini

## Slide 10: Effect of RRR on stability – 2/4
‘Perturbation region’: the quench current depends on the energy of the tiny perturbation acting on the strand (big variation of quench currents can occur)
‘Energy Region’: the quench current mainly depends on the potential energy stored in the current distribution
V-H measurements at low fields shows that the minimum quench current significantly decrease by reducing the RRR below 100
4.2 K
By courtesy of B. Bordini

## Slide 11: Effect of RRR on stability – 3/4
At 1.9 K and with the same type of perturbation, the larger Jc and the smaller Cp of the wire (with respect to the values at 4.3 K) extend the ‘energy region’ and move the ‘perturbation region’ towards higher magnetic fields.
The semi-analytical model is in good agreement with the experimental data in the ‘energy region’
1.9 K
By courtesy of B. Bordini

## Slide 12: Effect of RRR on stability – 4/4
The quench current at 4.3 K was computed for the minimum in the low field region (point C ) and for 12 T in the case of self-field instability and large perturbations (point B’ ).
For RRR larger than 100, the instability at low field (in the case of the considered conductor) is not a problem for a magnet designed to work at 12 T (or larger fields).
The high field instability does not improve much increasing the RRR above 100.
By courtesy of B. Bordini

## Slide 13: Microstructure and real estate
By courtesy of I. Pong and L. Oberli
Strand center
Coarse grains
Fine grains

## Slide 14: A summary of what (we think) we understood
The initial NED specifications were possibly too demanding for stable performance in a magnet environment
There is an intrinsic interplay of critical current density, filament diameter, and RRR, equivalent to a critical surface for the overall performance of a given strand

## Slide 15: Performance targets for Nb3Sn
JC (kA/mm2)
Dfil (m)
RRR (-)
Performance
Peak field
Cost
Stability Protection
Magnetization Field Quality
Stability
2.5
2
1.5
3
3.5
1
4
200
150
100
50
10
20
50
100
PIT
RRP
target
Target performance:
Jc > 3 kA/mm2
Dfil < 20 m
RRR > 100

## Slide 16: Present strand specifications
 |  | NED (achieved) | FReSCa-II | DS-MB
Strand diameter | (mm) | 1.25 | 1 | 0.7
Sub-element diameter | (mm) | 50 | 50 | 30*
Copper:non-Copper | (-) | 1.25 | 1.25 | 1.15
JC(12 T, 4.2 K) | (A/mm2) | 2740 | 2500 | 2650
JC(15 T, 4.2 K) | (A/mm2) | 1530 | 1250 | 
n-index | (-) | > 30 | 30 | 30
RRR | (-) | 220 | 150 | 100
Piece length | (m) | > 1000 | 800 | 800
(*) one of the main topics of the discussion today

## Slide 17: Magnetization related matters
Scaled persistent current b3PC vs. strand M in dipoles for all SC synchrotrons to date
Generic multipole (approximate integration in a coil of radius Rcoil):
Case of sextupole in a dipole magnet:

## Slide 18: Expected field quality
OST-RRP 54/61
M ≈ 500 mT
M ≈ 200 mT
b3 ≈ 300 units !!!
What is the actual field error ?
What can be tolerated and corrected ?

## Slide 19: On-going strand work
Work is on-going on a new strand architecture (169 stack) to reduce the filament diameter to 52 mm at 1 mm strand diameter, and 35 mm at 0.7 mm strand diameter
R&D started for an alternative architecture with filaments of 30 mm at 0.7 mm strand diameter
0.7 mm, 108/127 stack RRP from OST
1 mm, 192 tubes PIT from Bruker EAS

## Slide 20: Questions
Do we agree on specifications (strand, cable) for magnet R&D and magnet production ?
Material lead time is long (> 12 months), and we are already late. How do we manage/share the present stock ?
What is the procurement strategy beyond the magnet R&D ?