## Slide 1: Silicon Photonics links for High Energy Physics
Particle sensor
PIC
>> 100 m Single-mode fibre
Photodiode
Modulator
Fiber coupler
ASIC
OPTO
FPGA
System concept under development in the
EP R&D WP6 project
More details in TWEPP 2024 contribution:
https://indico.cern.ch/event/1381495/contributions/5988694/
Photonic Integrated Circuits (PICs)
  Chiplet fabricated using CMOS process
  Fiber couplers, optical waveguides, modulators, photodiodes
  Radiation tolerant
Wavelength division multiplexing:
  Lane: 25 Gbps NRZ
  Fibre: 100 Gbps
  COTS 100G CWDM4 QSFP28 off-detector
Laser sits outside of radiation environment
  Wavelength 1300 nm
  Transparent window for Silicon
  COTS External Laser Source
Low power / Low mass

## Slide 2: PIC System Testing
Demonstrated 4-channel wavelength division multiplexing WDM) operation using an optical circuit integrated into the SystemPIC
  25 Gb/s per channel – 100 Gb/s into a single fibre
Optical power supply: External Laser Sources (ELS) standardised and available from multiple vendors
ELSFP
4-wavelengths ELS optical spectrum
Channel 1 – 1271 nm
Channel 3 – 1311 nm
Channel 2 – 1291 nm
Channel 4 – 1331 nm
25 Gb/s PRBS31
Bond pad
Electrical data in
Ring modulator
200 µm
5 mm
SystemPIC

## Slide 3: PIC Optical Packaging
R&D fiber attachment machine for PICs purchased by CERN
Supporting the R&D activity and build internal knowhow on photonic assembly
Active alignment and vision-based processes fully customisable by the user
8-channel fiber arrays attached to the SystemPIC using UV-cure epoxy
Test vehicle for 4-channel coarse wavelength division multiplexing (CWDM4) transmitter
High coupling efficiency ( ≈ 2 dB per fibre) and flat spectral response
https://ep-news.web.cern.ch/content/silicon-photonics-circuits-integrated-optical-readout-future-high-energy-physics-detectors
Check out the video at:
Edge coupler
Optical fiber
8-channel
fiber arrays
5 mm

## Slide 4: PIC Co-Packaging with DART28
Proof of concept for PIC and driver co-packaging
Stepping stone for the EP R&D WP6 project
Wire bond length is crucial for signal integrity at 25 Gb/s data rate
Wide open optical eye diagram at 25.6 Gb/s with fast edges
SystemPIC
DART
Fibers
25.6 Gb/s PRBS7 data
Ring modulator
~ 500 µm
Fiber coupler
CW laser

## Slide 5: PIC Co-Packaging with Timepix4
Proof of concept of PIC co-packaging with particle sensor readout chips (ROCs), to achieving ultimately low-power and reduced mass
It is a paradigm shift respect to the traditional optical module approach, e.g., VTRx+
Saving power for sending and receiving high-speed data streams off-chip over copper traces
Timepix4 post-processed with Through Silicon Vias (TSVs) bonded onto a FR4 carrier board
The SystemPIC optical subassembly was mounted back-to-back with the Timepix4
Wedge wire bonds using 25 µm diameter gold wire
Timepix4
GND
OUT
Ring modulator
Channel 1
Waveguide
Timepix4
SystemPIC
Fibre array

## Slide 6: PIC Design: PIC4links
Design submitted for fabrication through an MPW run in Sept. 2025
To achieve tight integration the PIC must be co-designed with its driver circuit
Pad fame matching the SPRINT for chip-to-chip wire bonding connection
Transceiver chiplet footprint 2.2 mm x 3 mm
PIC4links
SPRINT
2.2 mm
ELS
Tx out
3 mm
Rx in
DC pads for RM
thermal tuning
4 µ-heater and
4 photodiodes
25.6 Gb/s
SPRINT output signals
SiN passband
optical filters
PIC
ELS
Tx channel
Modulator
Fibre coupler
Rx channel
PIC floorplan ≈ 5 mm x 5 mm

## Slide 7: PIC Radiation tolerance - Total Ionizing Dose (TID)
Online dynamic test with VNA
Four ring modulators up to 12 MGy
Electro-optic frequency response up to 25 GHz
Online static test with tunable laser
12 ring modulators up to 12 MGy
I-V curves and spectra
X-ray irradiation facility at CERN

## Slide 8: PIC Radiation tolerance - TID results for ring modulators
Modulation efficiency degradation due to trapped charge in the silicon dioxide
Both charge trapping and annealing are temperature dependent
The possibility of heating up locally the ring modulator allows fast recovery of TID the damage
This thermal annealing mechanism effectively recovers the electro-optic (EO) frequency response from DC to 25 GHz
  These latest results will be presented at RADECS 2025 next week
Low doping
High doping
All high doping
M. Lalović et al., "Ionizing Radiation Effects in Silicon Photonics Modulators," in IEEE Transactions on Nuclear Science, vol. 69, no. 7, pp. 1521-1526, July 2022
M. Lalović et al., "Thermal annealing in silicon photonics ring modulators," in Journal of Instrumentation, vol. 18, no. 3, pp. C03028, Mar 2023

## Slide 9: PIC Radiation tolerance - Displacement Damage
Neutrons beam at the UCL in Louvain la Neuve (BE)
Irradiation of PICs up to 1016 neutron/cm2 fluence
Be target
SystemPIC
PackagingPICs
Deuteron beam
Polarization controllers
O-band laser
Sourcemeters
DAQ
O-band laser controller
Heater power supply
C-band laser
Optical switch
SystemPIC test setup for online data acquisition
Deuteron beam
neutrons

## Slide 10: PIC Radiation tolerance - Neutron Irradiation Results
Moderate ring modulator modulation efficiency degradation up to a fluence of 1016 n/cm2
Negligible degradation of responsivity and I-V characteristic of Ge-photodiodes to fluences above 3·1016 n/cm2
L. Olanterä et al., "Effects of High Fluence Particle Irradiation on Germanium-on-Silicon Photodiodes," in IEEE Transactions on Nuclear Science, vol. 71, no. 4, pp. 728-735, April 2024
L. Olanterä et al., "Effects of High Fluence Neutron Irradiation on
Silicon Photonics Ring Modulators," in RADECS 2024 proceedings, in review.

## Slide 11: Next Steps: Silicon Photonics
System demonstration and design
Evaluation of system-control devices/circuits (temperature, polarisation, wavelength)
Characterise and test PIC4links submitted in Sept. 2025
  Photonic circuits co-designed with the SPRINT, the new modulator driver ASIC instantiated in the Picopix
Radiation Tolerance
  Evaluation of radiation tolerance of waveguide structures
  Continuing the evaluation and modelling of RM radiation eﬀects
Packaging/Integration
  Exploitation of ﬁbre-attachment machine to evaluate prototypes based on ﬁbre edge-coupling
  Evaluation of industry developments in PIC packaging
  Co-packaging the SystemPIC and the next PIC generations with Picopix when it becomes available

## Slide 12
Backup slides

## Slide 13: Resonance wavelength tuning
From 17 °C to 34 °C
Ring modulators are highly selective wavelength filters
Resonance wavelength (λres) influenced by temperature and fabrication
λres needs to be aligned to the input laser
Thermo-optic effect in Silicon to adjust λres (Δλres ~70 pm/°C)
Tungsten µ-heater on top of the ring waveguide for local and active tuning of λres
λres
Input laser
SiO2
µ-heater
Si waveguide
10 µm
input laser
20 µm
Temperature
300 K
400 K

## Slide 14: Control system for wavelength stabilisation
Goal is to build a system that automatically locks the ring to the input laser wavelength
This requires measurement of photodiode average current and steering of heater current
Electrical
Data in
µ-heater
Optical data out
Input laser
Δλ(V)
Photodiode
PID controller
Δλ(T)
Drop port
+
-
error
setpoint

## Slide 15: Proof of concept stabilisation test results
Temperature sweep
Ring modulator test board in a climatic chamber
Control OFF
Wavelength sweep
Tunable laser scan in a wide wavelength range
Control OFF
Control ON
Control ON
The controller keeps the modulator resonance locked to the laser wavelength to produce constant and maximum OMA
Controller concept demonstrated with discrete components
OMA