## Slide 1: Electron gun & collector for the new AD e-cooler Numerical assessment
Teresa Guillen Hernandez
22/05/2025

## Slide 2: Ceramic assessment – bake out
Mesh sensitivity
Chart: Mesh size [mm]
| 3 | 1 | 0.5
250 degrees | 179.55 | 271.78 | 316.65
T room | 56.761 | 107.91 | 107.36
Chart: Mesh size [mm]
| 3 | 1 | 0.5
250 degrees | -167.67 | -231 | -398.59
T room | -49.292 | -88.706 | -123.3
250 °C
T room
Rankine criteria |  | 
 | ⩽ | = 259 MPa
 | ⩽ | = 2900 MPa
Rankine criteria |  | 
 | ⩽ | 
 | ⩽ | 

## Slide 3: Ceramic assessment – bake out
Mesh sensitivity but superficial – filler should absorb this because is very soft
Include Filler in the simulation – 50 microns of very soft material (E=500MPa)
Do a test?
 |  | Step 1 - 250 degrees |  |  | 
 |  | Peak |  |  | 
 | mesh size [mm] | Max ppal stress [MPa] | Variation % Max ppal stress | Min ppal stress [MPa] | Variation % Min ppal stress [MPa]
Softer material | 3 | 55.86 | 68.89 | -46.07 | 72.52
 | 0.5 | 169.27 | 46.54 | -193.57 | 51.44
No filler | 3 | 179.55 | - | -167.67 | -
 | 0.5 | 316.65 | - | -398.59 | -
 |  | Step 2 - Troom |  |  | 
 |  | Peak |  |  | 
 | mesh size [mm] | Max ppal stress [MPa] | Variation % Max ppal stress | Min ppal stress [MPa] | Variation % Min ppal stress [MPa]
Softer material | 3.00 | 11.11 | 80.44 | -27.53 | 44.16
 | 0.50 | 11.88 | 88.94 | -27.53 | 77.68
No filler | 3.00 | 56.76 | - | -49.29 | -
 | 0.50 | 107.36 | - | -123.30 | -