## Slide 1: Target station configuration & Vacuum vessel design study
Gemma Humphreys
18/06/2025

## Slide 2: Introduction
Feedthroughs
FLUKA Differences
Sample Testing
Specification

## Slide 3: Feedthroughs
Feedthroughs brainstorming discussion held in May
Support structure and clamping mechanism proposed
Flexible pipe section
Clamp
Remote Connector Attachment
Possibility to launch a design study covering the connector design, integration with surroundings and leak testing the connection. The full extent of the study is to be clarified.
Support Structure
Flexible Pipe

## Slide 4: FLUKA Differences
Comparison between FLUKA and CATIA being checked
Major differences so far:
Shielding gap next to MHS
Room missing in the CATIA model
Differences in thickness of the proximity shielding and slight positional differences
Floor height differences
More Differences to be identified

## Slide 5: Vacuum Vessel Door Seal Sample Testing
Samples to be irradiated at n_TOF under compression (10% compression rate)
3 irradiation containers, 3 dose rates (1,2,3 months)
  6 O rings
  12 Round samples
Tests to be conducted:
Leak Test (O-rings)
Compression
Tensile Strength
Weight loss
Elongation at break
Round Samples 13mmø 6mm thickness
3 materials
  1 EPDM
  2 silicon rubber
4 samples per material
O Rings 20mmø 3mm thickness
3 materials
  1 EPDM
  2 silicon rubber
2 samples per material
83.5mm

## Slide 6: Leak Testing
Technetics to develop a leak test rig for the O ring seals
Vacuum pump to direct helium to 1 seal and use mass spectrometer to measure any leaks

## Slide 7: Vacuum Vessel Specification
Specification almost complete
Aim to be finished by end of June
Finalising and checking being completed currently

## Slide 9
Vacuum vessel finishes 93mm before
MHS shielding 87mm closer to target than should be
Rear shielding 49.5mm further forward
Proximity shielding 900mm thick instead of 550mm
Shielding 855mm thick instead of 695mm
Shielding 530mm thick?, should be 600mm
Shielding 190mm longer

## Slide 10
374mm offset of shielding pit
610mm Floor height offset
810mm Floor height offset
2.6m experiment finishing difference?