## Slide 1: Nb3Sn Strand Trilogy
10.06.2025
M. Wozniak
Conductors for protection – Nb3Sn WP4.5-T2-D1

## Slide 2: The trilogy
Magnetization
Jc scaling
AC loss
For each:
Progress
Issues
Next steps
Key paper conclusion

## Slide 3: Magnetization - progress
Measurements:
done for MQXF strand at 2mm / 8 turns sample
sample volume calculated and understood from linear density
Simulations:
4.2 K sim with coarse mesh and guessed Jc(B, T) – next slides
Wire size and area corrections are still needed – next slides

## Slide 4: Digitized cross-sections (to be used across all 3 papers)
Measured values 1) -> |  | n/a | 0.8523 | 1.1455 | n/a
Geometry ID | Date | Number of points | Wire diameter | Cu/NonCu ratio2) | Cu/Layer ratio2),5)
0 | 2024.11.19 | older files not checked |  |  | 
1 | 2025.05.15 | 2243 | 0.852393 | 1.236884 | 1.67188
2 | 2025.05.21 | 2246 | 0.871926 | 1.225278 | 1.65317
3 | 2025.06.04 | 5091 | 0.8719263) | 1.1705534) | 1.56585
1) Simon’s email on 14.05.2025, 2) Neglecting diffusion barriers areas,
3) 2.3% above measured, 4) 2.7 % above measured,
5) This ratio is used for Jc,layer which is used directly in the simulation.

## Slide 5: Jc scaling guess – transport
Tc0: 17.7234 K (vs 16.25 K)
Bc20: 28.9113 T (vs 29.56 T)
C0: 225615879888 AT/m²
(vs: 220303000000)
Used fit in Simon’s presentation:
https://indico.cern.ch/event/1510243/
(numbers in brackets are Simon’s for MQXF)
With self-field correction as in the transport data
α | 1
ν | 1.52
p | 0.5
q | 2
Transport data from Joanna, no idea if this is the same strand
Calculated with Cu/noCu ratio: 1.2381 (vs 1.2)
Geometry data has these ratios:
(without accounting for diffusion barriers area)
Cu/noCu ratio: 1.236884
Cu/Layer: 1.67188
For Jc,layer (which is used in the simulations):
C0: 279709748639 AT/m²

## Slide 6: Extracting Jc from magnetization at 4.2 K
C0 = 279709748639 A T/m²
Bc20 = 28.9113 T
Tc0 = 17.7234 K
Jc = 5422147073 A /m² at B=10.0 T and T=4.25 K
d_eff for layer Jc and rod (circular) filaments is 25.99 um
delta_M (mT) = 4 / (3 * π) * d_eff * Jc * mu0

## Slide 7
Exact ramping scheme used in simulation
Sample does not appear to be field cooled (it is not in virgin state).
Is it possible to warm up above Tc before ramp?
Alternatively, we can simulate ‘from non-virgin state’.
Measurement volume normalization:
M(emu/cm³)/ Volume (cm³)
M(A/m) M(emu/cm³) *1000
Simulations volume normalization:
m(A m) – magnetic moment is direct output of sim.
M(A/m) = m(A m)/filaments_area
Dividing by filaments area as this area is what the Jc is normalized to
Volume = 0.04225 cm³ (sample volume from linear density)
The lower the field the worse is the agreement.
Still a bit off at 10 T, wrong wires size?
Need to correct the Jc scaling to make this match.
Still some thinking required.

## Slide 8: Magnetization – Next steps
Measurements:
Is more MQXF wires to be measured at at different geometry?
PIT to be measured?
Simulations:
Need to still correct the wire diameter and Cu/NonCu ratio
Jc (B, T) – low filed scaling needs an update
Mesh sensitivity (in progress)
Disable CATI coupling as it has no impact for low ramps (speed up)
Simulations for all measured temperatues
Transition from Mariusz to Josef running sims

## Slide 9: Magnetization – key paper conclusions
Some ideas:
Validation of simulation and model inputs for exact geometry and layer Jc.
Obtain Jc magnetization from magnetization measurement in as corrected way as possible (preliminary using the simple formula is wrong). This is to be used in Jc scaling paper.
Comparison of magnetization for more geometries (all undeformed):
  Exact geometry – with filament holes (i.e. using layer Jc)
  Exact geometry – filled filament (i.e. using nonCu Jc)
  The two above cases, but for hex (ideal) filaments
  As above but for round filaments
Discussion of the meaning of deff as geometrical quantity and how does it compare to the diameter of filaments in the above cases
Deformed geometry magnetization simulation – how much different is it (need for additional exact deformed geometry if this is in scope)?
Direction of applied filed (strands are not rotationally symmetric), so this already has impact on the simulated result and it would be nice to discuss it. Simulations at varying angle of applied field are possible. In the measurement it is averaged for twisted strand.

## Slide 10: Jc scaling - progress
Need more work for getting magnetization simulation and measurement to agree. This will give the Jc based on magnetization at low field.
Do we simply tweak the pinning parameters (p and q) or introduce additional term in the equation?

## Slide 11: Jc scaling – next steps
Need transport data for the same spool as magnetization
Need to align transport data and magnetization data and wire cross-sections.
We can simulate E-I curves to match transport data if available.
Do we work ‘only’ on RRP or also on PIT?
The self-field correction for Jc in transport measurements seems to be done with peak B. Are we sure this is correct? (sorry, a bit off topic)

## Slide 12: Jc scaling – key paper conclusions?
New fitting parameters/equation valid for low field
Show the methodology of how the fit was obtained with supporting transport and magnetization data. Rely on magnetization paper for the Jc magnetization.

## Slide 13: AC loss - progress
Mesh sensitivity study for 5 T DC, 50 mT AC, and 50, 500 and 1500 Hz, with geometry “3”
As expected, the hysteresis loss is the most sensitive to mesh size
50 Hz
500 Hz

## Slide 14: AC loss - progress
1500 Hz
Other loss components less sensitive to mesh

## Slide 15: AC loss - progress
Mesh 13 – too coarse
Mesh 14 – just about fine
Note:
For mesh 14 there is good match of points spacing to mesh size.
No penalty at the solution level for using 5091 points to resolve geometry “3”

## Slide 16: AC loss – progress – global diffusion barrier added to CATI model capability
This functionality is needed for PIT
It allows discontinuity of coupling currents and should affect AC loss vs frequency
After update of PIT geometry a reference solution will give the first idea of how important this is.

## Slide 17: AC loss - issues
Only preliminary result run as many things are still off in the inputs
Need to correct for diffusion barrier area. They are not present in the geometry but define as line with thickness. Surface of the barriers accounts for 3.34 % of total wire cross-section. Is this value expected from the wire design? How is the thickness calculation done?
What is the resistivity of diffusion barriers around filament and global for PIT?
What do we know about Cu RRR distribution in the wire cross-section (RRP and PIT)?
Could we introduce at the digitized geometry an additional region around filaments for RRP for which we assign lower RRR?
Need corrected dimensions and Cu/NonCu for PIT digitized strand

## Slide 18: AC loss – next steps
Work on magnetization and Jc scaling first as otherwise the AC loss hysteresis part (dominant in many cases) is going to be wrong
Measurement at 4 BDC, 4 B AC and 10 frequencies – agree with Arend what they will be and launch ‘reference’ simulations
Adjust material properties to see how sensitive the results are to RRR of Cu and diffusion barriers resistivity
Arrange a visit to Twente to participate in measurements – tbc.

## Slide 19: AC loss – key paper conclusion steps
Reference AC loss for RRP and PIT wires as measured
Validation of model inputs to best match the measurements
With validated inputs, computation of full amplitude and frequency loss map for the two wires
Discussion of key loss components for AC loss-based protection