## Slide 1: Rutherford cable development status and plans
J. Fleiter, A. Bonasia and T. Boutboul
26 June 2025 2nd FCC-hh MQ project meeting https://indico.cern.ch/event/1560951/

## Slide 2
Cable specification EDMS 3224233
First Cu unit length of cable produced in April 2025
  Cable ID C09UC0506A ~270 m long
  Conform to specification
  Tooling’s for cabling validated
Cabling trials with Nb3Sn wire foreseen in August 2025
Cabling of 5 Nb3Sn UL of 60 m foreseen in August 2025