## Slide 1: Fabrication Techniques for RF Cavities
2025-07-15
CERN-CODELCO Copper Mini-workshop
Marco GARLASCHÈ
On behalf of CERN FCC SRF R&D Project

## Slide 3: FCC Collider – 400 MHz Cavity System
Superconducting elliptical cavity
400 MHz, 2-cell
Copper substrate, Nb layer
264x
700mm
1400mm
Typical Cavity Subcomponents
…Flanges, Beam pipes , Extremities,…
…Half-cells, cells…
400 MHz – LHC type
≈>100kg

## Slide 4: Core Technologies:

## Slide 5: Core Technologies: Shaping
Metal Sheet Shaping
High precision shaping (≈ 0.3 mm)
Ultra high precision Edge Calibration (≈0.1mm)
Spinning
Deep Drawing
Rolling &
(Press)Bending

## Slide 6: Core Technologies: Shaping
Metal Sheet Shaping
High precision shaping (≈ 0.3 mm)
Ultra high precision Edge Calibration (≈0.1mm)
Spinning
Deep Drawing
Rolling &
(Press)Bending
Hydroforming
Open Die

## Slide 7: Core Technologies: Machining
CNC Turning and Milling
Both on bulk parts & on metal sheet shapes
Machining Copper at different tempers (Half-hard, Annealed)
Both lubricated and dry (alcohol, …UHV compatibility)
High precision (finishing ≈ 0.02 mm)
Milling for elliptical cavities : 3x Axis sufficient

## Slide 8: Core Technologies: Joining
Main Features of interest:
Join dissimilar materials &/OR not possible to weld (Cu-SS, ceramic)
NO welding shrinkage/fusion deformation of base materials
Process under vacuum  good protection against oxidation
Complex & inaccessible geometries
Main Features of interest:
Process under vacuum  good protection against oxidation
Very high energy density  low distortion
Large range of weldable thicknesses (from 0,1mm to 200mm)
Many combination possible (Nb/Cu, Cu/SS, Al/Cu,…)
Gun column diagram
EB weld on 12 mm Ti gr.5
Vacuum Brazing
Electron Beam Welding
For both processes: High purity Copper requirement

## Slide 9
400 MHz SRF Cavity Fabrication Route

## Slide 10: Extremity Pipes
Alternative to raw sheet : ‘’standard’’ tubes
Alternative to necking : thicker tube (or cored rod)  Machined
Cu Raw material : Thin Sheet (~4mm)
Processes: Bent, Machined, EB-welded, Calibrated, Re-machined
Necking

## Slide 11: Flanged Connections
Cu Raw material : as per extremities
Alternative : bulk from rod/thick sheet
Processes:
Machined, Brazed, Re-machined
EBW of Flanged Connections & pipes…
… Extremity subcomponents  Beam Pipes

## Slide 12: The Cells
Cu Raw : thin sheet
Cu Raw : thick tube
Calibration
Machining
Remachining
EB Welding
Half-Cells
Intermediate Stress Relief

## Slide 13: Final EB welding Steps
LHC 400 MHz cavity
Iris electron beam weld with inner deflector
RF side internal weld

## Slide 14: Additional Technologies
Additional Core technologies involved in manufacturing:
Precision Metrology and NDT
Surface treatments
  Degreasing, Cu chemical etching
  (Electropolishing, Nb sputtering)
Manufacturing SRF components calls for strongly Interlaced and Multi-technology production
What goes Hand-in-hand ?
  Shaping + Machining
  Surface treatments + Joining

## Slide 15: SRF Complementary Systems
Additional equipment required:
Fundamental Coupler (1x per cavity)
HOM Couplers/Antennas (few per cavity)
Core Technologies :
All the ones mentioned (machining > shaping)
Raw Material:
Bulk (rods, discs), thin sheet
~700mm
Beam
Screens
2025-07-15
M. Garlaschè [CERN EN-MME] | CERN-CODELCO Meeting

## Slide 16: Additional Systems : Cu Requirements
Subsystem | Quantity [tons, order of magn.] | Type
Magnets | Cu OFE : 4400 | Hollow conductors
Vacuum Equipment collider chambers + relative interconnections cooling channels + booster chamber photon absorbers + internal shielding flanges | Cu OFS : 1000 Cu OFE : 577 CuCrZr : 680 CuNiCrSi o CuBe : 50 | Sheets, rods, bulk
RF systems FCC Injector | Cu OFE : 285 | Sheets, rods, bulk
Additional Copper & Alloys will be required, for FCC subsystems other than SRF
Source : S. Calatroni , A. Milanese, D. Schoerling, M. Morrone, A. Grudiev
2025-07-15
M. Garlaschè [CERN EN-MME] | CERN-CODELCO Meeting

## Slide 18: Back up – Crossectional view

## Slide 20: EN-MME: Mechanical & Materials Engineering Group
Engineering & Design
Fabrication
Materials & Metrology
Design Office:
  40+ designers and engineers
  CATIA / SmarTeam, ANSYS, LS-Dyna...
Experimental Mechanics Lab.
Mechanical workshop (4000 m2):
  ~100 technicians and engineers
  CNC machining
  Assembly & metal forming
  Welding (TIG, MIG, electron beam, laser, vacuum brazing)
Technical Subcontracting Service (MME-FS)
Material science consultancy:
  metallurgical analyses, microscopy, mechanical tests
NDT: US, radiography, tomography
Metrology: 350 m2 lab. equipped with CMM.

## Slide 21: Hydroforming : Further Info
09/04/2025
Annealing
2ND hydroforming
HF2
1ST hydroforming
HF1
09/04/2025
Process design
Testing
Process control
Hydroforming : process under study for FCC 400 MHz
No equatorial weld seam